	PLASTIC  PRODUCTS

	Sl. No.
	Export Item
	Quantity
	      Import Item
	Qty. Allowed


	H1
	35 mm Perforated Positive Film Rolls
	100 sq.mtrs.
	1
	
	Unexposed Positive jumbo Rolls
	103.45 sq.mtrs.

	H2
	ABS Beautycase Size : 15"
	1 No.
	1
	
	A.B.S. Film
	1.05 Sq.mtr/ 115 Sq.meter content in export.

	
	
	
	2
	
	Aluminium
	1.05 kg/kg content in export.

	
	
	
	3
	
	Polypropelene
	1.05 kg/kg content in export.

	
	
	
	4
	
	Lining(Polyester)
	1.05 kg/kg content in export.

	
	
	
	5
	
	Side Lock
	Net to net.

	
	
	
	6
	
	L.D.P.E.
	1.05 kg/kg content in export.

	
	
	
	7
	
	PVC
	1.05 kg/kg content in export.

	H3
	ABS Briefcases/ Suitcase/ Beautycases with/ without Aluminium Frame of all sizes
	1 No.
	1
	
	ABS Moulding Powder/Granules
	1.10 kg/kg content in export.

	
	
	
	2
	
	LDPE Moulding Powder/Granules
	1.05 Kg/kg content in export

	
	
	
	3
	
	Polypropylene Moulding Powder/Granules
	1.05 Kg/kg content in export

	
	
	
	4
	
	Aluminium Sheet/Strips
	1.05 Kg/kg content in export

	
	
	
	5
	
	PVC Compound
	1.05 Kg/kg content in export

	
	
	
	6
	
	ABS/PVC/Acrylic Film
	1.10 kg/kg content in export.

	
	
	
	7
	
	Combination Lock/Number Lock/Side Lock and parts thereof
	Net to Net

	
	
	
	8
	
	Relevant Lining (Rayon/Polyester/Nylon)
	1.10 Sq.Mtr./Sq.Mtr. content in export

	
	
	
	9
	
	Carrying Handle
	Net to Net

	
	
	
	10
	
	Handle Lugs
	Net to Net

	
	
	
	11
	
	Pulling Handle
	Net to Net

	
	
	
	12
	
	Granules of relevant Nylon Chips for manufacture of Frame/Moulded Components
	1.05 kg/kg content in export

	
	
	
	13
	
	Glue Foil
	1.05 kg/kg content in export

	
	
	
	14
	
	Hot Melt Glue
	1.02 kg/kg content in export

	
	
	
	15
	
	Kraft Paper/Board for Lining/Divider
	1.05 kg/kg content in export.

	
	
	
	16
	
	Fibre/Chip Board
	1.05 kg/kg content in export.

	
	
	
	17
	
	Relevant Metallic/non-Metallic Components
	Net to Net

	
	
	
	18
	
	Extruded Flexible Plastic Profiles
	1.02 Mtr/Mtr content in export.

	
	
	
	19
	
	Relevant Zip Fastener
	Net to Net

	Note: In case of export of coloured items, the relevant colour Master Batch are allowed as an input @0.02 Kg/kg weight of Polymer. In case Colour Master Batch is imported, then relevant Polymer at Sl.Nos.1,2 & 3 will be reduced to 1.03 kg/kg content in export product.

	H4
	ABS Resin/Granules (Based on Bulk/Mas Polymerization Process)
	1 MT
	1
	
	Styrene
	691.10 kgs

	
	
	
	2
	
	Acrylonitrile
	218.00 kgs

	
	
	
	3
	
	Poly Butadiene Rubber
	100.4 kgs

	
	
	
	4
	
	Ethyl Benzene
	11.80 kgs

	
	
	
	5
	
	Tert. Butyl Peroxy Benzonate(TBPB)
	0.34 kg

	
	
	
	6
	
	Trinonyl Phenyl Phosphite
	4.23 kgs

	
	
	
	7
	
	Irgonox
	1.6 kg

	
	
	
	8
	
	Dioctyl Phthalate
	12.09 kgs

	H5
	ABS Resin/Granules (Injection Moulding Sheeting Grade)
	1 MT
	1
	
	Styrene
	639 kg

	
	
	
	2
	
	Acrylonitrile
	271 kg

	
	
	
	3
	
	Butadiene
	190 kg

	
	
	
	4
	
	Oleic Acid or Distilled Fatty Acid
	21 kg

	
	
	
	5
	
	Teritary Dodecyl Mercaptan/Normal Dodecyl Mercaptan
	7 kg.

	
	
	
	6
	
	Potassium Persulphate
	5 kg.

	
	
	
	7
	
	Disprosin / Rosin
	25 kg.

	
	
	
	8
	
	Ethylene Bis-stearamide
	25 kg.

	
	
	
	9
	
	Antioxidant (OBP/Sumilizer/DTDTDP/DBP/TNPP/BHT/Irgonox-1076)
	31 kg.

	
	
	
	10
	
	Pigment/ Titanium Dioxide/Relevant Colour Master Batch
	20 kg.

	
	
	
	11
	
	Stearic Acid
	3 kg.

	
	
	
	12
	
	Palmitic Acid
	2 kg.

	Note: 1. The import of item Nos.11 & 12 may be allowed for the export of ABS Resin (Sheetings Grade) and item No. 10 may be reduced to 15 kgs instead of 20 kg per ton export. 
Note: 2. For the export of ABS Resin/Granules (Injection Moulding Grade) item No. 11 & 12 may not be allowed for import.

	H6
	ABS Resin/Granules(Based on Emulsion Polymerization Process)
	1 MT
	1
	
	Acrylonitrile
	168.13 kg

	
	
	
	2
	
	Butadiene
	217.37 Kgs.

	
	
	
	3
	
	Styrene
	410.17 Kgs

	
	
	
	4
	
	Styrene Butadiene latex (100% basis)
	13.15 Kgs.

	
	
	
	5
	
	Styrene Acrylonitrile Resin
	265.0 Kgs.

	
	
	
	6
	
	Cumene Hydroperoxide
	2.33 Kgs.

	
	
	
	7
	
	N.N. Diethylhydroxylamine
	0.03 Kg.

	
	
	
	8
	
	2,2, Methylene Butyl Phenol
	0.38 Kg.

	
	
	
	9
	
	Octadecil Butyl Propionate
	0.76 Kg.

	
	
	
	10
	
	Rosin
	25.33 Kgs.

	
	
	
	11
	
	Tetra Sodium Phosphate Anhydride
	1.43 Kgs.

	
	
	
	12
	
	Tertiary Dede - cycle Mercaptan
	3.65 Kgs.

	
	
	
	13
	
	N-N, Ethylene Bisstearmide
	6.68 Kgs.

	
	
	
	14
	
	Distearyl Pentaerythritol Diphosphate
	0.22 Kg

	
	
	
	15
	
	Pigment/ Titanium Dioxide/ Master Batch (for coloured ABS Resin/Granules)
	24.34 Kgs.

	H7
	Acrylic Pellets (Poly Methyl Methacrylate)
	1 kg.
	1
	
	Methyl Methacrylate Monomer
	0.929 kg

	
	
	
	2
	
	N-Octyl Mercaptan
	0.002 kg

	H8
	Acrylic Polymer Emulsion (Thickner) (Solid content 38-40%)
	1 kg
	1
	
	Acrylamide
	0.147 kg

	
	
	
	2
	
	Acrylic Acid
	0.182 kg

	
	
	
	3
	
	Solvent Oil
	0.293 kg

	
	
	
	4
	
	Emulsifier/Speciality Monomers
	0.074 kg

	H9
	Acrylic Resin Binder(R-7000) Total Solid content 28-30%
	1 kg
	1
	
	Acrylic Acid
	0.0043 kg

	
	
	
	2
	
	Butyl Acrylate Monomer
	0.172 kg

	
	
	
	3
	
	Styrene Monomer
	0.095 kg

	
	
	
	4
	
	Emulsifiers/ Speciality Chemicals
	0.020 kg

	H10
	Acrylic sheet -Diecast
	1 kg
	1
	
	Methyl Methacrylate Monomer
	1.13 kg

	
	
	
	2
	
	Aso-bis-iso butyronitrite
	0.0066 kg

	
	
	
	3
	
	Pigment
	0.0204 kg

	H11
	Acrylic sheet Centrifugal Cast
	1 kg
	1
	
	Methyl Metha crylate Monomer
	1.1 kg

	
	
	
	2
	
	Aso-bis-iso butyronitrite
	0.006 kg

	
	
	
	3
	
	Pigment
	0.0184 kg

	H12
	Acrylic sheet Extruded
	1 kg
	1
	
	Acrylic Resin
	1.0333kg

	H13
	Acrylic Tray with Relevant Fabric/with Decorative Foil/with PVC Printed Film/with Brass Fittings
	1 kg
	1
	
	Acrylic Sheets/off Cuts
	1.10 kg/kg content in the export product.

	
	
	
	2
	
	Relevant Fabric
	1.10 kg/kg content in the export product.

	
	
	
	3
	
	PVC Printed Films
	1.10 kg/kg content in the export product.

	
	
	
	4
	
	Decorative Foil (Relevant)
	1.00 kg/kg content in the export product.

	
	
	
	5
	
	Brass Scrap
	1.075 kg/kg content in the export product.

	
	
	
	6
	
	Printing Ink
	0.001 kg

	
	
	
	
	
	
	

	H14
	Acrylonitrile monomer 99.9% minimum
	1 kg
	1
	
	Ammonia 100%
	0.5567 kg

	
	
	
	2
	
	Prophlone 100%
	0.1300 kg

	
	
	
	3
	
	Catalyst 41 or 49
	0.1321 kg

	
	
	
	4
	
	Hydroquinone Tech
	0.3812 kg

	H15
	Additive Master Batches
	1 kg
	1
	
	Relevant Polymers such as Polyethylene, Polypropylene, Polystrene, Polyester (PET/PBT),EVA
	1.03 kg/kg content in the export product

	
	
	
	2
	
	Relevant Additive i.e. 
a) U V Stabilizer 
b) Anti Block Agent 
c) Antistatic Agent 
d) Slip Agent 
e) Antioxidant
	1.03 kg/kg content in the export product

	Note: The additives indicated at import item 2 will not be more than 20% (by weight) of export and only relevant additives as required/ used in the export product should be allowed for import.

	H16
	Deleted
	
	
	
	
	

	H17
	Adhesive coated PVC furniture film with PVC film weighing 143 gms/sq.mtr and base paper with adhesive 100 gms/sq.mtr +/- 5%
	1000 sq.mtrs
	1
	
	PVC Resin
	82.23 kgs

	
	
	
	2
	
	PVC Plasticiser
	57.56 kgs

	
	
	
	3
	
	PVC Stabilizer
	7.40 kgs

	
	
	
	4
	
	Titanium Dioxide/Pigments
	2.30 kgs

	
	
	
	5
	
	UV Stabilizer
	0.16 kg

	
	
	
	6
	
	Processing Aid
	9.87 kgs

	
	
	
	7
	
	Impact Modifier
	4.93 kgs

	
	
	
	8
	
	Solvent (MEK/MIBK/Toluene Cyclohexanone)
	25.00 kgs

	
	
	
	9
	
	Adhesive (total Solid contents 100% basis)
	28.6 kgs

	
	
	
	10
	
	Silicon Coated Release Paper (73-75 gms/sq.mtr)
	1100 sq.mtrs
(81.4 kgs)

	
	
	
	11
	
	Polypropylene Film
	1.02 kg/kg content in export product.

	Note: In case of variation in the weight of PVC Film, item no. 1 to 7 may be allowed to be imported proportionately as per following formula:
A x B/143
where A = Quantity allowed for 143 kgs of PVC Film
B = Weight of PVC Film to be exported.

	H18
	All Plastic (PVC) Playing Cards packed in relevant Plastic Cases
	1 kg
	1
	
	Rigid PVC Sheet Opaque Antistate Treatment
	1.22 kg/kg content in export product

	
	
	
	2
	
	High Impact Polyestyrene Granules
	1.05 kg/kg content of the relevant material in the export packing.

	
	
	
	3
	
	Ultraviolet Ink off set printing
	1.5% of weight of Rigid PVC Sheet in export.

	
	
	
	4
	
	U.V. Coating (Acrylic)
	2% of weight of Rigid PVC Sheet in export.

	
	
	
	5
	
	Photo Polymers Relief Images Plates
	1 No. per colour in the design.

	
	
	
	6
	
	Printers Rubber Blankets Thickness 1.9 mm +/-5%
	0.006 Sq.Meter per 28 packs of PVC Playing Cards

	H19
	Anion Exchange Resin
	1 kg
	1
	
	Styrene
	0.435 kg

	
	
	
	2
	
	Divinyl Benzene Monomer
	0.030 kg

	
	
	
	3
	
	Ethylene Dichloride
	0.975 kg

	
	
	
	4
	
	Polyvinyl Alcohol
	0.1755 kg

	
	
	
	5
	
	Methanol Formaldehyde Solution
OR
	0.788kg

	
	
	
	5
	a)
	Methanol
	0.448 kg

	
	
	
	
	b)
	Paraformaldehyde
	0.330 kg

	
	
	
	6
	
	Dimethyl Ethanol Amine
	0.275 kg

	H20
	Anionic Polyacrylamide Emulsion (Total Solid content 38-40%)
	1 kg
	1
	
	Acrylamide
	0.251 kg

	
	
	
	2
	
	Acrylic Acid
	0.136 kg

	
	
	
	3
	
	Solvent Oil (Paraffinic Solvent)
	0.286 kg

	
	
	
	4
	
	Emulsifiers
	0.085 kg

	
	
	
	5
	
	Speciality Chemicals and Monomer
	0.006 kg

	H21
	Articles made of ABS
	1 kg
	1
	
	ABS Resin Powder/Granules
	1. 050 kg/kg content in export

	H22
	Articles made of ABS with Metallic/ Non-metallic components
	1 kg
	1
	
	ABS Moulding Powder/ Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Metallic Components used during insert moulding
	Net + 2% wastage.

	
	
	
	3
	
	Metallic/Non- Metallic Components
	Net + 1% wastage.

	H23
	Articles made of HDPE
	1 kg
	1
	
	HDPE Granules
	1. 050 kg/kg content in export

	H24
	Articles made of HDPE/PP twine/ Rope OR Articles made of blend of HDPE&PP Twine/Ropes
	1 kg
	1
	
	Relevant HDPE/PP Granules/ Chips
	1.08 kg/kg content in the export product.

	Note : 1. The relevant HDPE & PP Granules may be allowed as 1.08 kg/kg content in the export product both for exclusive Articles made of HDPE/PP Twine/Ropes and for Articles made of blended HDPE & PP Twine/Rope on the actual net content of that relevant polymer i.e. HDPE or PP in the blended export product. 
Note : 2. In case of coloured export items, the relevant Colour master Batch shall also be allowed as an additional input @ 0.02 kg/kg weight of relevant polymer and accordingly the quantity of relevant polymer i.e. HDPE/PP shall be reduced to 1.06 kg/kg content in the export product.

	H25
	Articles made of LDPE/ LLDPE
	1 kg
	1
	
	Relevant LDPE/LLDPE Granules
	1.050 kg/kg content in export

	H26
	Articles made of Nylon 6
	1 kg
	1
	
	Nylon 6 Chips/Granules
	1. 050 kg/kg content in export

	H27
	Articles made of Nylon 66
	1 kg
	1
	
	Nylon 66 Chips/Granules
	1. 050 kg/kg content in export

	H28
	Articles made of Polycarbonate
	1 Kg
	1
	
	Polycarbonate Resin/ Moulding Powder/ Granules/ Compound
	1.05 Kg/Kg content in export

	H29
	Articles made of Polycarbonate with Metallic/ Non-metallic components
	1 kg
	1
	
	Polycarbonate Resin/ Moulding Powder/ Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Metallic Components used during insert moulding
	Net + 2% wastage.

	
	
	
	3
	
	Metallic/Non- Metallic Components
	Net + 1% wastage.

	H30
	Articles made of Polypropylene
	1 kg
	1
	
	Polypropylene Granules
	1. 050 kg/kg content in export

	H31
	Articles made of Polystyrene
	1 kg
	1
	
	Relevant GPPS/HIPS Granules
	1. 050 kg/kg content in export

	H32
	Articles made out of Acrylic sheet/off cuts
	1 Kg
	1
	
	Acrylic Sheet/Off cuts
	1.05 Kg./kg. content in export

	H33
	Articles such as Junction boxes with lids, switch and socket boxes, saddle clips, bends, circular boxes, courlers, adaptor boxes, lids, bushes, shrouds, looping boxes, clips, trunkings, ovals, conduits, covers, connectors, pipes,pattress, bush adaptors, space bar saddle etc., made out of PVC
	1 kg
	1
	
	PVC Resin
	0.84 kg

	
	
	
	2
	
	Impact Modifier
	0.021 kg

	
	
	
	3
	
	Stabilizer/Heat Stabilizer (other than Tin Based)
	0.017 kg

	
	
	
	4
	
	Flow Promotor
	0.0252 kg

	
	
	
	5
	
	Plasticizers (in 37)
	0.00837 kg

	H34
	Asbestos Tape
	1 kg
	1
	
	Asbestos Fibre of Relevant Grade
	1.05 kg

	H35
	Biaxially Oriented Poly- propylene Self Adhesive Tapes in width upto 3"
	1 Sq. Mtr.
	1
	
	Biaxially Oriented Polypropylene Gummed Film in Jumbo Rolls
	1.05 Sq.Mtr.

	
	
	
	2
	
	Kraft Paper
	1.05 kg/kg content in the export product.

	Note: For the export of the above resultant product of above 3 inch and upto 8 inch size, import item at Sl. No. 1 with 2% wastage may be allowed.

	H36
	Bicycle Helmet made of Polystyrene
	1000 Nos. (Net weight 0.301 Kg and gross weight per helmet 0.67 Kg.)
	1
	
	Polystyrene Granules
	137 Kgs.

	
	
	
	2
	
	Polyamide (Nylon) Granules
	28 Kgs.

	
	
	
	3
	
	ABC Graules
	79 Kgs.

	
	
	
	4
	
	Cynoacralate Adhesive
	3 Ltrs.

	
	
	
	5
	
	Stickers
	1050 Sets

	
	
	
	6
	
	Laminated Cloth
	73 mtrs. width

	
	
	
	7
	
	Packing Material:-
	

	
	
	
	
	a)
	HDPE/ LDPE/ Polypropylene of each item
	1.05 Kg/Kg. content of each item in the export product.

	
	
	
	
	b)
	Card Board
	1.05 Kg./Kg.content in the export product

	
	
	
	
	
	
	

	H37
	Black Compound Polyethylene Copolymer Granules for Cabled Jacket containing minimum 94+/-1% LDPE and 2.5+/-0.5% Carbon Black
	1 MT
	1
	
	LDPE Granules
	0.9662 MT

	
	
	
	2
	
	EVA Copolymer Granules
	0.0368 MT

	
	
	
	3
	
	Phenolic Antioxidant
	0.0019 MT

	
	
	
	4
	
	Carbon Black (Grade Furnace Black)
	0.0256 MT

	H38
	Black Master Batches
	1 kg
	1
	
	Relevant Polymers such as Polyethylene, Polypropylene, Polystrene, Polyester (PET/PBT), EVA
	1.04 kg/kg content in the export product.

	
	
	
	2
	
	Carbon Black
	-do-

	
	
	
	3
	
	Relevant fillers such as calcium carbonate
	-do-

	H39
	Blend of aromatic polyester polyol, amino polyols with blowing agents,catalyst, surfactants and additives PE 7060 BF
	100 kgs.
	1
	
	Phthalic Anhydride
	21.53 kgs

	
	
	
	2
	
	Diethanol Amine
	9.93 kgs

	
	
	
	3
	
	Diethylene Glycol
	32.90 kgs

	
	
	
	4
	
	Nonyl Phenol
	7.71 kgs

	
	
	
	5
	
	Trichloro fluoro methane
	10.65 kgs

	
	
	
	6
	
	Silicone Surfactant
	1.06 kg

	
	
	
	7
	
	Dimethyl cyclo hexyl amine
	0.81 kg

	
	
	
	8
	
	Glycerine
	2.15 kgs

	
	
	
	9
	
	Trichloro Ethyl Phosphate
	3.95 kgs

	H40
	Blend of aromatic polyester polyol, amino polyols with blowing agents,catalyst, surfactant and additives PE 7060 B
	100 kgs
	1
	
	Phthalic Anhydride
	22.41 kgs

	
	
	
	2
	
	Diethanol Amine
	10.35 kgs

	
	
	
	3
	
	Diethylene Glycol
	34.26 kgs

	
	
	
	4
	
	Nonyl Phenol
	8.03 kgs

	
	
	
	5
	
	Trichloro Fluoro Methane
	11.90 kg

	
	
	
	6
	
	Silicone Surfactant
	1.15 kg

	
	
	
	7
	
	Dimethylcyclohexyl amine
	0.85 kg

	
	
	
	8
	
	Glycerine
	2.24 kgs

	H41
	Blend of aromatic polyester polyol, amino polyols with blowing agents, catalyst, surfactants and additives PE 7040 BF
	100 kgs
	1
	
	Phthalic Anhydride
	19.95 kgs

	
	
	
	2
	
	Diethanol Amine
	9.66 kgs

	
	
	
	3
	
	Diethylene Glycol
	30.50 kgs

	
	
	
	4
	
	Nonyl Phenol
	7.93 kgs

	
	
	
	5
	
	Trichloro fluoro methane
	17.90 kgs

	
	
	
	6
	
	Silicone Surfactant
	0.97 kg

	
	
	
	7
	
	Dimethyl cyclohexyl amine
	0.75 kg

	
	
	
	8
	
	Glycerine
	1.99 kgs

	
	
	
	9
	
	Trichloroethylphosphate
	3.65 kgs

	H42
	Blend of aromatic polyester, polyol, amino polyols with blowing agents, catalyst, surfactants and additives PE 7040 B
	100 kgs
	1
	
	Phthalic Anhydride
	20.71 kgs

	
	
	
	2
	
	Diethanol Amine
	10.03 kgs

	
	
	
	3
	
	Diethylene Glycol
	31.66 kgs

	
	
	
	4
	
	Nonyl Phenol
	8.35 kgs

	
	
	
	5
	
	Trichloro Fluoro Methane
	10.46 kgs

	
	
	
	6
	
	Silicone Surfactant
	1.06 kg

	
	
	
	7
	
	Dimethyl cyclo hexyl amine
	0.77 kg

	
	
	
	8
	
	Glycerine
	2.06 kgs

	H43
	Blood Administration Set with HD Filter, one end having 18 G Needle (Net weight 40 gms each)
	100 Nos.
	1
	
	Poly Vinyl Chloride, Non-Toxic Medical Grade, Soft PVC Compound
	1.05 kg/kg content in export product.

	
	
	
	2
	
	Acrylonitrile Butadiene Styrene (ABS)
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Unsterile Needle SS 18 G x 1-1/4" Length
	101 Nos./100 Nos. in the export product.

	
	
	
	4
	
	Nylon Filter Cloth 15 Micron
	1.01 Sq.Cm/ Sq.Cm Filter Cloth

	H44
	Blood Donor Set Tubing having both side Needle (Net weight 32 gms each)
	100 Nos.
	1
	
	Poly Vinyl Chloride, Non-Toxic Medical Grade, Soft PVC Compound
	1.05 kg/kg content in export product.

	
	
	
	2
	
	Acrylonitrile Butadiene Styrene (ABS)
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Unsterile Needle SS 15G x 1-1/2" Length
	101 Nos./100 Nos. in the export product.

	
	
	
	4
	
	Unsterile Needle SS 17G x 1-1/2" Length
	101 Nos./100 Nos. in the export product.

	H45
	BOPP film
	1 Kg
	1
	
	Polypropylene resin/granules
	1.20 Kg.

	
	
	
	2
	
	HSD/ LDO/Furnace Oil (For Power generation
	0.512 Litre

	H46
	BOPP Film Synthetic Paper in Sheets/Reams
	1 kg
	1
	
	Polypropylene Resin/Granules
	1.067 kg

	
	
	
	2
	
	Master Batches of 70% Calcium Carbonate and 30% Polypropylene
	0.114 kg

	
	
	
	3
	
	Master Batches of 50% Titanium Dioxide and 50% Polypropylene
	0.073 kg

	
	
	
	4
	
	Master Batches of 75% Ethoxylated Tertiary Amine + 25% Polypropylene
	0.004 kg

	
	
	
	5
	
	Polystyrene
	0.061 kg

	
	
	
	6
	
	Ethylene Vinyl acetate
	0.021 kg

	
	
	
	7
	
	Ethyl Acetate (Solvant)
	0.082 kg

	H47
	Deleted
	
	
	
	
	

	H48
	Deleted
	
	
	
	
	

	H49
	Deleted
	
	
	
	
	

	H50
	BOPP self adhesive tapes/ Jumbo rolls
	1 kg
	1
	
	BOPP Film
	0.321 kg

	
	
	
	2
	
	2-Ethyl Hexyl Acrylate
	0.357 kg

	
	
	
	3
	
	Butyl Acrylate
	0.014 kg

	
	
	
	4
	
	Acrylic Acid
	0.0046 kg

	
	
	
	5
	
	Toluene
	0.0214 kg

	
	
	
	6
	
	Vinyl Acetate Monomer
	0.08 kg

	H51
	BOPP Self Adhesive Tapes/Jumbo Rolls (Net weight of BOPP in the export product is not less than 54%)
	1 kg
	1
	
	BOPP Film
	594 gms

	
	
	
	2
	
	Acrylic Water Based Adhesive (Total Solid content 55%) 
OR
	920 gms

	
	
	
	2
	a)
	2-Ethyl Hexyl Acrylate/Butyl Acrylate
	0.4906 Kg

	
	
	
	
	b)
	Acrylic Acid
	0.025 Kg

	
	
	
	
	c)
	Copolymerizable Anionic Surfactant
	0.04 Kg

	H52
	Cast Nylon Plates & Rods
	1 kg
	1
	
	Caprolactum
	1.21 kg

	
	
	
	2
	
	Catalyst: Sodium Caprolactamate
	0.026 kg

	
	
	
	3
	
	Relevant Activator: Isocyanate, Iso-cyanurate
	0.007 kg

	H53
	Clear LDPE Film Lamination Grade Film
	1 kg
	1
	
	LDPE Granules (Film Grade)
	1.05 kg

	H54
	Colour Master Batches
	1 kg
	1
	
	Relevant Polymers such as Polyethylene, Polypropylene, Polystyrene, Polyester (PET/PBT) EVA
	1.03 kg/kg content in the export product.

	
	
	
	2
	
	Titanium Dioxide
	1.03 kg/kg content in the export product

	
	
	
	3
	
	Relevant Colour Pigment/Dyes
	1.03 kg/kg content in the export product

	
	
	
	4
	
	Optional Brightener
	1.03 kg/kg content in the export product

	
	
	
	5
	
	Relevant PP/ PE/ Montan Wax
	1.03 kg/kg content in the export product.

	H55
	Colour Polyurethane Cast Parts for Chutes and Feed Hoppers such as Wear Plates, Scrapper Pads, Scrapper Wear Liners, Chute Liners, Rollers, Dust Seal Ring, Buffer Blocks and Buckerup Strips
	1 MT
	1
	
	Polyurethane Prepolymer
	0.961 MT/MT content of Polyurethane.

	
	
	
	2
	
	Polyol Curing Agent
	0.065 MT/MT content of Polyurethane.

	
	
	
	3
	
	Polyurethane Adhesive
	0.005 MT/MT content of Polyurethane.

	
	
	
	4
	
	Phthalocynine Blue Pigment
	0.016 MT/MT content of Polyurethane.

	
	
	
	5
	
	Silicone Release Agent
	0.003 MT

	H56
	Colour Polyurethane Cast Pump Parts for Mining Industry
	1 MT
	1
	
	Polyurethane Prepolymer
	0.738 MT/MT content of Polyurethane.

	
	
	
	2
	
	Polyol Curing Agent
	0.254 MT/MT content of Polyurethane.

	
	
	
	3
	
	Polyurethane Adhesive
	0.009 MT/MT content of Polyurethane.

	
	
	
	4
	
	Phthalocynine Blue Pigment
	0.015 MT/MT content of Polyurethane.

	
	
	
	5
	
	Silicone Release Agent
	0.003 MT

	H57
	Colour Polyurethane Cast Screens, Holddown Bar for Mining and Mineral Industry
	1 MT
	1
	
	Polyurethane Prepolymer
	1.005 MT/MT content of Polyurethane.

	
	
	
	2
	
	Polyol Curing Agent
	0.064 MT/MT content of Polyurethane.

	
	
	
	3
	
	Polyurethane Adhesive
	0.005 MT/MT content of Polyurethane.

	
	
	
	4
	
	Phthalocynine Blue Pigment
	0.016 MT/MT content of Polyurethane.

	
	
	
	5
	
	Silicone Release Agent
	0.003 MT

	H58
	Colour Polyurethane Hydrocyclone Cast Part for Mining and Mineral Industry
	1 MT
	1
	
	Polyurethane Prepolymer
	0.794 MT/MT content of Polyurethane.

	
	
	
	2
	
	Polyol Curing Agent
	0.281 MT/MT content of Polyurethane.

	
	
	
	3
	
	Phthalocynine Blue Pigment
	0.016 MT/MT content of Polyurethane.

	
	
	
	4
	
	Silicone Release Agent
	0.003 MT

	H59
	Coloured PP Woven tube/sack with U.V. stabilization and eyelets & draw string
	1 Kg
	1
	
	P.P. Granules
	1.045 Kg

	
	
	
	2
	
	U.V. Stabilizer
	0.020 Kg

	
	
	
	3
	
	Colour Master Batch
	0.030 Kg

	
	
	
	4
	
	Gromet (eyelet)
	1.02 No

	
	
	
	5
	
	Draw String
	Net to Net

	
	
	
	6
	
	Plastic tags
	Net to Net

	H60
	Coloured HDPE Tarpaulin with or without UV Stabilizer fitted with PP Rope and Eyelet (Gromet) Packed in LDPE filling bags
	1 kg
	1
	
	HDPE Resin Granules
	1.05 kg/kg content in the export.

	
	
	
	2
	
	Colour master Batch
	0.03 kg

	
	
	
	3
	
	LDPE Granules for coating/lamination
	1.05 kg/kg content in the export .

	
	
	
	4
	
	U.V. Stabilizer (for export with U.V. Stabilizers)
	0.003 kg/kg of HDPE Resin in the export product.

	
	
	
	5
	
	Eyelets(Gromets)
	101 Nos/100 Nos content in the export product.

	
	
	
	6
	
	P.P. Rope
	1.02 kg/kg content in the export product.

	H61
	Coloured Nylon 66 or 610 Monofilament Yarn (Dia 0.1-0.4 mm) in cut hanks upto maximum length of 45" for Tooth Brush
	1 kg
	1
	
	Nylon 66/610 (Relevant Nylon to be allowed)
	1.13 kg

	
	
	
	2
	
	Relevant Colour Master Batch
	0.02 kg

	H62
	Coloured/ White Pulverised Powder (containing minimum 98% LLDPE) Mesh Size - 25 to 35 Mesh
	1 kg
	1
	
	LLDPE Granules
	1 kg

	H63
	Cushioned vinyl Flooring Backed with Asbestos Paper
	1 kg
	1
	
	Asbestos Paper
	0.6171 kg

	
	
	
	2
	
	P.V.C. Resin
	0.3939 kg

	
	
	
	3
	
	Plasticizers
	0.2025 kg

	
	
	
	4
	
	Blowing agent
	0.0063 kg

	
	
	
	5
	
	Pigment
	0.0129 kg

	
	
	
	6
	
	Relevant Solvent
	0.0291 kg

	
	
	
	7
	
	Adhesive
	0.0039 kg

	
	
	
	8
	
	Matting Agent
	0.0002 kg

	
	
	
	9
	
	Stabilizer
	0.0156 kg

	
	
	
	10
	
	Inhibitor
	0.0039 kg

	H64
	Diazo Drafting Film (Polyester Based) thickness - 50/75/100 Microns
	1000 sq.mtrs.
	1
	
	Relevant Polyester Film Thickness - 50/75/100 Microns
	1175 sq.mtrs.

	
	
	
	2
	
	Couplor Colour Promotor
	0.67 kg

	
	
	
	3
	
	Dye Former - Diazo Type
	0.88 kg

	
	
	
	4
	
	Cellulostic Resin - Film Former
	8.71 kgs.

	
	
	
	5
	
	Silica Pigment
	7.74 kgs.

	
	
	
	6
	
	Solvents(MIBK/MEK)
	41.03 kgs.

	H65
	Diazo Duplicating film(Polyester Based) thickness - 50/75/100 Microns
	1000 sq.mtrs.
	1
	
	Relevant Polyester Film Thickness - 50/75/100 Microns
	1150 sq.mtrs.

	
	
	
	2
	
	Couplor Colour Promotor
	2.45 kgs.

	
	
	
	3
	
	Dye Former - Diazo Type
	2.3 kgs.

	
	
	
	4
	
	Cellulostic Resin - Film Former
	10.12 kgs

	
	
	
	5
	
	Solvents(MIBK/MEK)
	9.01 kgs.

	H66
	Disposable Plastic Cups, Bowls and Lids made of Polystyrene
	1 Kg Net content of import material in export
	1
	
	Polystyrene
	1.20 Kgs.

	H67
	Double Blood Bag with Tubing
	100 Nos.
	1
	
	PVC Compound Granules (Medical Grade)
	1.10 kg/kg content in the export product.

	
	
	
	2
	
	Polycarbonate Granules
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Stainless Steel Capillary
	1.25 kg/kg content in the export product.

	
	
	
	4
	
	Hot Melting Adhesive Label Medical Grade, Paper Tamper Evident Label Printed/Unprinted
OR
Evident Paper in Sheets/Rolls
	1.05 kg/kg content in the export product.

1.10 kg/kg content in the export product.

	
	
	
	5
	
	Adenine USP Grade
	0.0021 kg

	
	
	
	6
	
	Transfer Leg Closure
	105 Nos.

	H68
	Double Side Decorative Laminates with Barrier Paper
	1 Sq.Mtr x 10.00 mm thickness of 14.5 kg +/- 2.5%
	1
	
	Kraft Paper
	9.15 kg

	
	
	
	2
	
	Base Paper
	0.214 kg

	
	
	
	3
	
	Barrier Paper
	0.172 kg

	
	
	
	4
	
	Tissue Paper
	0.027 kg

	
	
	
	5
	
	Phenol
	3.52 kg

	
	
	
	6
	
	Melamine
	0.362 kg

	
	
	
	7
	
	Paraformaldehyde (91+/-1% Purity)
OR
Methanol
	2.90 kg


3.85 kg

	
	
	
	8
	
	B.O.P.P. Film
	0.01 kg

	Note:1.The above norms are based on 10.00 mm thickness with average weight of 14.5 kg +/- 2.5% and are applicable on 2.5 mm to 20 mm thickness. 
2. In case of variation in thickness/weight, the quantity of item of import viz. Phenol, Para formaldehyde/Methanol and Kraft paper to be allowed may be arrived at by adopting the following formula: AxB/Cwhere A=Quantity allowed for 10.00 mm thickness of weight.14.5 kg +/- 2.5%B=The thickness or weight/ sq. Meter of decorative laminates proposed to be exported. C = Either the Standard thickness of 10.00 mm or the Standard weight of 14.5 kg/Sq.Meter of 10.00 mm thickness.
3. The quantity of other items viz. Base Paper, Barrier Paper, Tissue Paper, Melamine and BOPP film will remain unchanged irrespective of thickness and weight of decorative laminate to be exported.

	H69
	Double Side PVC Coated Nylon Fabric: (Weight of Coated Fabric - 660 gms/ Sq.mtr. +/-3%, Weight of Coating Material - 470 gms/Sq.mtr., Weight of Nylon Yarn Fabric-190 gms/sqr.mtr.
	1 Sq. Metre
	1
	
	Relevant Nylon 6/Nylon 66 Industrial Yarn
	217 gms

	
	
	
	2
	
	PVC Resin
	274.90 gms

	
	
	
	3
	
	Dioctyl Phthalate
	210.88 gms

	
	
	
	4
	
	Titanium Dioxide (Anadase Grade)
	1.36 gm

	
	
	
	5
	
	Pigments - Red
	1.82 gm

	
	
	
	6
	
	Pigments - Blue
	4.0 gms

	
	
	
	7
	
	Pigments - Black
	3.0 gms

	
	
	
	8
	
	Ranuvin P/Tinuvin P(2-2-Hydroxy-5Methyl Phenyl)24-Benzo Triazole Phenyl
	1.0 gm

	
	
	
	9
	
	Bonding Agent (Vulcobond) Isocyanurate-TypePolymer in Dibutyl Phthalate-25%
	11.11 gms

	Note: 1. Only the relevant Denier and grade of Nylon i.e. 6 or 66 as contained in the export product shall be allowed.

	H70
	Drafting Film (Polyester Based) thickness - 50/75/100 Microns
	1000 sq.mtrs.
	1
	
	Relevant Polyester Film Thickness 50/75/100 Microns
	1150 sq.mtr.

	
	
	
	2
	
	Cellulosic Resin Film Former
	1.38 kgs

	
	
	
	3
	
	Acrylic Resin Binder
	17.05 kgs

	
	
	
	4
	
	Silica Pigment
	7.48 kgs

	
	
	
	5
	
	Solvents(MIBK/MEK)
	28.750 kgs

	H71
	Drappery (Curtain ) Rods made of High Impact Polystrene
	1 Set
	1
	
	High Impact Polystrene
	1.05 kg./kg. content in export.

	H72
	Electronic Mosquito Repellants
	1 Kg
	1
	
	Polypropylene Moulding Powder/Granules
	1.05 Kg. per Kg. content in export

	
	
	
	2
	
	PTC Thermistors
	Net to Net

	
	
	
	3
	
	LED/Neon lamp
	Net to Net

	
	
	
	4
	
	Packing Material
	

	
	
	
	
	a)
	LDPE
	1.05 Kg. per Kg. content

	
	
	
	
	b)
	Polypropylene
	1.05 Kg. per kg. content

	H73
	Epoxy Resin (Basic Liquid Resin having Epoxy value between 5.2 to 5.49)
	1 kg
	1
	
	Epichlorohydrin
	0.600 kg

	
	
	
	2
	
	Bisphenol-A
	0.676 kg

	
	
	
	3
	
	Caustic Soda Lye (100%)
	0.250 kg

	H74
	Epoxy Resin (TE 1004, KE 1004, YD-014)
	1 kg
	1
	
	Bisphenol-A 95%
	0.912 kg

	
	
	
	2
	
	Epichlorohydrin 95% Up
	0.451 kg

	
	
	
	3
	
	Sodium Hydroxide 98%
	0.194 kg

	
	
	
	4
	
	Methyl Isobutyl Ketone
	0.322 kg

	H75
	Epoxy Resin (TE-827.828, YD-127.128)
	1 kg
	1
	
	Bisphenol-A 95%
	0.804 kg

	
	
	
	2
	
	Epichlorohydrin 95%
	0.697 kg

	
	
	
	3
	
	Sodium Hydroxide 98%
	0.349 kg

	
	
	
	4
	
	Methyl Isobutyl Ketone
	0.041 kg

	H76
	Ethylene Vinyl Acetate Co-polymer (Grade 2806)
	1 MT
	1
	
	Ethylene
	786 Kgs.

	
	
	
	2
	
	Vinyl Acetate Monomer
	314 Kgs.

	
	
	
	3
	
	Bis 3,5,5 Trimethyl Hexanyl Peroxide
	0.27 Kgs.

	
	
	
	4
	
	Butylated Hydroxy Toluene
	1.20 Kgs.

	H77
	Ethylene Vinyl Acetate Copolymer (Grade 1408)
	1 MT
	1
	
	Ethylene
	900 Kgs

	
	
	
	2
	
	Vinyl Acetate Monomer
	163 Kgs

	
	
	
	3
	
	Isododecane
	6.00 Kgs

	H78
	Ethylene Vinyl Acetate Copolymer (Grade 1802)
	1 MT
	1
	
	Ethylene
	850 Kgs

	
	
	
	2
	
	Vinyl acetate Monomer
	200 Kgs

	
	
	
	3
	
	Propane
	1.0 Kg

	
	
	
	4
	
	Isododecane
	6.00 Kgs

	H79
	Ethylene Vinyl Acetate Copolymer of Grade 1202
	1 Kg
	1
	
	Ethylene
	925 gms

	
	
	
	2
	
	Vinyl Acetate Monomer
	149 gms

	
	
	
	3
	
	Propane
	10 gms

	
	
	
	4
	
	Bis 3,5, 5 Trimethyl Hexanoyl Peroxide
	0.27 gm

	
	
	
	5
	
	Teritary Butyl Peroxy-2 Ethyl Hexonate
	0.27 gm

	
	
	
	6
	
	Isododecane
	5.90 gms

	
	
	
	7
	
	Butylated Hydroxy Toluene
	0.50 gm

	H80
	Ethylene Vinyl Acetate Copolymer of Grade 1408
	1 Kg
	1
	
	Ethylene
	896 gms

	
	
	
	2
	
	Vinyl Acetate Monomer
	167 gms

	
	
	
	3
	
	Propane
	10 gms

	
	
	
	4
	
	Bis 3,5,5 Trimethyl Hexanoyl Peroxide
	0.27 gm

	
	
	
	5
	
	Tertiary Butyl Peroxy-2 Ethyl Hexonate
	0.27 gm

	
	
	
	6
	
	Isododecane
	5.90 gms

	H81
	Ethylene Vinyl Acetate Copolymer of Grade 1802
	1 Kg
	1
	
	Ethylene
	878 gms

	
	
	
	2
	
	Vinyl Acetate Monomer
	209 gms

	
	
	
	3
	
	Bis 3,5,5 Trimethyl Hexanoyl Peroxide
	0.27 gm

	
	
	
	4
	
	Tertiary Butyl Peroxy-2 Ethyl Hexonate
	0.27 gms

	
	
	
	5
	
	Isododecane
	5.90 gms

	
	
	
	6
	
	Butylated Hydroxy Toluene
	0.25 gms

	H82
	Ethylene Vinyl Acetate Copolymer of Grade 2825
	1 Kg
	1
	
	Ethylene
	746.90 gms

	
	
	
	2
	
	Vinyl Acetate Monomer
	312 gms

	
	
	
	3
	
	Bis 3,5,5 Trimethyl Hexanoyl Peroxide
	0.26 gms

	
	
	
	4
	
	Tertiary Butyl Peroxy-2 Ethyl Hexonate
	0.26 gms

	
	
	
	5
	
	Isododecane
	5.90 gms

	
	
	
	6
	
	Butylated Hydroxy Toluene
	1.20 gms

	H83
	EVA Sheets (Containing 60% EVA and 16% Synthetic rubber
	1 kg
	1
	
	EVA Resins (V.A. content 18%)
	0.60 kg

	
	
	
	2
	
	Synthetic Rubber (High Styrene Rubber)
	0.16 kg

	
	
	
	3
	
	Di-Cumyl Peroxide
	0.03 kg

	H84
	Expandable Poly Styrene Resin
	1 kg
	1
	
	Styrene 99% Monomer
	0.956 kg

	H85
	Expandable Polyestyrene General purpose grades
	1 MT
	1
	
	Styrene monomer
	956 kg

	
	
	
	2
	
	Pentane (Iso+Normal)
	83.438 kg

	
	
	
	3
	a)
	Softnal 3118 (Mono acid Diglyceride)
	1.4 kg

	
	
	
	
	b)
	Softnal 3995 (Glyceryl Mono Sterate)
	1.52 kg

	
	
	
	
	c)
	Tricalcium Phosphate
	3.598 kg

	
	
	
	
	d)
	Adwax 165 (Bisamide waxes)
	2.0 kg

	
	
	
	
	e)
	Adwax-280 (N-N ethylene Bis streamide)
OR
	1.0 kg

	
	
	
	3
	a)
	Protective Colloid (K-90)
	13 kg

	
	
	
	
	b)
	Benzoyl Peroxide
	1.52 kg

	
	
	
	
	c)
	Tertiary Butyl Perbenzoate
	2.47 kg

	
	
	
	
	d)
	Hexabromide
	0.2 kg

	
	
	
	
	e)
	Additive 451
	2.2 kgs

	
	
	
	
	f)
	Polyethylene Wax
	0.96 kg

	
	
	
	
	g)
	Alfa Methyl Styrene Dimmer
	0.42 kg

	
	
	
	
	h)
	Antistatic Agent
	0.1 kg

	
	
	
	
	I)
	Etingal A
	0.16 kg

	Note: The chemicals at S.No. 3(a) to (e) or alternative items at Sl.No. 3(a) to (I) in group may be allowed as per the applicant's requirement

	H86
	Expandable Polyestyrene Resin -Self-Extinguise grade
	1 MT
	1
	
	Styrene Monomer
	956.000 kg

	
	
	
	2
	
	Pentane (Iso + Normal)
	83.4380 kg

	
	
	
	3
	
	CD-75(Hexa Bromocyclo dedecane)
	18.000 kg

	
	
	
	4
	
	DE 60 F(Pentabromo dyphenyloxide)
	2.000 kgs

	
	
	
	5
	
	Tricalcium Phosphate
	3.598 kgs

	
	
	
	6
	
	Advawax 165 (Bisamide waxes)
	2.000 kgs

	
	
	
	7
	
	Advawax-280 (N-Nethylene Bis streamide)
	1.000 kgs

	H87
	Fabric Laminated Acrylic Tray of Various Size/ Colour/Designs
	1 kg
	1
	
	Fabric Laminated Acrylic Sheets of relevant thickness, Colour and Design
	1.05 kg/kg content in the export product.

	H88
	Fabricated Items made of PVC Leather Cloth/ Sheeting/ Sheet/ Film
	1 Kg
	1
	
	PVC Leather Cloth/Sheeting/Sheet/Film
	1.05 Kg./Kg. content in export.

	
	
	
	2
	
	ZIP Fastener
	Net to Net.

	
	
	
	3
	
	Sliders/Runners
	Net to Net.

	H89
	Feeding nipple based on natural rubber minimum 98% rubber content
	1 no.
	1
	
	Natural Rubber 
OR
	1.08 kg/kg content in export product.

	
	
	
	1
	
	Latex Natural Rubber (containing 60% DRC)
	1.80 kg/kg Rubber content in the export product.

	H90
	Feeding nipple based on silicon rubber(having min.98% rubber content)
	1 no.
	1
	
	Silicon Rubber
	1.08 kg/kg content in export

	
	
	
	2
	
	Trigonox 101 (2,5 Bistert-butylperoty-2.5- dimethyl hexane minimum 92% in solvent)
	0.007 kg/kg

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	H91
	Fibre Glass Reinforced Plastic Compression Plate 100 mm EDSU Compression Plate Top and Bottom containing 37 +/- 1% Glass Fibre Roving/Mats - Qty. 1000 Sets weighing 240 kgs +/- 2%
	1000 Sets (240 kg)
	1
	
	Fibre Glass Roving/Mats
	88.0 kgs

	
	
	
	2
	
	Unsaturated Polyester resin based on Ortho/Isophthalic Acid
	65.6 kgs.

	
	
	
	3
	
	Mineral Filters Relevant i.e. Calcium Carbonate/Alumina Trihydrate/Talc/Kaolin/Mica
	75.6 kgs

	
	
	
	4
	
	Peroxide Catalyst
	1.9 kg

	
	
	
	5
	
	Low Profile Additives - Polymeric
	12.6 kgs

	
	
	
	6
	
	Para Benzoquinone
	0.06 kg

	
	
	
	7
	
	Magnesium Oxide
	1.89 kgs

	
	
	
	8
	
	Relevant Pigments Paste
	5.06 kgs

	
	
	
	9
	
	Mould Resin Agent
	1.0 kg

	H92
	Fibre Tip Colour Pen (Sketch Pens/ Marker)
	100 pcs
	1
	
	Acetate Tow/ Polyester Tow/ polyster Top/ Polyester Fibre as are relevant to the export product (for Synthetic filters)
	1.05 kg/kg content in export

	
	
	
	2
	
	Nylon Yarn/ Hydro carbon Tips/ polyacetal Tips/ Polyester Tips
	Net + 2% wastage

	
	
	
	3
	
	Polypropylene/ HDPE/ LDPE/ ABS/ Polysterene/ PVC compound
OR
	1.05 kg/kg content in export

	
	
	
	3
	
	Plastic Extruded/ moulded components
	Net + 2% wastage

	
	
	
	4
	
	Printing Ink
OR
	1.05 kg/kg content in export

	
	
	
	4
	a)
	Ketonic/ Synthetic Resin
	0.40 kg/kg wt. of Ink in Export

	
	
	
	
	b)
	Glycol
	0.40 kg/kg wt. of Ink in export.

	
	
	
	
	c)
	Dye-stuff
	0.10 kg/kg wt. of Ink in Export

	H93
	Fine Liner Pens
	100 pcs
	1
	
	Polyacetal Tips with/ without feeder/ moulded Feeder
	Net + 2% wastage

	
	
	
	2
	
	Synthetic Filters
	Net + 2% wastage

	
	
	
	3
	
	Metal Clips
OR
	Net + 2% wastage

	
	
	
	3
	
	SS Strips for clips
	184 gm

	
	
	
	4
	
	HDPE/LDPE
OR
	637.35 gm

	
	
	
	4
	
	Plastic extruded/ moulded components
	Net + 2% wastage

	
	
	
	5
	
	Writing Inks 
OR
	168 gm

	
	
	
	5
	
	Dyestuff
	17 gm

	
	
	
	6
	
	Printing Ink
	1.05 gm

	H94
	Fire Hoses - Cotton-Polyester Jacketted , Natural-Rubber lined (containing minimum 26% Polyester)in Cotton/Polyester blend
	1000 kgs
	1
	
	Polyester filament yarn 1000 denier & above
	204 kg

	
	
	
	2
	
	Latex Natural rubber 60% DRC
	211 kgs.

	
	
	
	3
	
	Rubber chemicals (Antioxidant and Accelerator)
	4.3 kgs.

	
	
	
	4
	
	Zinc oxide
	0.21 kg

	
	
	
	5
	
	Insoluble sulpher
	1.56 kg

	
	
	
	6
	
	Relevant Pigment
	4.3 kgs.

	H95
	Fire Hoses - Double Polyester Jacketted Synthetic Rubber lined
	1000 kg.
	1
	
	Polyester Staple Fibre
	493.46 kg

	
	
	
	2
	
	Polyester filament Yarn 1000 Denier & above
	200.0 kg

	
	
	
	3
	
	Synthetic Rubber/PVC Nitrile/Nitrile Rubber
	167.15 kg

	
	
	
	4
	
	Carbon Black
	78.6 kg

	
	
	
	5
	
	Thermoplastic Polymer
	12.4 kg

	
	
	
	6
	
	Ethyl Vinyl Acetate
	6.19 kg

	
	
	
	7
	
	Rubber Chemicals (Accelarator, Antioxidant, Pepitizers or Processing Agents & Synthetic Plasticizers).
	7.50 kg

	
	
	
	8
	
	Zinc Oxide
	7.38 kg

	
	
	
	9
	
	Relevant Synthetic Resin
	24.61 kg

	
	
	
	10
	
	Titanium Dioxide
	11.61

	
	
	
	11
	
	Curing Agent (Sulphur)
	2.18 kg

	
	
	
	12
	
	Zinc Stearate
	1.81 kg

	
	
	
	13
	
	Bonding Agent
	6.60 kg

	H96
	Fire Hoses - 100% Polyester Filament Yarn jacketted Synthetic rubber lined
	1000 kg
	1
	
	Polyester Filament Yarn 1000 Denier and above
	498.61 kg

	
	
	
	2
	
	Synthetic Rubber PVC Nitrile/Nitrile rubber
	238.31 kg

	
	
	
	3
	
	Carbon Black
	112.11 kg

	
	
	
	4
	
	Thermoplastic Polymer(SBS type)
	17.67 kg

	
	
	
	5
	
	Ethyl Vinyl Accetate
	8.84 kg

	
	
	
	6
	
	Rubber Chemicals(Accelerator, Antioxidant Peptizers or Processing agents and synthetic Plasticizer)
	10.5 kgs.

	
	
	
	7
	
	Zinc Oxide
	10.51 kg

	
	
	
	8
	
	Relevant Synthetic Resin
	35.1 kg

	
	
	
	9
	
	Titanium Dioxide
	16.53 kg

	
	
	
	10
	
	Curing Agent (Sulphur)
	3.13 kg

	
	
	
	11
	
	Zinc Stearate
	2.57 kg

	
	
	
	12
	
	Bonding Agent
	9.39 kg

	H97
	Flexible Intermediate Bulk containers
	1 kg
	1
	
	Polypropylene Granules
	1.10 kg/kg content in the export product.

	
	
	
	2
	
	Relevant U.V. Stabiliser (for export with U.V.Stabilizers)
	2% of the Resin content.

	
	
	
	3
	
	LDPE Granules
	1.05 kg/kg content in the export product.

	
	
	
	4
	
	Polypropylene Yarn for Stitching
	1.05 kg/kg content in the export product.

	
	
	
	5
	
	Narrow Weaving Fabric for Tape
	1.05 kg/kg content in the export product.

	Note:1. The U.V Stabiliser will be allowed wherever the export product contains U.V stabiliser. The level of U.V Stabiliser to be permitted is 2% of the basic Polypropylene Resin.

	H98
	Flexible PVC Articles
	1 kg
	1
	
	PVC Resin/ granules
	0.600 kg

	H99
	Formulated Polyester Polyols (with 20% CFC, Spary grade)
	1 MT
	1
	
	Dibutyl tin Dilaurate
	26 Kgs.

	
	
	
	2
	
	Surfactant (silicon)
	28 Kgs.

	
	
	
	3
	
	Trimethylol Propane
	123 Kgs.

	
	
	
	4
	
	Adipic Acid
	105 Kgs.

	
	
	
	5
	
	N-N Dimethyl Cyclohoxylamine
	28 Kgs.

	
	
	
	6
	
	Freon 1 (CFC)
	200 Kgs.

	
	
	
	7
	
	Diethanol amine
	155 Kgs.

	
	
	
	8
	
	Dimethyl methyl phosphonate
	50 Kgs.

	H100
	Furniture Canes made of HDPE
	1 kg
	1
	
	High Density Polyethylene
	1.05 kg

	H101
	Deleted
	
	
	
	
	

	H102
	General Purpose Polystyrene
	1 kg
	1
	
	Styrene Monomer
	1.0382 Kg

	
	
	
	2
	
	Mineral Oil (Liquid Paraffin)
	0.0168 Kg

	H103
	Hair Brush with/without Comb with / without Mirror/ Comb with Mirror
	1 No.
	1
	
	Polypropylene Moulding Powder/ Granules
	Net + 5% wastage

	
	
	
	2
	
	LDPE Moulding Powder/Granules
	Net + 5% wastage

	
	
	
	3
	
	HDPE MouldingPowder/ Granules
	Net + 5% wastage

	
	
	
	4
	
	Relevant Mirror
	Net + 10% wastage

	H104
	HDPE (High density Polyethylene)/ LLDPE (Linear Low Density Poly Ethylene)
	1 MT
	1
	
	Monomer/ Co-monomer a) Ethylene/ Butene-1
	1031.2 kg

	
	
	
	2
	
	Solvent a) Cyclohexane
	15 kg

	
	
	
	3
	
	Catalyst and Other Miscellaneous Chemicals:
	

	
	
	
	
	a)
	Catalyst
	0.46 kg

	
	
	
	
	b)
	De-Activator
	2.88 kg

	
	
	
	
	c)
	Alumina
	13.50kg

	
	
	
	
	d)
	Anti- Oxidants
	2.40 kg

	
	
	
	
	
	
	

	H105
	HDPE Tapes with U.V. Stabilisation 2% by weight Plain/Fabricated
	1 kg
	1
	
	HDPE Granules
	1.029 kg

	
	
	
	2
	
	U.V. Stabiliser
	0.021 kg

	H106
	HDPE Woven bags with LDPE liner fitted with Zips, Velcro Canvas, Snap fastners.
	1 Kg
	1
	
	HDPE
	1.05 Kgs./Kg. content in the export product

	
	
	
	2
	
	LDPE
	1.05 Kgs./Kg. content in the export product

	
	
	
	3
	
	Zips
	Net to Net.

	
	
	
	4
	
	Canvas
	Net content + 5% wastage

	
	
	
	5
	
	Velcro (20Cm x 7.62 CM)
	Net content + 2% wastage

	H107
	HDPE Woven fabrics
	1 kg
	1
	
	HDPE Granules
	1.080 kg

	H108
	HDPE Woven fabrics laminated/ coated
	1 kg
	1
	
	HDPE Granules
	1.080 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	Granules of material used for lamination/ coating
	1.050 kg/kg content of the relevant material in the export product

	H109
	HDPE Woven Fabrics/Sacks coated and glued with kraft paper
	1 kg
	1
	
	HDPE Granules
	1.10 kg/kg content in export product.

	
	
	
	2
	
	LDPE Granules for coating
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Kraft Paper
	1.05 kg/kg content in export product.

	
	
	
	4
	
	Synthetic Adhesive
	0.04 kg

	H110
	HDPE Woven Fabrics/Sacks laminated with kraft paper
	1 kg
	1
	
	HDPE Granules
	1.10 kg/kg content in export product

	
	
	
	2
	
	LDPE Granules for lamination
	1.05 kg/kg content in export product

	
	
	
	3
	
	Kraft Paper
	1.05 kg/kg content in export product.

	H111
	HDPE Woven Fabrics/Sacks with U.V. Stabilisation 2% by weight
	1 kg
	1
	
	HDPE Granules
	1.058 kg

	
	
	
	2
	
	U.V. Stabiliser
	0.022 kg

	H112
	HDPE Woven sacks
	1 kg
	1
	
	HDPE granules
	1.10 kg

	H113
	HDPE Woven sacks laminated/ coated with/without Liner
	1 kg
	1
	
	HDPE Granules
	1.100 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	Granules of material used for lamination/ coating
	1.050 kg/kg content of the relevant material in the export product

	
	
	
	3
	
	Granule of material used for liner
	1.050 kg/kg content of the relevant material in the export product

	H114
	HDPE Woven Sacks with LDPE liner
	1 kg
	1
	
	HDC Leather Cloth
	1.100 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	HDPE Granules
	1.050 kg/kg content of the relevant material in the export product

	H115
	HDPE/PP Beautycase/Briefcase/Suitcases with/without Aluminium Frame of all sizes.
	1 No
	1
	
	Granules of relevant polymers for manufacture of main body/Components
	1.05 kg /kg content in export

	
	
	
	2
	
	PVC Compound
	1.05 kg /kg content in export

	
	
	
	3
	
	Aluminium Sheet/Strips
	1.05 kg/kg content in export

	
	
	
	4
	
	Combination Lock/Number Lock/Side Lock/Parts thereof
	Net to Net.

	
	
	
	5
	
	Relevant Lining (Rayon/Polyester/Nylon/Polypropylene)
	1.10 Sq.Mtr./Sq.Mtr. content in export.

	
	
	
	6
	
	Carrying Handle
	Net to Net

	
	
	
	7
	
	Handle Lugs
	Net to Net

	
	
	
	8
	
	Pulling Handle
	Net to Net

	
	
	
	9
	
	Glue Foil
	1.05 kg/kg content in export

	
	
	
	10
	
	Kraft Paper/Board for Lining/Divider
	1.05 kg/kg content in export.

	
	
	
	11
	
	Relevant Metallic/Non-Metallic Components
	Net to Net

	
	
	
	12
	
	Extruded Flexible Plastic Profiles
	1.02 Mtr/Mtr content in export.

	
	
	
	13
	
	Relevant Zip Fastener
	Net to Net

	Note: In case of export of coloured items, the relevant coloured master batch may be allowed as an input at the rate of 0.02kg/kg weight of polymer. In case, colour master batch is imported, then relevant polymer at item 1 will be reduced to 1.03 kg/kg content in export product.

	H116
	Hessian Bags with LDPE/ HDPE/ PP Liner/ Lamination and with/ without Zipper Handle
	1 kg weight of LDPE/ HDPE/ PP Liner including weight of Hessian
	1
	
	Relevant LDPE/ HDPE/ PP Granules for Liner
	1.05 kg/ kg content of the relevant item in export

	H117
	Hi-Liter Pens
	100 pcs
	1
	
	Fibre Tips/Rods or
	Net + 2% wastage

	
	
	
	
	
	Hydrocarbon Tip
	Net + 2% wastage

	
	
	
	2
	
	Polypropylene
	315 gm

	
	
	
	3
	
	Synthetic Filters
	Net + 2% wastage

	
	
	
	4
	
	Dyestuffs
	68.2 gm

	
	
	
	5
	
	Printing Ink
	1.10 gm

	H118
	High Density Polyethylene Resin
	1 kg
	1
	
	Ethylene
	1.0197 kg

	
	
	
	2
	
	Propylene
	0.0089 kg

	
	
	
	3
	
	Butene-1
	0.0026 kg

	
	
	
	4
	
	Hexane or Heptane
	0.0182 ltr

	
	
	
	5
	
	Stabilizer
	0.0092 kg

	
	
	
	6
	
	Catalyst
	0.0108 kg

	H119
	High Impact Polystyrene Resin
	1 kg
	1
	
	Stryene Monomer 99%
	0.9715 kg

	
	
	
	2
	
	Poly Butadiene Rubber
	0.0632 kg

	
	
	
	3
	
	Plasticizer
	0.0116 kg

	
	
	
	4
	
	Mineral Oil (Liquid Paraffin)
OR
	0.0103 kg

	
	
	
	4
	
	i)Styrene Monomer 
ii)Polybutadiene Rubber
iii)Mineral Oil (Liquid Paraffin)
	0.9470 kg
0.0875 kg
0.0221 kg

	H120
	I.V. Cannula
	1 No.
	1
	
	ABS Resin for Tube Clamp
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	HDPE Granules for Plug
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	PP Granules for Adapter, Butterfly Cannula Holder, Protector Cover, Cap with Band, Vent Fitting
	1.05 kg/kg content in the export product.

	
	
	
	4
	
	Stainless Steel Cannula of relevant length and dia
	105 Nos./ 100 Nos. of export product.

	
	
	
	5
	
	Silicone Polymer Tube in cut pieces
OR


Silicone Polymer Tube in rolls
	105 Nos./ 100 Nos. of export product (for cut pieces)
1.0 Mtr./ 100 Nos. of export product (for Rolls)

	
	
	
	6
	
	Relevant Polymer Tube in pieces

OR

Relevant Polymer Tube in rolls
	110 Nos./ 100 Nos. of export product (for cut pieces)
6.24 Mtr./ 100 Nos. of export product (for rolls)

	
	
	
	7
	
	Relevant Tyvek (coated or uncoated) of relevant GSM
OR
Relevant Medical Kraft Paper (Coated or Uncoated) of relevant GSM
	0.00528 Sq. Mtr.

0.00528 Sq. Mtr.

	
	
	
	8
	
	Relevant Thermoforming Blister Sheet Rigid Sheet
OR

Soft Film
	0.614 Sq.Mtr./100 Nos. of export product

0.853 Sq.Mtr./100 Nos. of export product

	H121
	Indofil 850 (Acrylic Solution in water for dispersing having 25% solid content)
	1 MT
	1
	
	Methacrylic Acid
	247 kgs

	
	
	
	2
	
	HDPE
	53.55 kgs

	
	
	
	
	
	
	

	H122
	Indofil G 110 (Ammonium Polyacrylate Solution in water for Rheology modification having solid content 21.5% +/-1%)
	1 MT
	1
	
	Ethyl Acrylate
	124 kgs

	
	
	
	2
	
	Methacrylic Acid
	105.7 kgs

	
	
	
	3
	
	HDPE
	53.55 kgs

	H123
	Industrial Laminates (Fabric based)
	1 MT
	1
	
	Phenol
	649.58 Kg

	
	
	
	2
	
	Paraformaldehyde
(90-92% Purity)
OR
	263.96 kgs.

	
	
	
	2
	
	Methanol
	350.53 kgs

	H124
	Industrial Laminates (Paper based electrical)
	1 MT
	1
	
	Phenol
	385.0 Kg

	
	
	
	2
	
	Kraft Paper
	504.90 Kg

	
	
	
	3
	
	Kraft Paper Electrical Grade
	128.70 Kg

	
	
	
	4
	
	Paraformaldehyde(90-92% purity)
OR
	178 kg

	
	
	
	4
	
	Methanol
OR
	236.38 kg

	
	
	
	4
	a)
	Paraformaldehyde(90-92% purity)
OR
Methanol
	148.13 kg

196.72 kg

	
	
	
	
	b)
	Di-Butyl Phthalate
	48.26 kg

	
	
	
	
	c)
	High Boiling Tar Acid
	20.76 kg

	H125
	Industrial Laminates (paper based mechanical)
	1 MT
	1
	
	Phenol
	362.78 Kg

	
	
	
	2
	
	Kraft Paper
	694.98 Kg

	
	
	
	3
	
	Paraformaldehyde (90-92% Purity)
OR
	142.63 kgs.

	
	
	
	3
	
	Methanol
	189.41 kg

	
	
	
	4
	
	Di-Butyl Phthalate
	4.32 Kg

	
	
	
	5
	
	Poly Vinyl Butyral Resin
	0.14 Kg

	H126
	Inflatable balls made out of PVC materials (Size - 5)
	1 No.
	1
	
	PVC Resin (Suspension grade)
	125.67 gms.

	
	
	
	2
	
	Plasticizer (DOP/DVP)
	87.44 gms.

	
	
	
	3
	
	PVC Blowing Agent
	3.50 gms.

	
	
	
	4
	
	Titanium Dioxide
	10.51 gms.

	
	
	
	5
	
	Release paper (width upto 60")
	0.79 mts.

	
	
	
	6
	
	Processing Aids
	3.50 gms.

	H127
	Injection Moulded Polyacetal components (Slotted Lever Insert/ Pivot Lever Insert)
	1 kg
	1
	
	Polyacetal Granules
	1.05 kg/kg content in export product.

	H128
	Isopthalate Unsaturated Polyester Resin
	1 kg
	1
	
	Propylene Glycol
	0.257 kg

	
	
	
	2
	
	Isophthalic Acid
	0.310 kg

	
	
	
	3
	
	Styrene Monomer
	0.403 kg

	H129
	Inlaid Linoleum Floor Covering of 2.0 mm thickness having a coating weight of 245 +/-3% kg.
	100 Sq. Mtr.
	1
	
	Raw Linseed Oil
	87.14 kgs

	
	
	
	2
	
	Granulated Cork/ Cork Powder
	5.21 kgs

	
	
	
	3
	
	Wood Powder
	33.23 kgs

	
	
	
	4
	
	Gum Rosin, Gum Copal
	17.12 kgs

	
	
	
	5
	
	Hydro Carbon Resin
	2.39 kgs

	
	
	
	6
	
	Titanium Dioxide Rutile
	28.40 kgs

	
	
	
	7
	a)
	Neocryl XK 70 (Modified Acrylic/ Styrene Co-polymer Emulsion)
	0.64 kg

	
	
	
	
	b)
	Poligen MV 250/Syntran MV 250 (Aqueous, Metal-cross-linked Styrene-Acrylate Copolymer Dispersion)
	

	
	
	
	8
	
	Poligen WE 1 (Polyethylene based Wax Emulsion)
	0.16 kg

	
	
	
	9
	a)
	Surfinol 104H (Surfactant) (2,4,7,9 Tetramethyl 5 Decyn-4, 7-Diol) (Tetramethyl Decyndiol)
	0.05 kg

	
	
	
	
	b)
	Fluorade FC-129 (Surfactant) (Potassium Fluoroalkyl Carboxylate)
	

	
	
	
	
	c)
	Rewopol SBDO 75 (Sodium Di-isooctyl Sulfosuccinate)
	

	H130
	Inlaid Linoleum Floor Covering of 2.5 mm thickness having a coating weight of 300 +/-3% kg.
	100 Sq. Mtr.
	1
	
	Raw Linseed Oil
	110.00 kgs

	
	
	
	2
	
	Granulated Cork/ Cork Powder
	5.51 kg

	
	
	
	3
	
	Wood Powder
	41.91 kg

	
	
	
	4
	
	Gum Rosin, Gum copal
	21.60 kgs

	
	
	
	5
	
	Hydro Carbon Resin
	2.39 kg

	
	
	
	6
	
	Titanium Dioxide Rutile
	36.67 kgs

	
	
	
	7
	a)
	Neocryl XK 70 (Modified Acrylic/ Styrene Co-polymer Emulsion)
	0.64 kg

	
	
	
	
	b)
	Poligen MV 250/Syntran MV 250 (Aqueous, Metal-cross-linked Styrene-acrylate Copolymer Dispersion)
	

	
	
	
	8
	
	Poligen WE 1 (Polyethylene based Wax Emulsion)
	0.16 kg

	
	
	
	9
	a)
	Surfinol 104H (Surfactant) (2,4,7,9 Tetramethyl 5 Decyn-4, 7-Diol) (Tetramethyl Decyndiol)
	0.05 kg

	
	
	
	
	b)
	Fluorade FC-129 (Surfactant) (Potassium Fluoroalkyl Carboxylate)
	

	
	
	
	
	c)
	Rewopol SBDO 75 (Sodium Di-isooctyl Sulfosuccinate)
	

	Note: Packing materials (Green kraft Paper and Green Gum Tape) should be allowed as per packing Policy while issuing the licences

	H131
	Jute bag/Hand bag with HDPE/LDPE Liner
	1 Kg.
	1
	
	HDPE/LDPE Granules
	1.05 Kg. per Kg. content of each material in export

	H132
	Jute bags with HDPE liner/Lamination and with/without Zipper/ Handle
	1 Kg. content of import item in the export product
	1
	
	HDPE Granules
	1.05 Kg.

	H133
	Jute Bags with LDPE liner/ Lamination and with/without Zipper/ Handle
	1 Kg. content of import item in the export product
	1
	
	LDPE granules
	1.05 Kg.

	H134
	Lacquer Coated Aluminium Metallized Polyester Film in different colours (Yarn Grade)
	1 Kg
	1
	
	Polyester Film
	1.25 kg.

	
	
	
	2
	
	Aluminium Wire
	0.0260 kg.

	
	
	
	3
	
	Melamine Resin
	0.200 kg.

	
	
	
	4
	
	Modified Epoxy Resin
	0.200 kg.

	
	
	
	5
	
	Relevant Dyestuff
	0.0302 kg.

	
	
	
	6
	
	Induction/Evaporation Boat
	0.007 No.

	
	
	
	7
	
	Solvent (Ethyl Acetate/Toluene/MEK/MIBK/DAA/Glycol)
	0.500 ltr.

	H135
	Lamination Adhesive
	1 kg
	1
	
	Adipic Acid
	0.350 kg

	
	
	
	2
	
	Isophthalic Acid
	0.10 kg

	
	
	
	3
	
	Neopentyl Alcohol/ Neo Pentyl Glycol
	0.20 kg

	
	
	
	4
	
	Trimethylol Propane
	0.20 kg

	
	
	
	5
	
	Propylene Glycol
	0.10 kg

	
	
	
	6
	
	Toluene Di-Iso-Cyanate
	0.205 kg

	H136
	Laser Printer Film (Polyester Based) Thickness 100 Micron
	1000 Sq. Mtr.(Wt. 147.86 kgs +/- 5%)
	1
	
	Polyester Film (Thickness 100 Micron)
	1150 Sq.Mtr. (Wt.164.2 kg +/- 5%)

	
	
	
	2
	
	Cellulosic Resin
	3.60 kgs

	
	
	
	3
	
	Silica Pigment
	3.60 kgs

	
	
	
	4
	
	Methyl Ethyl Ketone
	24.250 kgs

	H137
	LDPE Fly Curtains
	1 No.
	1
	
	LDPE Granules
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Dye for LDPE
	1% of weight of LDPE content in the export

	
	
	
	3
	
	Header Plastic - 120 cm
	101 No./100 Nos. content in the export product

	
	
	
	4
	
	Header Plastic - 100 cm
	101 No./100 Nos. content in the export product

	
	
	
	5
	
	Combs Plastic
	101 No./100 Nos. content in the export product

	
	
	
	6
	
	Stoppers Plastic
	101 No./100 Nos. content in the export product

	
	
	
	7
	
	Hook Plastic
	101 No./100 Nos. content in the export product

	H138
	LDPE/LLDPE blended film lin tubular rolls
	1 Kg
	1
	
	LDPE Granules (film grade)
	1.03 kg/kg. content in export.

	
	
	
	2
	
	LLDPE Granules (film grade)
	1.03 kg./kg. content in export.

	H139
	Lead Strap Carcass made of Nylon 66 and Cotton
	1 kg
	1
	
	Nylon 66 Yarn of relevant Denier
	1.1 kg/kg of Nylon content in export.

	H140
	Marker Pens
	100 pcs
	1
	
	Acrylic Fibre Tips/ Rods
	Net + 2% wastage

	
	
	
	2
	
	Polypropylene
	330.75 gm

	
	
	
	3
	
	HDPE/LDPE
	44.1 gm

	
	
	
	4
	
	Synthetic Filters
	Net + 2% wastage

	
	
	
	5
	
	Writing Inks
OR
	525 gm

	
	
	
	5
	
	Dyestuff for inks
	45 gm

	
	
	
	6
	
	Printing Ink
	1.05 gm

	H141
	Medium Density Polyethylene Compound Granules for Telephone Wire containing 75+/-1% LDPE and 25+/-1% HDPE
	1 MT
	1
	
	LDPE Granules
	0.770 MT

	
	
	
	2
	
	HDPE Granules
	0.258 MT

	
	
	
	3
	
	Phenolic Antioxidants
	0.0020 MT

	H142
	Melamine Formaldehyde Resin(Butylated) 60% Active ingredients
	1 kg
	1
	
	N. Butanol
	0.973 kg

	
	
	
	2
	
	Melamine
	0.3 kg

	
	
	
	3
	
	Isophthalic Acid
	0.10 kg

	H143
	Metal Ball Pens
	100 pcs
	1
	
	Metal Clips
	Net +2% wastage

	
	
	
	2
	a)
	Ball Pen Refill Tip Nozzles
OR
	Net +2% wastage

	
	
	
	2
	a)
	Ball Pen Refills
	Net + 2% wastage

	
	
	
	
	b)
	Polypropylene
	266.70 gms

	
	
	
	
	c)
	Writing Ink 
OR
	115.50 gms

	
	
	
	2
	c)
	Dyestuff/Ketonic Resins.
	11.55 gms

	
	
	
	3
	
	Mechanism
	Net + 2% wastage

	
	
	
	4
	
	Printing Ink
	1.25 gms

	H144
	Metal Fountain Pen & Ball Pen Set in a plastic Box (Gift sets)
	100 pcs
	1
	
	Clips
	Net + 2% wastage

	
	
	
	2
	
	Polystyrene Powder 
OR
	3.15 kg

	
	
	
	2
	
	Plastic Moulded Components
	Net + 2% wastage

	
	
	
	3
	
	Ball Pen Tips
	51 pcs

	
	
	
	4
	
	Writing Ink
	0.052 kg

	
	
	
	5
	
	Polyester Printed film (Transfer film)
	200 sq. mm

	
	
	
	6
	
	Stamping Foil
	50 sq. inch

	H145
	Metal Spectacle Frames with Acrylic Lense (Sunglass) in various colours and models
	100 Nos.
	1
	
	Side & Front of Frame made of relevant metal with or without Hinges.
	100 Pairs.

	
	
	
	2
	
	Acrylic Lenses
	100 Pairs.

	H146
	Metallic yarn made from Lacquer Coated Aluminium Metallized Polyester Film
	1 Kg
	1
	
	PET Chips
	1.39 kg.

	
	
	
	2
	
	Aluminium Wire
	0.028 kg.

	
	
	
	3
	
	Induction/Boats Evaporation
	0.007 no.

	
	
	
	4
	
	Modified Epoxy Resin
	0.212 kg.

	
	
	
	5
	
	Melamine Resin
	0.212 kg.

	
	
	
	6
	
	Dyes
	0.032 kg.

	
	
	
	7
	
	ABS Granules for Bobbin
	1.05 kg.

	H147
	Multi Coloured Synthetic Carpet (Jacquard) containing Polypropylene (BCF) and Polyester Yarn
	1 kg
	1
	
	Dyed Polypropylene BCF Yarn(Relevant Quality)
	1.15 kg/kg content in the export product.

	
	
	
	2
	
	Polyester Spun Yarn(Relevant Quality)
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	SBR/Latex (Solid Content)
	120 gms

	
	
	
	4
	
	Cotton Yarn (Relevant Quality)
	1.01 kg/kg content in the export product.

	
	
	
	5
	
	Polythene Tube (10-12" Dia)
	Net + 0.5% wastage.

	
	
	
	6
	
	Labels
	Net to net.

	H148
	Multilayer Extruded Plastic Packing Material (Unprinted - 5 Ply)
	1 kg.
	1
	
	LDPE Film Grade
	1.12 kg/kg content in the export Product.

	
	
	
	
	a)
	LLDPE Film Grade
	1.12 kg/kg content in the export Product.

	
	
	
	2
	
	Ethylene Acrylic Acid co-polymer granules
	1.10 kg/kg contained in the export product.

	
	
	
	3
	
	Aluminium foil
	1.10 kg/kg contained in the export product.

	H149
	Multilayer Extruded Plastic packing Material (Printed 5 Ply)
	1 kg
	1
	
	LDPE Film Grade
	1.12 kg/kg content in the export product.

	
	
	
	
	a)
	LLDPE Film Grade
	1.12 kg/kg content in the export product.

	
	
	
	2
	
	Ethylene acrylic Acid copolymer granules
	1.10 kg/kg content in the export product.

	
	
	
	3
	
	Aluminium Foil
	1.10 kg/kg content in the export product.

	
	
	
	4
	
	U.V. Ink
	0.5% of weight of LDPE/LLDPE in the export product.

	
	
	
	5
	
	U.V. Varnish
	0.3% of weight of LDPE/LLDPE in the export product.

	H150
	Multilayer Plastic Laminated Tubes with Caps (5-Ply Printed)
	1 kg
	1
	
	LDPE Film Grade
	1.17 kg/kg content in the export product.

	
	
	
	
	a)
	LLDPE Film Grade
	1.17 kg/kg content in the export product.

	
	
	
	2
	
	Ethylene Acrylic Acid copolymer granules
	1.17 kg/kg content in the export product.

	
	
	
	3
	
	Aluminium Foil
	1.12 kg/kg content in the export product.

	
	
	
	4
	
	Master Batch
	1.2% of weight of LDPE/LLDPE

	
	
	
	5
	
	U.V. Ink
	0.5% of weight of LDPE/LLDPE in the export product.

	
	
	
	6
	
	U.V. Varnish
	0.3% of weight of LDPE/LLDPE in the export product.

	
	
	
	7
	
	HDPE Granules (For shoulder of the Tube)
	1.05 kg/kg content in the export product.

	
	
	
	8
	
	Polypropylene granules for caps.
	1.05 kg/kg content in the export product.

	Note : 1. The above norms are for the export product with Caps and Without Insert in the cap. 
2. If the export product contains caps with inserts made out of Polypropylene, the raw material - Polypropylene to be permitted at the rateof 1.05 Kg/Kg of Polypropylene content in the export product.

	H151
	Multilayer Plastic laminated tubes(with 7 Ply Printed)
	1 kg
	1
	
	LDPE/LLDPE (Film Grade)
	1.22 kg/kg contained in the export product.

	
	
	
	2
	
	Ethylene Acrylic Acid
	1.22 kg/kg content in the export product.

	
	
	
	3
	
	Aluminium Foil
	1.15 kg/kg content in the export product.

	
	
	
	4
	
	U.V. Ink
	0.5% of weight of LDPE/LLDPE in the export product

	
	
	
	5
	
	U.V. Varnish
	0.3% of weight of LDPE/LLDPE in the export product.

	
	
	
	6
	
	HDPE Granules (For shoulder of the tube)
	1.05 kg/kg content in the export product.

	
	
	
	7
	
	Polypropylene granules (for caps)
	1.05 kg/kg content in the export product.

	H152
	Nail Varnish Brush
	1 kg
	1
	
	Relevant Nylon Monofilament/ Nylon Bristles
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	LLDPE Granules
	1.05 kg/kg content in the export product.

	H153
	Non Pyrogenic Sterile intravenous infusion Set/ Blood Collection Set
	1 No.
	1
	
	Relevant HDPE/PP/HMHPE/LDPE
	1.05 kg/kg content in the export product

	
	
	
	2
	
	PVC Compound Granules
	1.05 kg/kg content in the export product

	
	
	
	3
	
	(i) Relevant Needle 
OR

(ii) Stainless Steel Cannula of Relevant length and dia 
OR
(iii) Stainless Steel Capillary Tube
	102/100 Nos. content in the export product 
105/100 Nos. content in the export product 
4.4 Mtrs/100 Nos. content in the export product

	
	
	
	4
	
	Relevant Luer Adapter
	102/100 Nos. content in the export product

	
	
	
	5
	
	Relevant Safety Shield/ Security Protector
	102/100 Nos. content in the export product

	
	
	
	6
	
	Relevant LDPE Soft Film/ PVC Rigid sheet
	72 gms / 100 Nos. content in the export product

	
	
	
	7
	
	Relevant Medical Kraft Paper
	33 gms / 100 Nos. content in the export product

	H154
	Non-Weatherable Dyed Polyester Film
	100 Kg
	1
	
	D.M.T.
	154.35 kg

	
	
	
	2
	
	M.E.G.
	58.80 kg

	
	
	
	3
	
	Relevant Solvent
	33.60 kg

	
	
	
	4
	
	M.E.G.
	44.80 kg

	
	
	
	5
	
	Disperse Dyes Blue
	2.464 kg

	
	
	
	6
	
	Disperse Dyes Red
	0.672 kg

	
	
	
	7
	
	Disperse Dyes Yellow
	0.224 kg

	H155
	Nylon 66 or 610 Monofilament Yarn (Dia 0.2-0.4 mm) in cut hanks upto maximum length of 45" for Tooth Brush
	1 kg
	1
	
	Nylon 66/610 (Relevant nylon to be allowed)
	1.21 kg

	
	
	
	2
	
	White Master Batch
	0.01 kg

	H156
	Nylon based bag with stopper cap
	1 Kg
	1
	
	EVA Co-Polymer
	1.05 kg/kg. content in export.

	
	
	
	2
	
	Low Density Poly Ethylene
	1.05 kg/kg. content in export.

	
	
	
	3
	
	Chemically Modified linear low density poly ethylene
	1.05 kg/kg. content in export.

	
	
	
	4
	
	Ultra low density poly ethylene
	1.05 kg/kg. content in export.

	
	
	
	5
	
	Very low density poly ethylene
	1.05 kg/kg. content in export.

	H157
	Nylon Filament Twine
	1 kg
	1
	
	Caprolactum
	1.10 kg

	H158
	Nylon Filament knitted Nets
	1 kg
	1
	
	Relevant Nylon 6/66 Monofilament Yarn/ Nylon Multifilament Yarn/ Nylon Multimono Twine/ Nylon Mono Twine/ Polyester Twisted Twine
	1.05 kg

	H159
	Nylon Tyre Cord Fabric
	1.00 MT
	1
	
	Nylon Chips
	1.098 MT

	
	
	
	2
	
	Mercapto-Benzimidazole
	3.00 kg.

	
	
	
	3
	
	Spin Finish Oil
	11.40 kg.

	
	
	
	4
	
	Cuprous Iodide
	0.44 kg.

	
	
	
	5
	
	Tetra Methyl Thiuram Di-Sulphide (TT)
	0.107 kg.

	H160
	Nylon- 6 Crimpled Raw White Intermingled with Elastane Yarn
	1 kg
	1
	
	Caprolactum
	1.155 kg

	
	
	
	2
	
	Titanium Dioxide
	0.0054 kg

	
	
	
	3
	
	Elastane yarn
	1.05 kg/kg content in export.

	H161
	Nylon-6 Chips
	1 Kg
	1
	
	Caprolactum
	1.008 Kg

	H162
	Orthopthalate Unsaturated Polyester Resin
	1 kg
	1
	
	Fumed Silica Aerosil 200
	0.01 kg

	
	
	
	2
	
	Propylene Glycol
	0.327 kg

	
	
	
	3
	
	Phthalic Anhydride
	0.257 kg

	
	
	
	4
	
	Styrene Monomer
	0.307 kg

	
	
	
	
	
	
	

	H163
	Overhead Projector film polyester based
	1 kg
	1
	
	Polyester Volume
	1.1 kgs.

	
	
	
	2
	
	Coupler
	0.035 kg.

	
	
	
	3
	
	Pigments
	0.032 kg.

	
	
	
	4
	
	Cellulose Acetate Propionate
	0.071 kg.

	H164
	Oxygen Mask made of Non-Toxic Medical Grade Soft PVC (Net weight 122 gms each)
	100 Nos.
	1
	
	Poly Vinyl Chloride, Non-Toxic Medical Grade, Soft PVC Compound
	1.05 kg/kg content in export product.

	
	
	
	2
	
	LDPE Non-Toxic Granules
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Elastic Band Nylon Woven
	101 Nos./100 Nos. in the export product.

	
	
	
	4
	
	Metal Clip 0.5 mm Thick Aluminium Sheet
	101 Nos./100 Nos. in the export product.

	H165
	P.P Tapes with U.V. Stabilisation 2% by weight Plain/Fabricated.
	1 kg
	1
	
	P.P. Granules
	1.029 kg

	
	
	
	2
	
	U.V. Stabiliser
	0.021 kg

	H166
	Paper backed Vinyl wall paper
	1 Roll(10 Mtrs length x 0.53 mtr width having net weight of 950 gms
	1
	
	PVC Resin (Paste grade)
	0.160 Kg.

	
	
	
	2
	
	Stabilizer
	0.005 Kg.

	
	
	
	3
	
	Plasticizer
	0.111 Kg.

	
	
	
	4
	
	Surface Active agent (Phosphate ester)
	0.0002 Kg.

	
	
	
	5
	
	Pigment/Titanium Dioxide
	0.016 Kg.

	
	
	
	6
	
	Base Paper (100 Gms.)
	0.636 Kg.

	
	
	
	7
	
	Blowing agent
	0.005 Kg.

	
	
	
	8
	
	Filler
	0.126 Kg.

	
	
	
	9
	
	Solvent
	0.064 Kg.

	H167
	Deleted
	
	
	
	
	

	H168
	Deleted
	
	
	
	
	

	H169
	Pen Parts (viz.) Metal Refills
	1000 Nos
	1
	
	Brass tubes/Brass Scrap or Copper Tube/Copper scrap
	1.05 Kg. per Kg. content in export

	
	
	
	2
	
	Nickel Silver Wire/Brass Wire/S.S. Wire/Scrap
	1.05 Kg. per Kg. content in export.

	
	
	
	3
	
	Stainless Steel Balls/Tungston Carbide Ball/Ceramic Ball
	Net + 2% wastage

	
	
	
	4
	
	Derilyn Plastic Powder
	1.05 Kg. per Kg. content in export.

	
	
	
	5
	
	Refil Ink
OR
	1.05 Kg. per Kg. content in export.

	
	
	
	5
	a)
	Glycol
	0.40 Kg

	
	
	
	
	b)
	Ketonic Resin
	0.45 Kg.

	
	
	
	
	c)
	Pigments
	0.05 Kg

	
	
	
	
	d)
	Dye Stuff for Ink
	0.10 Kg

	H170
	Pet Containers with Polypropylene/ HDPE/ LDPE Cap
	1 kg
	1
	
	Pet Chips (Bottle Grade)
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Polypropylene/ HDPE/ LDPE (Moulding grade)
	1.05 kg/kg content in the export product.

	H171
	Pheno-therm (Phenolic Foam in Bun form)
	1 Cubic Metre (Density 40.0 Kg per cubic metre)
	1
	
	Phenol
	36.46 Kg

	
	
	
	2
	
	Methanol
	25.44 Kg

	
	
	
	3
	
	Di-Methyl Ethanol Amine
	1.07 Kg

	
	
	
	4
	
	Surfactant L-5340
	1.82 Kg

	
	
	
	5
	
	Gama Butyro Lactone
	3.04 Kg

	
	
	
	6
	
	N-Pentane
	8.29 Kg

	For other density = Above requirement x Actual Density/ 40

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	H172
	Phenol Formaldehyde Moulding Powder (Filler content not exceeding 51% by weight)
	1 M.T.
	1
	
	Phenol
	353 kgs.

	
	
	
	2
	
	Hexamine
	40 kgs.

	
	
	
	3
	
	Relevant Pigments
	13 kgs.

	H173
	Plain Paper Copier Film/Xerographic Drafting Film (Polyester Based) thickness - 50/75/100 Microns
	1000 sq.mtrs.
	1
	
	Relevant Polyester Film Thickness - 50/75/100 Microns
	1150 sq.mtrs.

	
	
	
	2
	
	Silica Pigment
	12.32 kgs.

	
	
	
	3
	
	Acrylic Resin Film Former
	18.78 kgs.

	
	
	
	4
	
	Melamine resin
	10.81 kgs.

	
	
	
	5
	
	Solvents(MIBK/MEK)
	9.01 kgs.

	H174
	Plastic Bags with top Rubber spout multilayered
	1 kg.
	1
	
	EVA Co-polymer
	1.05 Kg./Kg. content in export.

	
	
	
	2
	
	LDPE
	1.05 Kg./Kg. content in export.

	H175
	Plastic Body Ball pens & parts thereof including refills
	100 pcs
	1
	
	Ball pen Tips 
OR
	Net + 2% wastage

	
	
	
	1
	a)
	Nickle Silver Wire/ Brass Wire/ Brass Scrap/ SS Wire
	1.075 kg/kg content in export product

	
	
	
	
	b)
	SS Balls/ Tungsten Carbide Ball/ Ceramic Ball
	Net + 2% wastage

	
	
	
	2
	
	Writing Ink 
OR
	33.6 gms.

	
	
	
	2
	a)
	Ketonic Resin/ Synthetic Resin
	0.40 kg per kg weight of ink in export product

	
	
	
	
	b)
	Glycol
	0.40 kg per kg. weight of Ink in export product

	
	
	
	
	c)
	Dyestuff for Ink
	0.10 kg per kg. weight of Ink in export product

	
	
	
	3
	
	Moulding Powder (PE/ PS/ PP/ ABS) and PVC Compound
	1.05 kg per kg. of specific material content in export product

	H176
	Plastic Body Vaccum Flask in various sizes with silver coated Glass Refill
	1 Kg
	1
	
	Polypropylene Moulding Powder/Granules
	1.05 kg/kg. content in export.

	
	
	
	2
	
	Refill(Silver coated Glass Refill)
	Net + 1% wastage

	
	
	
	3
	
	Silicon rubber Washers 
OR
	Net + 2% wastage

	
	
	
	3
	
	Synthetic Silicon Rubber
	1.05 Kg/Kg content of Silicon Rubber Washer in export

	H177
	Deleted
	
	
	
	
	

	H178
	Plastic Clips/ Pegs made of Polypropylene/ HDPE
	1 kg
	1
	
	Polypropylene Moulding Powder/Granules
OR
HDPE Granules
	1.05 kg/kg content in the export product.
1.05 kg/kg content in the export product.

	
	
	
	2
	
	Spring Steel Wire
	1.05 kg/kg content in the export product.

	H179
	Plastic Disposable Hand Gloves made from HDPE
	1 kg.
	1
	
	HDPE Granules
	1.15 kg

	H180
	Plastic Files/ Folders with or without Plastic/ Metallic Clips, with or without Pockets
	1 kg
	1
	
	Relevant Polypropylene Sheets
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Relevant Polystyrene/Polypropylene/Nylon Moulding Powder
	1.05 kg/kg content in export item.

	
	
	
	3
	
	Relevant Plastic/ Metal Clips
	Net to net.

	H181
	Plastic Fountain Pen
	100 pcs
	1
	a)
	Polypropylene
	Net + 2% wastage

	
	
	
	
	b)
	ABS
OR
	Net + 2% wastage

	
	
	
	1
	
	Plastic extruded/ moulded components
	Net + 2% wastage

	
	
	
	2
	
	Ink Cartidge
	Net + 2% wastage

	
	
	
	3
	
	Fountain pen nib
OR
	Net + 2% wastage

	
	
	
	3
	a)
	Iridium alloy Pen Points
	Net + 2% wastage

	
	
	
	
	b)
	Stainless Steel Strips
	69.44 gm

	
	
	
	
	
	
	

	H182
	Plastic Hand Gloves made from HDPE/LDPE/EVA
	1 kg
	1
	
	Relevant HDPE/LDPE/EVA
	1.15 kg

	H183
	Plastic hollow corrugated board made from polypropylene
	1 Kg
	1
	
	Polypropylene (co-polymer grade)
	1.063 kg.

	
	
	
	2
	
	Stabilizer
	0.005 Kg.

	
	
	
	3
	
	Pigments
	0.032 kg.

	H184
	Deleted
	
	
	
	
	

	H185
	Deleted
	
	
	
	
	

	H186
	Deleted
	
	
	
	
	

	H187
	Deleted
	
	
	
	
	

	H188
	Deleted
	
	
	
	
	

	H189
	Plastic Junction Box with Brass Revets made of High Impact Poly Styrene
	1 No.
	1
	
	High Impact Poly Styrene
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Brass Scrap
	1.05 kg/kg of Brass Rivets content in the export

	H190
	Plastic made-ups of Medical Grade PVC Compound
	1 kg
	1
	
	Medical Grade PVC Compound
	1.10 kg/kg content in the export product.

	
	
	
	2
	
	LDPE Granules for connectors
	1.05 kg/kg content in the export product.

	H191
	Plastic Moulded extruded components for Pens
	1 kg content of Polypropylene
	1
	
	Polypropylene
	1.05 kg

	
	
	
	2
	
	HDPE/LDPE
	1.05 kg

	
	
	
	3
	
	Polystyrene
	1.05 kg

	H192
	Plastic Petrol Filter for Four wheelers
	1,00,000 No.
	1
	
	Polycarbonate
	1.05 kg/kg content in export product.

	
	
	
	2
	
	Filter Paper
	1.25 kg/kg content in export product.

	
	
	
	3
	
	Zinc Plated M.S. Sheet Thickness, 0.3 mm & thinner.
	1.30 kg/kg content in export product.

	
	
	
	4
	
	Bonding Agent
	0.5 gm/ piece of export product.

	H193
	Plastic Rivets (Polyacetal)
	1 Kg
	1
	
	Polyacetal Resin
	1.05 Kg.

	H194
	Plastic Shaving/ Household Brushes/ Street Brooms
	1 kg
	1
	
	Relevant Nylon/ PP/ PVC Monofilament Bristles
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Relevant Polymers like ABS Granules/ PP Granules/ HIPS Granules
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Plastic Coated MS Handle
	Net to net

	
	
	
	4
	
	Relevant Dyes
	Upto 1% of weight of polymer content(Sl. 2 of import)

	Note: 1. In the case of export of coloured items, relevant colour master batch shall also be allowed as an additional input at 0.01 kg/kg weight of polymer and accordingly quantity of relevant polymerat Sl. No. 2 shall be reduced to 1.04kg/kg contained in the export product andNote: 2. In case of relevant dyes are allowed then masterbatch shall not be included.

	H195
	Poly Butylene Terephthalate(PBT) Chips
	1 kg
	1
	
	DMT
	1.00 kgs

	
	
	
	2
	
	Butanediol
	0.60 kgs

	
	
	
	3
	
	TBT
	0.0020 kgs

	
	
	
	4
	
	Titanium Dioxide
	0.0030 kgs

	H196
	Poly Isocynate Solution 50% Resin/Total Solid content in Ethyl Acetate Solvent
	1 kg
	1
	
	Adipic Acid
	0.012 kg

	
	
	
	2
	
	Isophthalic Acid
	0.037 kg

	
	
	
	3
	
	Monoethylene Glycol
	0.032 kg

	
	
	
	4
	
	Diethylene glycol
	0.060 kg

	
	
	
	5
	
	1,6-Hexane diol
	0.002 kg

	
	
	
	6
	
	Toluene Di-Iso-Cyanate
	0.372 kg

	
	
	
	7
	
	Ethyl Acetate
	0.500 kg

	H197
	Poly Jute Bag
	1 Kg.
	1
	
	PP Granules
	1.05 Kg per Kg content in export

	H198
	Poly Tetra Fluoro Ethylene (P.T.F.E.) Tapes
	1 kg
	1
	
	Poly Tetra Fluoro Ethylene Resin (P.T.F.E.Resin)
	1.050 kg

	
	
	
	
	
	
	

	H199
	Poly Urethane Foam Products
	1 Kg
	1
	
	Polyol
	0.673 Kg.

	
	
	
	2
	
	Iso Cyanate (TDI)
	0.477 Kg.

	
	
	
	3
	
	Tin Catalyst (Stennous Octoate)
	0.0019 Kg.

	
	
	
	4
	
	Methylene Chloride
	0.092 Kg.

	
	
	
	5
	
	Silicon Stabilizer
	0.115 Kg.

	H200
	Poly Vinyl Acetate Emulsion solid content 48%
	1 kg
	1
	
	Poly Vinyl Alcohol
	0.0078 kg

	
	
	
	2
	
	Emulsifier
	0.0009 kg

	
	
	
	3
	
	Vinyl Acetate Monomer
	0.4729 kg

	
	
	
	4
	
	Ammonium Per Sulphate Tech
	0.0009 kg

	
	
	
	5
	
	Dibutyl Phthalate Tech
	0.0689 kg

	H201
	Poly Vinyledene Chloride Coated Paper/Film
	1 kg
	1
	
	Poly Vinylidene Chloride
	1.05 kg/kg content in export product.

	
	
	
	2
	
	Base Materials:
	

	
	
	
	
	a)
	BOPP Film/Jumbo Roll
	1.05 kg/kg content in export product

	
	
	
	
	b)
	Paper in Sheet/Roll form
	1.05 kg/kg content in export product

	
	
	
	
	c)
	Polyester Film/Jumbo Roll
	1.05 kg/kg content in export product

	
	
	
	3
	
	Primers Resin/ Hardner
	0.028 kg

	H202
	Polyamide (Nylon66) Housing for universal type Rail mounted terminals of different specification
	1 Kg
	1
	
	Nylon 66 Moulding Powder
	1.05 Kg.

	H203
	Polybutylene Terephthalate compound containing Epoxy 1.5%
	1 kg
	1
	
	Polybutylene Terephthalate Resin
	1.005 kg

	
	
	
	2
	
	Epoxy
	0.01575 kg

	H204
	Polycarbonate drinking cup with Polypropylene lid printed
	1 kg.
	1
	
	Polycarbonate Resin
	1.05 kg/kg content in export.

	
	
	
	2
	
	Polypropylene Granules
	1.05 kg/kg content in export.

	
	
	
	3
	
	PVC film for blister packing
	1.05 kg/kg content of packing material in export

	
	
	
	4
	
	Printing Inks
	0.20% of the Polycarbonate & Polypropylene contained in export product.

	H205
	Deleted
	
	
	
	
	

	H206
	Polyester (PET) chips (High pressure moulding Grade/bottle grade)
	1 kg
	1
	
	Purified Terephthalic Acid (PTA)/ Para-phthalic Acid
	0.9846 kg

	
	
	
	2
	
	Ethylene Glycol Technical/Mono Ethylene Glycol (MEG)
	0.3937 kg

	
	
	
	3
	
	Relevant Catalyst
	0.00018 kg

	H207
	Polyester Chips(Textile Grade)(PTA Route).
	1 MT
	1
	
	Purified Terephthalic Acid (PTA)
	0.915 MT

	
	
	
	2
	
	Mono Ethylene Glycol (MEG)
	0.370 MT

	
	
	
	3
	
	Titanium Dioxide
	0.0034 MT

	H208
	Polyester film
	1 kg
	1
	
	PET Chips
	1.050 kg

	H209
	Polyester Film (Biaxially Oriented Polyester Film)/Polyethylene Terephthalic Film
	1 kg
	1
	
	PTA
	0.945 kg

	
	
	
	2
	
	MEG
	0.40263 kg

	
	
	
	3
	
	Antimony Trioxide
	0.00105 kg

	
	
	
	4
	
	Manganese Acetate
OR
	0.000524 kg

	
	
	
	4
	
	Triphenyl Phosphate
	0.00524 kg

	
	
	
	5
	
	Phosphoric Acid
	0.000314 kg

	
	
	
	6
	
	Silica
	0.0022575 kg

	
	
	
	7
	
	Triethylene Glycol
	0.010395 kg

	H210
	Polyester film (Biaxially oriented polyster film)
	1 kg
	1
	
	DMT
	1.04476 kg

	
	
	
	2
	
	MEG
	0.40263 kg

	
	
	
	3
	
	Antimony Trioxide
	0.00105 kg

	
	
	
	4
	
	Manganese acetate
	0.000524 kg

	
	
	
	5
	
	Phosphoric Acid
	0.000314 kg

	
	
	
	6
	
	Silica
	0.0022575 kg

	
	
	
	7
	
	Triethylene glycol
	0.010395 kg

	H211
	Polyester Jacketed Natural Rubber Lined Fire Hoses
	1 MT
	1
	
	Polyester Spun Yarn
	337 kgs.

	
	
	
	2
	
	Polyester Filament Yarn 1000 denier and above
	158.0 kgs

	
	
	
	3
	
	Synthetic rubber (Polychloroprene rubber)
	24.5 kgs.

	
	
	
	4
	
	Latex Natural rubber 60% DRC
	220.5 kgs.

	
	
	
	5
	
	Rubber Chemicals (Accelerator & Antioxident)
	6.3 kgs.

	
	
	
	6
	
	Zinc Oxide
	12 kgs.

	
	
	
	7
	
	Insoluble Sulphur
	2.2 kgs.

	
	
	
	8
	
	Zinc Stearate
	0.2 kg.

	
	
	
	9
	
	Plasticiser
	12 kgs.

	
	
	
	10
	
	Peptizers or Processing agents and Synthetic Plastiscers
	10.00 kg

	H212
	Polyester Jacketted Synthetic Rubber Lined Fire Hoses
	1 MT
	1
	
	Polyester Staple Fibre
	374.28 kgs

	
	
	
	2
	
	Polyester Filament Yarn
	158.57 kgs

	
	
	
	3
	
	Polychloroprene/ EPDM/PVC Nitrile Rubber
	245.76 kgs

	
	
	
	4
	
	Carbon Black
	115.63 kgs

	
	
	
	5
	
	Ethylene Vinyl Acetate
	18.23 kgs

	
	
	
	6
	
	PVC Resin
	9.13 kgs

	
	
	
	7
	
	Rubber Chemicals (Accelerator & Antioxidant)
	7.37 kgs

	
	
	
	8
	
	Zinc Oxide/ Activator
	10.86 kgs

	
	
	
	9
	
	Synthetic Resin
	36.20 kgs

	
	
	
	10
	
	Titanium Dioxide
	17.05 kgs

	
	
	
	11
	
	Curing Agent (Sulphur)
	3.23 kgs

	
	
	
	12
	
	Zinc Stearate
	2.65 kgs

	
	
	
	13
	
	Bonding Agent
	9.71 kgs

	
	
	
	14
	
	Peptizers or Processing Agents and Synthetic Plasticisers
	10.00 kgs

	H213
	Polyester Metallized film (Aluminium coated film)
	1 kg
	1
	
	Polyester Film
	1.100 kg

	
	
	
	2
	
	Aluminium wire 99.9%
	0.0246 kg

	
	
	
	3
	
	Induction/Evaporation Boat
	0.007 No

	H214
	Polyester Monofilament Yarn(Diameter 0.5 mm to 0.8 mm)
	1 kg
	1
	
	Polyester Chips
	1.05 kg

	
	
	
	2
	
	ABS Granules for making Bobbin
	1.05 kg/kg content in the export product.

	H215
	Polyester Offset Plate (60-130 Micron)
	1000 Sq. Mtr.
	1
	
	Relevant Polyester film (50 - 100 Micron +/-5%)
	1250 Sq.Mtrs.

	
	
	
	2
	
	Acrylic Resin
	3.93 Kg.

	
	
	
	3
	
	Silica Pigment
	9.60 Kg.

	H216
	Polyester Resin Solution @ 80% Resin Content
	1 kg
	1
	
	Adipic Acid
	0.133 kg

	
	
	
	2
	
	Isophthalic Acid
	0.384 kg

	
	
	
	3
	
	Monoethylene glycol
	0.071 kg

	
	
	
	4
	
	Diethylene Glycol
	0.290 kg

	
	
	
	5
	
	1,6-Hexane diol
	0.024 kg

	
	
	
	6
	
	Ethyl Acetate/ Methyl Ethyl Ketone(relevant)
	0.200 kg

	Note:- 1. For different percentage of Resin content, the requirement of import item Nos. 1 to 5 may be worked out on pro-rata basis. For item No. 6 i.e. solvent, the requirement may be worked out in the inverse ratio depending on sloventcontent/percentage.

	H217
	Polyester Snood Twines (in rope form)
	1 kg
	1
	
	Polyester Filament Yarn
	1.02 kgs

	H218
	Deleted
	
	
	
	
	

	H219
	Deleted
	
	
	
	
	

	H220
	Deleted
	
	
	
	
	

	H221
	Deleted
	
	
	
	
	

	H222
	Deleted
	
	
	
	
	

	H223
	Deleted
	
	
	
	
	

	H224
	Deleted
	
	
	
	
	

	H225
	Polyethylene Foam
	1 kg
	1
	
	Low density Polyethylene Resin
	0.856 kg

	
	
	
	2
	
	Blowing agent
	0.180 kg

	
	
	
	3
	
	Dicumyl Peroxide
	0.006 kg

	H226
	Polypropylene Frame Fitted with Mirror and Hard Board(shape to be specified)
	1 No.
	1
	
	Polypropylene granules
	1.05 kg/kg content in export

	
	
	
	2
	
	Glass Mirror of relevant thickness (in case of round/oval shape of fitting)
	1.25 sq.mtr/sq.mtr content in export

	
	
	
	3
	
	Hard Board of relevant thickness (in case of Round/Oval shape of fitting)
OR

Hard Board of relevant thickness (in case of Square/Rectangular shape of fitting)
	1.20 sq.mtr./sq.mtr. content in export.

1.05 sq.mtr./sq.mtr. content in export.

	H227
	Polypropylene Insulated Ware/Casserole
	1 kg
	1
	
	PP Granules
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Glass Wool Insulation
	1.02 kg/kg content in the export product.

	H228
	HDPE/PP Knitted Coloured Bags
	1 kg
	1
	
	Relevant HDPE/PP Granules
	1.11 Kg

	
	
	
	2
	
	Relevant HDPE/PP Colour Master Batch
	0.01 Kg

	H229
	Polypropylene Mats
	1 Kg
	1
	
	Polypropylene Granules (As raw material)
	1.21 Kg/Kg content in export

	
	
	
	2
	
	Polypropylene Granules (As Packing Material)
	1.05 Kg/Kg content in packing

	H230
	Polypropylene Multifilament Yarn
	100 Kg
	1
	
	Polypropylene Chips/Granules/ Resins
	105.10 Kg.

	
	
	
	2
	
	Master Batch (Polypropylene Dyed Chips/ Relevant Colour Master Batches)
	4.15 Kg.

	
	
	
	3
	
	U.V. Stabilizer
	0.75 Kg.

	
	
	
	4
	
	Spin Finish Oil
	2.33 Kg.

	H231
	Polypropylene plain bags (without liner)
	1 kg
	1
	
	Polypropylene
	1.05 kg

	H232
	Polypropylene woven Fabrics/Leno Bags
	1 kg
	1
	
	PP Granules
	1.080 kg

	H233
	Polyester Chips
	1 kg
	1
	
	DMT
	1.030 kg

	
	
	
	2
	
	MEG
	0.390 kg

	
	
	
	3
	
	DMIP
	0.020 kg

	
	
	
	4
	
	Antimony Trioxide
	0.001 kg

	
	
	
	5
	
	Manganese Acetate
	0.0005 kg

	
	
	
	6
	
	Triethylene Glycol
	0.010 kg

	
	
	
	7
	
	Phosphoric Acid
	0.0003 kg

	
	
	
	8
	
	Titanium dioxide
	0.004 kg

	H234
	Polystyrene disposable plastic Cups, Bowls & Lids etc.
	1 Kg
	1
	
	Polystyrene Granules
	1.05 Kg/Kg content in export

	H235
	Polytetra Fluoroethylene (PTFE) Resin (Suspension Grade)
	1 MT
	1
	
	Chloroform
	4.75 MT

	
	
	
	2
	
	Perfluoro Octanoic Acid (FC-26)
	0.21 kg

	H236
	Polyurethane Resin Solution @60% Resin/Total solid content in relevant Solvent
	1 kg
	1
	
	Adipic Acid
	0.094 kg

	
	
	
	2
	
	Isophthalic Acid
	0.270 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.050 kg

	
	
	
	4
	
	Diethylene Glycol
	0.204 kg

	
	
	
	5
	
	1,6-Hexane Diol
	0.016 kg

	
	
	
	6
	
	Toluene Di-Iso-Cyanate
	0.035 kg

	
	
	
	7
	
	Ethyl Acetate/ Methyl Ethyl Ketone
	0.400 kg

	H237
	Polyurethane Resin Solution containing 66% Resin in relevant Solvent
	1 kg
	1
	
	Adipic Acid
	0.107 kg

	
	
	
	2
	
	Isophthalic Acid
	0.308 kg

	
	
	
	3
	
	Monoethylene Glycol
	0.057 kg

	
	
	
	4
	
	Diethylene glycol
	0.232 kg

	
	
	
	5
	
	Toluene Di-Iso-Cyanate
	0.018 kg

	
	
	
	6
	
	Ethyl Acetate/ Methyl Ethyl Ketone
	0.340 kg

	
	
	
	7
	
	1,6-Hexane diol
	0.019 kg

	H238
	Polyvinyl Acetate Homopolymer Emulsion(having minimum solid content 49%)
	1 kg
	1
	
	Vinyl Acetate Monomer
	0.480 kg

	
	
	
	2
	
	Polyvinyl Alcohol
	0.021 kg

	H239
	PP laminated/ coated woven sacks (Lamination/ coating of PP)
	1 kg
	1
	
	PP Granules
	1.100 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	PP Granules for lamination/ coating
	1.050 kg/kg content of the relevant material in the export product

	H240
	PP woven fabrics laminated/ coated
	1 kg
	1
	
	PP Granules
	1.080 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	Granules of material used for lamination/ coating
	1.050 kg/kg content of the relevant material in the export product

	H241
	PP Woven Sacks with/without liner
	1 kg
	1
	
	PP Granules
	1.10 kgs/kg content in export

	
	
	
	2
	
	Plastic Material Used for liner
	1.05 kgs/kg content in export

	H242
	PP woven sacks laminated or coated with liner
	1 kg
	1
	
	PP Granules
	1.10 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	PP Granules for lamination / coating
	1.050 kg/kg content of the relevant material in the export product

	
	
	
	3
	
	Granule of material used for liner
	1.050 kg/kg content of the relevant material in the export product

	H243
	PP/HDPE Tarpauline
	1 kg
	1
	
	Granule of material (i.e. PP/HDPE) used for manufacture of Tarpauline
	1.080 kg

	H244
	PP/HDPE Tarpauline coated wth LDPE
	1 kg
	1
	
	Granule of material (i.e. PP/HDPE) used for manufacture of Tarpauline
	1.080 kg/kg content of the relevant material in the export product

	
	
	
	2
	
	LDPE Granule (for coating)
	1.050 kg/kg content of the relevant material in the export product

	Note: In the application alongwith the description of the export product, the HDPE or woven Fabric contents (percentage by weight) and LDPE Liner contents (percentage by weight) shall also be indicated.

	H245
	Printed baby feeding bottle with rubber nipple(polycarbonate bottle,hood, cap and insert) rubber nipple contains silicon rubber/natural rubber having minimum 98% rubber content.
	1 Bottle
	1
	
	Polycarbonate Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Polypropylene Granules
	1.05 kg/kg content in export.

	
	
	
	3
	
	Liquid Silicon Rubber/Natural Rubber
OR
	1.08 kg/kg of relevant Rubber content in the export product.

	
	
	
	4
	
	Printing Inks
	0.2 gm per Bottle.

	H246
	Printed baby feeding bottle with rubber nipple(polypropylene bottle, hood, cap and insert) rubber nipple contains silicon rubber/natural rubber having minimum 98% rubber content.
	1 Bottle
	1
	
	Polypropylene Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Liquid Silicon Rubber/Natural Rubber
OR
	1.08 kg/kg.of Relevant Rubber content in the export

	
	
	
	3
	
	Printing inks
	0.2 gm/Bottle

	H247
	Printed baby Soother(polycarbonate based)with latex natural rubber nipples having minimum 98% rubber content.
	1 No.
	1
	
	Polycarbonate Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Latex Natural Rubber (containing 60% DRC).
	1.80 kg/kg Rubber content in the export product.

	
	
	
	3
	
	Printing Inks
	0.1 gm/No.

	H248
	Printed baby soother(polypropylene based) with latex natural rubber nipples having minimum 98% rubber content.
	1 No.
	1
	
	Polypropylene Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Latex Natural Rubber (containing 60% DRC)
	1.80 kg/kg Rubber content in export.

	
	
	
	3
	
	Printing Inks
	0.1 gm/No.

	H249
	Printed drinking/juice Cup(Polycarbonate cup and Polypropylene cap)
	1 No.
	1
	
	Polycarbonate Granules
	1.05 kg/kg content in export.

	
	
	
	2
	
	Polypropylene Granules
	1.05 kg/kg content in export.

	
	
	
	3
	
	Printing Inks
	0.2 gm/No.

	H250
	PTFECoated Glass fabrics
	1 Sq. Meter
	1
	
	Glass Fabric of relevant GSM
	1.05 Sq. Meter.

	
	
	
	2
	
	PTFE Dispersions (on solid basis)
	1.05 kg/kg content of PTFE in export


	H251
	PU Lacquered flooring impregnated with glass fibre tissue/glass fleece tissue or with glass fibre reinforced rigid PVC sheet, coating weight 2325 gm. +/- 5%, thickness 3.2 mm +/- 0.25 mm.
	1 Sq. Mtr.
	1
	
	PVC Resin
OR
	1365 gms

	
	
	
	1
	a)
	Ethylene
	327.60 gms

	
	
	
	
	b)
	Ethylene Dichloride
	1156.20 gms

	
	
	
	
	c)
	Oxy chloro Catalyst
	0.258 gm

	
	
	
	
	d)
	Solvent Naphtha consisting of C-9, C-10, C-11 & C-12 aromatics alongwith 2% non aromatics
	1.15 gms

	
	
	
	
	e)
	Poly Vinyl Alcohol (88%/72.5%)
	1.5 gm

	
	
	
	
	f)
	Hydroxy propyl Cellulose/Hydroxy Propyl Methyl Cellulose
	0.68 gm

	
	
	
	
	g)
	Proxy Ethylene, 4-Sorbitol Monolaurate
	0.008 gm

	
	
	
	
	h)
	Disodium salt of Polymerised Resorcinol
OR
	0.008 gm

	
	
	
	2
	
	Plasticizer (Phthalic, NonPhthalic epoxy etc.)
OR
	1055 gms

	
	
	
	2
	a)
	Phthalic Anhydride
	420 gms

	
	
	
	
	b)
	Ethyl Hexanol (Octanol)
	739 gms

	
	
	
	3
	
	PVC Stabilizer (Toxic, Non-Toxic, UV, Tin)
	40 gms

	
	
	
	4
	
	Processing Aids (Impact Modifier/ Humidity Eliminator/Lubricants/ Dispersing Agents/ Luxiol/Syloid/ Flotting/Matting Agent)
	62 gms

	
	
	
	5
	
	Silicone Oil
	3 gms

	
	
	
	6
	
	Titanium Dioxide (Anetose/Rutile)
	22 gms

	
	
	
	7
	
	Surfactant/Silicone Profoamer/ Foam stabilizer
	28 gms

	
	
	
	8
	a)
	Microlith Pigments
OR
	5 gms

	
	
	
	8
	b)
	Microlith WA Pigments
OR
	5 gms

	
	
	
	8
	c)
	Water Based Printing Inks (Medium/Colour)
	60 gms

	
	
	
	9
	a)
	Glass Fibre Tissue/Glass Fleece Tissue
OR
	64 gms

	
	
	
	9
	b)
	Glass Fibre Reinforced Rigid PVC Sheet
	206 gms

	
	
	
	10
	
	Methyl Ethyl Ketone
	25 gms

	
	
	
	11
	
	Polyurethene Lacquer (Total Solids 35%)
	71.42 gms

	
	
	
	12
	
	Polyester Film Adhesive Tape & Kreppe/Masking Adhesive Tapes having width of 30"x65 Meter subject to maximum of 2% of FOB value of export.
	0.0003 Roll

	
	
	
	13
	
	Blowing Agent
	8 gms

	
	
	
	14
	
	Inhibitor
	2 gms

	Note:1. In case of variation in coating weight, the quantity of item of imports viz. all except 9 and 10 will be arrived at by adopting the following formula: A x B/2325 gms.
A= Qty. allowed for 2325 gm. coating weight.B=Coating weight in gms of floor covering.2(a) The minimum weight of 58 gm of item 9(a) will be in addition to the coating weight in all types of floor covering in case glass fibre tissue/glass fleece tissue is opted for as substrate.2(b) The minimum weight of 187 gm of item 9(b) will be in addition to the coating weight in all types of floor covering in case glass fibre reinforced rigid PVC Sheet is opted for as substrate.
3. In case of variation in percentage, total solid content of PU Lacquer, quantity of import can be arrived at by adopting the following formula:25 x 100/xWhere x = Percentage total solid content of polyurethane Lacquar to beimported.
4. Methyl Ethyl Ketone i.e. item No.10 is permitted only if item No.8(a) Microlith Pigment is opted for.5. Processing Aid i.e. item No.4 will read as 78 gms in case of alternative item 8(a) or 8(b).

	H252
	PU Unit Sole
	1 kg.
	1
	
	Polyol
	515 gms

	
	
	
	2
	
	Isocynate
	451 gms

	
	
	
	3
	
	Catalyst for Polyurethane
	53 gms

	
	
	
	4
	
	Pigment Paste
	31 gms

	
	
	
	5
	
	Release Agent
	40 gms

	H253
	Deleted
	
	
	
	
	

	
	
	
	
	
	
	

	H254
	PVC Coated Paper(Wall Paper) with coating weight 100 gm/sq.mtr. +/- 5% with base paper of 80 gms +/- 5%
	1 sq.mtr.
	1
	
	PVC Resin
	60.2 gms.

	
	
	
	2
	
	PVC Plasticizer
	42.1 gms.

	
	
	
	3
	
	Titanium Dioxide/Pigment
	13.6 gms.

	
	
	
	4
	
	PVC Stabilizer
	2.1 gms.

	
	
	
	5
	
	Base Paper (80 gms)
	96 gms.

	
	
	
	6
	
	Blowing/Foaming Agent
	2.5 gms.

	
	
	
	7
	
	Solvant(MEK/Toluene/MIBK/
Cyclohexanone)
	60 gms.

	Note: 1. In case of variation in coating weight,Item No. 1 to 5 may be allowed adopting the following formula:
A x B/100
where A = Quantity allowed for 100 gms of coating weight per Sq.Mtr and
B = Coating weight of PVC coated paper (wall paper)to be exported/Sq.Mtr.2. The Quanity of item No.7 i.e., solvent will not change with change of coating weight.3. In case of variation in GSM ofBase paper, the quantity may be allowed adopting the following formula C x D 80 where C = quantity of Base paper allowed andD = GSM of Base Paper to be exported per Sq.Mtr ofthe product.

	H255
	PVC compound (Shoe sole Grade)
	1 kg
	1
	
	PVC Resin
	0.5329 kg

	
	
	
	2
	
	DOP
	0.3997 kg

	
	
	
	3
	
	Epoxidized Soyabean Oil
	0.0319 kg

	
	
	
	4
	
	Ba-Cd_Zn Stabilizer
	0.0159 kg

	
	
	
	5
	
	Calcium Carbonate
	0.0639 kg

	
	
	
	6
	
	Stearic Acid
	0.0053 kg

	
	
	
	7
	
	Pigments
	0.0080 kg

	H256
	PVC Cushion Vinyl Floor covering Impregnated with Glass Fliss Tissue Coating Weight 1300 gms. plus or Minus 5%
	1 Sq. Mtr.
	1
	
	PVC Resin
	728.00 gms.

	
	
	
	2
	
	Plasticizer
	532.32 gms.

	
	
	
	3
	
	PVC Stabilizer
	15.20 gms.

	
	
	
	4
	
	Processing Aids.
	4.00 gms.

	
	
	
	5
	
	Silicon Emulsion
	1.28 gms.

	
	
	
	6
	
	Titanium Dioxide
	11.40 gms.

	
	
	
	7
	
	Surfactant
	22.40 gms.

	
	
	
	8
	
	Microlith Pigments
	2.60 gms.

	
	
	
	9
	
	Glass Fibre Tissue
	64.00 gms.

	
	
	
	10
	
	Methyl Ethyl Ketone
	25.00 gms.

	H257
	PVC Cushion Vinyl flooring impregnated with glass fibre tissue/glass fleece tissue or with glass fibre reinforced rigid PVC Sheet, coating weight 2300 gms +/- 5%, thickness 3.2 mm +/- 0.25 mm.
	1 Sq. Mtr.
	1
	
	PVC Resin
OR
	1365 gms

	
	
	
	1
	a)
	Ethylene
	327.60 gms

	
	
	
	
	b)
	Ethylene Dichloride
	1156.20 gms

	
	
	
	
	c)
	Oxy chloro Catalyst
	0.258 gm

	
	
	
	
	d)
	Solvent Naphtha consisting of C-9, C-10, C-11 & C-12 aromatics alongwith 2% non aromatics
	1.15 gms

	
	
	
	
	e)
	Poly Vinyl Alcohol (88%/72.5%/55%)
	0.805 gm

	
	
	
	
	f)
	Hydroxy propyl Methyl Cellulose/ Hydroxy Propyl Cellulose
	0.15 gm

	
	
	
	
	g)
	Proxy Ethylene, 4-Sorbitol Monolaurate
	0.008 gm

	
	
	
	
	h)
	Disodium salt of Polymerised Resorcinol
	0.008 gm

	
	
	
	2
	
	Plasticizer (Phthalic, NonPhthalic epoxy etc.)
OR
	1055 gms

	
	
	
	2
	a)
	Phthalic Anhydride
	420 gms

	
	
	
	
	b)
	Ethyl Hexanol (octanol)
	739 gms

	
	
	
	3
	
	PVC Stabilizer (Toxic, Non-Toxic, UV, Tin)
	40 gms

	
	
	
	4
	
	Processing Aids (Impact Modifier/ Humidity Eliminator/Lubricants/ Dispersing Agents/ Luxiol/Syloid/ Flotting/Matting Agent)
	62 gms

	
	
	
	5
	
	Silicone Oil
	3 gms

	
	
	
	6
	
	Titanium Dioxide (Anetose/Rutile)
	22 gms

	
	
	
	7
	
	Surfactant/Silicone Profoamer/ Foam stabilizer
	28 gms

	
	
	
	8
	a)
	Microlith Pigments
OR
	5 gms

	
	
	
	8
	b)
	Microlith WA Pigments
OR
	5 gms

	
	
	
	8
	c)
	Water Based Printing Inks (Medium/Colour)
	60 gms

	
	
	
	9
	a)
	Glass Fibre Tissue/Glass Fleece Tissue or
	64 gms

	
	
	
	10
	
	Methyl Ethyl Ketone
	25 gms

	
	
	
	11
	
	Polyester Film Adhesive Tape & Kreppe/Masking Adhesive Tapes having width of 30"x65 Meter subject to maximum of 2% of FOB value of export.
	0.0003 Roll

	
	
	
	12
	
	Blowing Agent
	8 gms

	
	
	
	13
	
	Inhibitor
	2 gms

	Note:1. In case of variation in coating weight, the quantity of item of imports viz. all except 9 and 10 will be arrived at by adopting the following formula:A x B/2300 gms.
Where, A=Qty. allowed for 2300 gm. coating weight.
B= Coating weight in gms. of floor covering.2(a) The minimum weight of 58 gm of item 9(a) will be in addition to the coating weight in all types of floor covering in case glass fibre tissue/glass fleece tissue is opted for as substrate.2(b) The minimum weight of 187 gm of item 9(b) will be in addition to the coating weight in all types of floor covering in case glass fibre reinforced rigid PVC sheet is opted for as substrate.3. Methyl Ethyl Ketone i.e. item No.10 is permitted only if item No.8(a) Microlith Pigment is opted for.4. Processing Aid i.e. item No.4 will read as 78 gms in case of alternative item 8(a) or 8(b).

	H258
	PVC Drift Eliminator
	1 kg
	1
	
	PVC Transparent Rigid Sheet of Thermo Forming Non-toxic Grade Black
	1.02 kg/kg content in export product

	H259
	PVC Electrical Insultation Tapes
	1 Kg
	1
	
	PVC Film
	0.814 Kg.

	
	
	
	2
	
	Toluene
	0.084 Kg.

	
	
	
	3
	
	Poly terpene Resin
	0.012 Kg.

	
	
	
	4
	
	Petroleum Hydrocarbon resin
	0.013 Kg.

	
	
	
	5
	
	Di-Tertiary amyl Hydroquinone
	0.0007 Kg.

	
	
	
	6
	
	Synthetic Rubber/SBR
	0.022 Kg.

	H260
	PVC EPDM Door Seal
	100 kgs
	1
	
	EPDM Rubber
	14.19 kgs

	
	
	
	2
	
	Rubber Chemicals:
Antioxidants/ Accelerator/ Retarders and Peptizer
	0.28 kg

	
	
	
	3
	
	Carbon Black
	8.7 kgs

	
	
	
	4
	
	PVC Resin
	16.72 kgs

	
	
	
	5
	
	D.O.P
	11.15 kgs

	
	
	
	6
	
	Steel Strip
	44.64 kgs

	
	
	
	7
	
	PU Adhesive
	3.46 kgs

	
	
	
	8
	
	Miscellaneous Chemicals:
	

	
	
	
	
	a)
	Process Oil
	5.8 kgs

	
	
	
	
	b)
	Stearic Acid
	0.1 kg (Restricted to 1% of Rubber)

	H261
	Soft Travel Goods i.e. Suit Cases, Brief Cases, Luggage, Uprights, Backs, Packs, Totes, etc.
	1 No
	1
	
	Relevant PVC Leather cloth backed with Cotton/ Rayon/ Nylon/ Polyester Fabric
	1.10 Sq. Mtr/Sq. Mtr content in export product

	
	
	
	2
	
	Relevant Synthetic Fabric Coated/ Uncoated with/ without backing
	1.10 Sq. Mtr. per Sq. Mtr. content in the export product.

	
	
	
	3
	
	PVC Film/ Sheet
	1.10 Sq. Mtr. per Sq. Mtr. content in the export product.

	
	
	
	4
	
	Zip Fastener/ Zipper
	1.02 Mtr/ Mtr content in export product.

	
	
	
	5
	
	Zip Slider
	Net to Net

	
	
	
	6
	
	Castor Wheels/ Wheel Housing
	Net to net.

	
	
	
	7
	
	Trolly/ Cart
	Net to net.

	
	
	
	8
	
	Logo Plate/ Name Plate/ Back Plate
	102 Nos./ 100 Nos. content in the export product.

	
	
	
	9
	
	Fastners like Screw/ Rivets, Washers
	102 Nos./ 100 Nos. content in the export product.

	
	
	
	10
	
	Relevant Piping
	1.02 Mtr./ Mtr. content in the export product.

	
	
	
	11
	
	Lock/ Combination Lock/ Turn Lock/ assembled/ unassembled
	Net to net.

	
	
	
	12
	
	Metal fitting like snap hooks, fastners, buckles, "D" ring
	102 Nos./100 Nos. content in the export product

	
	
	
	13
	
	P.P Webbing
	1.02 mtr./ mtr. content in the export product

	
	
	
	14
	
	Side Handle
	Net to Net

	
	
	
	15
	
	Shoulder pad
	Net to Net

	H262
	PVC Fill Media
	1 kg
	1
	
	PVC Resin (Suspension Grade)
	0.900 kg

	
	
	
	2
	
	Titanium Dioxide
	0.058 kg

	
	
	
	3
	
	Processing Aid
	0.011 kg

	
	
	
	4
	
	Impact Modifier
	0.014 kg

	
	
	
	5
	
	Parafin wax
	0.005 kg

	
	
	
	6
	
	Calcium Citrate
	0.003 kg

	
	
	
	7
	
	Lubricant/Heat stabiliser
	0.037 kg

	
	
	
	8
	
	Filler(Calcium Carbonate)
	0.020 kg

	
	
	
	9
	
	Carbon Black
	0.002 kg

	H263
	PVC Films for Photo Album
	1 kg
	1
	
	PVC Resin
	0.897 kg

	
	
	
	2
	
	Plasticizer
	0.113 kg

	
	
	
	3
	
	Stabilizer
	0.015 kg

	H264
	PVC Foam Sponge Sheet (Unsupported) weight - 1000 gms per Sq.mtr. +/-5%
	1 Sq. Mtr.
	1
	
	PVC Resin
	611.0 gms

	
	
	
	2
	
	PVC Plasticizer (Phthalic and Non-Phthalic)
	396.2gms

	
	
	
	3
	
	Blowing Agent
	24.4 gms

	
	
	
	4
	
	Titanium Dioxide/ Pigments
	46.6 gms

	
	
	
	5
	
	Processing Aid/Stabilizers
	16.4 gms

	
	
	
	6
	
	Release Paper
	0.50 Sq. Mtr./ Sq. mtr.

	Note: In case of variation in coating weight/ PVC Foam Sponge Sheet weight the quantity of inputs at S.Nos. 1 to 5 would be determined as under:-
A x B
1000
Where A = Quantity permitted above for 1000 gms coating/ export product weight/ Sq.Mtr.
B=Coating wt./ wt. of PVC Foam Sponge Sheet (Unsupported)/ Sq. Mtr. to be exported.

	H265
	PVC Footwear
	1 kg.
	1
	
	PVC Resin
	0.5329 kg

	
	
	
	2
	
	Plasticizer (DOP)
	0.3997 kg

	
	
	
	3
	
	Stabilizers (Ba-Cd-Zn)
	0.0159 kg

	
	
	
	4
	
	Antimony Trioxide
	0.014 kg

	
	
	
	5
	
	Pigments
	0.008 kg

	
	
	
	6
	
	Solvents (MEK/Xylene)
	0.0015 kg

	H266
	PVC Hoses Reinforced with Synthetic Yarn
	1 kg
	1
	
	PVC Resin
	0.600 kg

	
	
	
	2
	
	PVC Plasticiser(DOP/Epoxy Plasticiser)
	0.330 kg

	
	
	
	3
	
	PVC Stabilizer
	0.030 kg

	
	
	
	4
	
	Relevant Colours
	0.003 kg

	
	
	
	5
	
	Polyester Yarn
	0.09 kg

	H267
	PVC inflatable Toys
	1 kg
	1
	
	PVC Sheet
	1.4604 kg

	H268
	Drop Cloth made of PVC Leather Cloth/PVC Leather Cloth/Foam Leather Cloth, Single sided/ Both sided (PVC Tarpaulin) having coating weight 1000 gms. per Sq. Meter +/- 5%
	1 Sq. Mtr.
	1
	
	PVC Resin 
OR
	617.52 gms.

	
	
	
	1
	a)
	Oxy Chloro Catalyst
	0.117 gms

	
	
	
	
	b)
	Ethylene
	148.20 gms

	
	
	
	
	c)
	Ethylene Di-Chloride
	523.03 gms

	
	
	
	
	d)
	Solvent Naphtha consisting of C-9, C-10, C-11 and C-12 aromatic alongwith 2% non-aromatics
	0.520 gms

	
	
	
	
	e)
	PV Alcohol (72.5%)
	0.364 gms

	
	
	
	
	f)
	PV Alcohol (88%)
	0.278 gms

	
	
	
	
	g)
	Hydroxy Propyl Methyl Cellulose Metolose 65 51 +/-50
	0.068 gms

	
	
	
	
	h)
	Propoxy Ethylene 4-Sorbitol Mono-laurate
	0.0036 gms

	
	
	
	
	i)
	Disodium Salt of Polymerised Resorcinol
	0.0038 gms

	
	
	
	2
	
	PVC Plasticizer (Phthalic, Non-Polymeric) 
OR
	429.20 gms

	
	
	
	2
	a)
	2-Ethyl Hexanol (Octanol)
	300.44 gms

	
	
	
	
	b)
	Phthalic Anhydride
	171.00 gms

	
	
	
	3
	
	Titanium Dioxide/Pigments
	29.20 gms

	
	
	
	4
	
	Release Paper (155-240 gms/Sq. Meter)
	0.55 Sq. Meter

	
	
	
	5
	
	Processing Aid/Stabilizers
	14.60 gms

	
	
	
	6
	
	Blowing /Foaming Agent
	21.90 gms

	
	
	
	7
	
	Polyester Adhesive Tapes having maximum width of 30" subject to maximum of 2% of FOB value of export product.
	0.0003 Roll

	
	
	
	8
	
	Yarn (Polyester/ Cotton Viscose) & combination there of in varying proportion for backing material)
OR
	1.06 Kg/Kg of respective item contained in the export product.

	
	
	
	8
	
	Relevant Woven/Non woven/Knitted Fabric for backing material
	1.05 Sq. Meter/Sq. Meter contained in the export product.

	
Note : 1. In case of variation in coating weight the quantity of imports of PVC Resin or its inputs, PVC Plasticizer,or 2-Ethyl Hexanol (Octanol) and Phthalic Anhydride, Blowing/Foaming Agent, Titanium Di-oxide/Pigment, Processing Aid to be allowed by adopting the following formula:
AxB/1000 
Where A= Quantity allowed for 1000 gmsCoating weight/Sq. Meter. and B = Coating weight of leather cloth proposed to be exported per Square Meter. The quantity of other items will not change.

	H269
	PVC Mist Eliminator/Tube Settler
	1 kg
	1
	
	PVC Resin (Suspension Grade)
	920.6 gms

	
	
	
	2
	
	Plasticizer
	4.6 gms

	
	
	
	3
	
	Processing Aids
	9.1 gms

	
	
	
	4
	
	Impact Modifier
	7.9 gms

	
	
	
	5
	
	Paraffin Wax
	5.5 gms

	
	
	
	6
	
	Calcium Sitrate
	9.1 gms

	
	
	
	7
	
	Lubricant & Heat Stabiliser
	36.8 gms

	
	
	
	8
	
	Fillers
	55.1 gms

	
	
	
	9
	
	Carbon Black
	1.3 gms

	H270
	PVC Printed Leather Cloth/Foam Leather Cloth having coating weight 1000 gms. per square meter +/- 5%
	1 sq.mtr.
	1
	
	PVC Resin
	587.38 gms.

	
	
	
	2
	
	PVC Plasticizer (Phthalic, Non-phthalic Epoxy)
OR
	405.30 gms.

	
	
	
	2
	a)
	2-Ethyl Hexanol (octanol)
	283.71 gms.

	
	
	
	
	b)
	Phthalic Anhydride
	161.51 gms.

	
	
	
	3
	
	Anti-fungal Agent
	7.58 gms.

	
	
	
	4
	
	Butyl Benzyl Phthalate Plasticizer
	22.72 gms.

	
	
	
	5
	
	Polymeric Plasticizer
	7.58 gms.

	
	
	
	6
	
	Blowing/Foaming Agent
	7.58 gms.

	
	
	
	7
	
	Titanium Dioxide/Pigments
	30.28 gms.

	
	
	
	8
	
	Microlith Pigments/Pearl Pigments (To be allowed only for the Leather Cloth having Pearl effect)
	7.58 gms.

	
	
	
	9
	
	Flatting Agent/Matting Agent
	13.62 gms.

	
	
	
	10
	
	Solvent (Toluene/Cylohexanone/MEK/MIBK)
	40.00 gms.

	
	
	
	11
	
	Polyurethene Lacquer(Solvent or water base )(Total solid content upto 25%)
	36.34 gms.

	
	
	
	12
	
	Processing Aid
	7.58 gms.

	
	
	
	13
	
	Release Paper (155-240 gms./sq.mtr)
	0.55 sq.mtr.

	
	
	
	14
	
	Polyester Adhesive Tape having max. width of 30" subject to maximum of 2% of FOB value of export product
	0.0003 Roll

	
	
	
	15
	
	Yarn (Polyester/Cotton Viscose and combination there of in varying proportion) for backing material.
OR
	1.06 kg./kg. of respective item contained in the export product

	
	
	
	15
	
	Woven/Non-Woven Fabric for backing material.
	1.05 Sq.Mtr./Sq.Mtr contained in export product.

	Note :1. In case of variation in coating weight, the quantity of imports of PVC Resin, PVC Plasticizer or 2-Ethyl Hexanol (Octanol) and Phthalic Anhydride, Anti-fungal Agent, Butyl Benzyl Phthalate, Plasticizer, Polymeric Plasticizer, Blowing/Foaming Agent,Titanium Di-oxide/Pigment, Microlith Pigments/ Pearl Pigments, Flatting Agent/Matting Agent and item 10, 11 and 12 to be allowed adopting the following formula:
AxB/1000
Where A = Quantity allowed for 1000 gms coating weight/Sq. Meter. and B=Coating weight of leather cloth proposed to be exported per Square Meter. The quantity of other items will not change. 2. In case of variation of solid content of Item No. 11 i.e. Polyurethene Lacquer, the quantity can be arrived at by the following formula: 
Z=36-34 gms x 25/Y 
Where Z=Quantity to be allowed for import. Y =% solid content of the proposed import.

	H271
	PVC Profiles
	100 Kgs
	1
	
	PVC
	47.10 Kgs

	
	
	
	2
	
	Carbon Black
	0.60 Kg

	
	
	
	3
	
	Stearic Acid
	0.200Kg

	
	
	
	4
	
	DOP
	31.50 Kgs

	
	
	
	5
	
	Calcium Carbonate
	25.20 Kgs

	
	
	
	6
	
	Barium/ Zinc Stabiliser
	0.40 Kg

	H272
	PVC Profiles with steel strips
	100 Kgs
	1
	
	PVC
	29.67 Kgs

	
	
	
	2
	
	Carbon Black
	4.89 Kgs

	
	
	
	3
	
	DOP
	14.85 Kgs

	
	
	
	4
	
	Calcium Carbonate
	4.89 Kgs

	
	
	
	5
	
	Steel strip (Unpunched)
	61.30 Kgs

	H273
	PVC Reinforced Hoses Reinforcement with rigid PVC in soft PVC)
	1 Kg
	1
	
	PVC Resin
	0.705 Kg.

	
	
	
	2
	
	Di-Octyl Phthalate/Epoxy Plasticizer.
	0.253 Kg.

	
	
	
	3
	
	Impact Modifier Processing aids.
	0.057 Kg.

	
	
	
	4
	
	PVC Stabilizers (Such as liquid barium-Cadmium, Zinc Barium Cadmium, Complex Stabilizers and Lead Stabilizers)
	0.035 Kg.

	H274
	PVC Resin
	1 kg
	1
	
	Vinyl chloride Monomer
	1.021 kg

	
	
	
	2
	
	Relevant Catalyst
	0.0005kg

	
	
	
	3
	
	Polyvinyl Alcohol
	0.0007kg

	
	
	
	4
	
	Cethyl, Stearyl Alcohol
	0.0006kg

	H275
	PVC Resin
	1 kg
	1
	
	Naphtha
	1.140 kg

	H276
	PVC Resin
	1000 kg
	1
	
	Ethylene
	240.00 kgs

	
	
	
	2
	
	Ethylene Dichloride
	847.00 kgs

	
	
	
	3
	
	Oxychloro Catalyst 
OR
i)Oxy Catalyst
ii)Polymerisation Catalyst (100% basis)(Dilauroyl Peroxide/ 2-Ethyl Hexyl Peroxydicarbonate)
	0.189 kg

0.12 kg
0.069 kg

	
	
	
	4
	
	Solvent Naptha consisting of C-9, C-10, C-11 and C-12 Aromatics alongwith 2% Non Aromatics.
	0.848 kg

	
	
	
	5
	
	Poly Vinyl Alcohol (88%/72.5%/55%)
	1.10 kg

	
	
	
	6
	
	Hydroxyl Propropyl Methyl Cellulose/ Hydroxyl Propyl Cellulose
	0.500 kg

	
	
	
	7
	
	Proxyethylene, 4 Sorbitol Monolaurate
OR
Organic Coating Agent (Alfa 8/NOXOL)
	0.0059 kg


0.0050 kg

	
	
	
	8
	
	Disodium Salt of Polymerised Resorcinol
OR
Mixture of Monocyclic Terpene Hydrocarbon (Depanol)
	0.005 kg


0.005 kg

	H277
	PVC Rigid Free Foam Board
OR
Cellular Film, Foil & Sheets of PVC Rigid Free Foam Board
	1 Kg
	1
	
	PVC Resin
	0.816 Kg.

	
	
	
	2
	
	PVC Stabilizer
	0.041 Kg.

	
	
	
	3
	
	Pigments
	0.041 Kg.

	
	
	
	4
	
	PVC Processing Aid/Impact Modifier
	0.204 Kg.

	
	
	
	5
	
	PVC Lubricants
	0.049 Kg.

	
	
	
	6
	
	Blowing Agent
	0.020 Kg.

	
	
	
	7
	
	P.E. Wax
	0.006 Kg.

	
	
	
	8
	
	Masking Film
	0.018 Kg.

	H278
	PVC Rigid Film/ Sheet (General purpose/ Stationary Grade)
	1 kg
	1
	
	PVC Resin
	0.916 kg

	
	
	
	2
	
	Plasticizer (Epoxidised Soya bean Oil)
	0.018 kg

	
	
	
	3
	
	Pigments
	0.005 kg

	
	
	
	4
	
	PVC Stabilizer
	0.028 kg

	
	
	
	5
	
	PVC Processing Aid
	0.014 kg

	
	
	
	6
	
	ABS Resin (PVC impact modifier)
	0.073 kg

	
	
	
	7
	
	Lubricants
	0.009 kg

	Note: An additional 5% quantity for all the above items may be allowed in case the above resultant products are Cut Size films/sheets/(viz. Size A4, A3 etc.).

	H279
	PVC riser main pipe with Nitrile rubber fittings for Hand pump
	1 No. (Net wt. not less than 4.2 kg)
	1
	
	PVC Resin
	3.96 Kg.

	
	
	
	2
	
	Master Batch
	0.304 Kg.

	
	
	
	3
	
	Titanium Dioxide
	0.042 Kg.

	
	
	
	4
	
	Nitrile Rubber
	0.104 Kg.

	H280
	PVC Flexible Sheet/ Film
	1 kg
	1
	
	PVC Resin
	0.6673 kg

	
	
	
	2
	
	Plasticizer
	0.367 kg

	
	
	
	3
	
	Stabilizer
	0.0266 kg

	H281
	PVC Soles
	1 M T
	1
	
	PVC Resin
	0.5329 MT

	
	
	
	2
	
	Plasticizer (DOP)
	0.3997 MT

	
	
	
	3
	
	Stabilizer (Ba-Cd-Zn)
	0.0159 MT

	
	
	
	4
	
	Antimony Trioxide
	0.014 MT

	
	
	
	5
	
	Pigments
	0.008 MT

	
	
	
	6
	
	Solvents (MEK/Xylene)
	0.0015 MT

	H282
	PVC Transparent Hose
	1 kg
	1
	
	PVC Resin
	0.706 kg

	
	
	
	2
	
	D.O.P.
	0.282 kg

	
	
	
	3
	
	Stabilizer
	0.040 kg

	H283
	PVC Vinyl lace table cover (Square & Rectangular Shape)
	1 Kg
	1
	
	PVC Resin
	0.580 kg.

	
	
	
	2
	
	PVC Plastisizer
	0.464 kg.

	
	
	
	3
	
	PVC Stabilizer
	0.0288 kg.

	
	
	
	4
	
	Processing Aid
	0.0574 kg.

	
	
	
	5
	
	Pigments
	0.0288 kg.

	H284
	PVC Vinyl lace table cover of 54" Dia (Round Shape)
	1 Kg
	1
	
	PVC Resin
	0.667 kg.

	
	
	
	2
	
	PVC Plastisizer
	0.5336 kg.

	
	
	
	3
	
	PVC Stabilizer
	0.0331 kg.

	
	
	
	4
	
	Processing Aid
	0.0660 kg.

	
	
	
	5
	
	Pigments
	0.0331 kg.

	H285
	Rail pads made out of EVA for concrete sleeper
	1 Kg
	1
	
	EVA Moulding powder
	1.025 Kg.

	
	
	
	2
	
	Carbon Black
	0.025 Kg.

	H286
	Reconstructed Synthetic Block(containing 50% Melamine Resin by weight)
	1 MT
	1
	
	Melamine Resin
	550 kgs

	H287
	Rigid PVC Casing Pipes
	1 kg
	1
	
	PVC Resin
	0.966 kg

	
	
	
	2
	
	Master Batch
	0.074 kg

	
	
	
	3
	
	Titanium Dioxide
	0.010 kg

	H288
	Rigid PVC Conduit Fittings such as junction boxes, Couplers, saddles with base, famale Adaptors, Switch boxes, Adaptable boxes, extension rings, reducers, elbows tees, loop in boxes, Bends etc.
	1 kg
	1
	
	PVC Resin (Suspension grade)
	0.9526 kg

	
	
	
	2
	
	Stabilisers other than Tin based stabiliser
	0.0190 kg

	
	
	
	3
	
	Epoxy Plasticizers
	0.0095 kg

	
	
	
	4
	
	Impact modifiers
	0.0190 kg

	
	
	
	5
	
	Processing aid
	0.0190 kg

	
	
	
	6
	
	Lubricant (Fatty Alcohols)
	0.0190 kg

	
	
	
	7
	
	Pigments
	0.0047 kg

	H289
	Rigid PVC Film/ Sheet/ Foil (Vacuum forming grade)
	1 Kg
	1
	
	PVC Resin
	0.830 Kg

	
	
	
	2
	
	Plasticizer (Epoxidised Soyabean Oil)
	0.055 Kg

	
	
	
	3
	
	Pigments
	0.005 Kg

	
	
	
	4
	
	PVC Stabilizer
	0.030 Kg

	
	
	
	5
	
	PVC Processing Aid
	0.016 Kg

	
	
	
	6
	
	Impact Modifier for PVC
	0.102 Kg

	
	
	
	7
	
	Lubricants
	0.012 Kg

	H290
	Rigid PVC well casing/screen pipes
	100 kgs
	1
	
	PVC Resin
	98.18 Kgs.

	
	
	
	2
	
	Master Batch of following ingredients:
	

	
	
	
	
	1)
	PVC Stabilizer
	3.34 Kgs.

	
	
	
	
	2)
	Lubricant
	1.17 Kgs.

	
	
	
	
	3)
	Flow Promoter
	4.14 Kgs.

	
	
	
	
	4)
	Impact Modifier
	4.14 Kgs.

	
	
	
	3
	
	Filler (Calcium Carbonate)
	4.14 Kgs.

	
	
	
	4
	
	Colouring Pigments
	0.0015 Kg.

	
	
	
	5
	
	Titanium Dioxide
	3.62 Kgs.

	H291
	Roller Pens
	100 pcs
	1
	
	Roller Pen Tips with feeder
	Net + 2% wastage

	
	
	
	2
	
	Writing Inks 
OR
	173.25 gm

	
	
	
	2
	
	Dyestuff/Resins
	17 gm

	
	
	
	3
	
	Metal Clips 
OR
	Net + 2% wastage

	
	
	
	3
	
	SS Strips for Clips
	184 gm

	
	
	
	4
	
	Polyethylene 
OR
	157.5 gm

	
	
	
	4
	
	Plastic Extruded/ Moulded components
	Net + 2% wastage

	
	
	
	5
	
	Synthetic Filters
	Net + 2% wastage

	
	
	
	6
	
	Roller Refills
	Net + 2% wastage

	
	
	
	7
	
	Rubber Seal
	Net + 2% wastage

	
	
	
	8
	
	Printing Ink
	1.05 gm

	H292
	Rosin Modified Phenolic Resin
	1000 kgs.
	1
	
	Gum Rosin
	689 kgs

	
	
	
	2
	
	Para Tertiary Butyl Phenol
	230 kgs

	
	
	
	3
	
	Paraformaldehyde
	115 kgs

	
	
	
	4
	
	Pentaerythritol
	115 kgs

	H293
	Rugs/Bath Mat/ Floor covering made of Polypropylene Non-Woven Sheets and Braided Cotton Yarn
	1 kg
	1
	
	Relevant type of Polypropylene Non-Woven Sheets in rolls
	1.02 kg/kg content in the export product.

	H294
	Safety Helmet (made out of fibre glass reinforced plastics) weight 1425 gms +/- 20 gms.
	1 No.
	1
	
	Fibre Glass Mat
	0.525 Kgs.

	
	
	
	2
	
	Fibre Glass woven roving
	0.105 Kg.

	
	
	
	3
	
	Laminated cloth 6 mm thick
	0.185 Sq.mtr.

	
	
	
	4
	
	Laminated cloth 10 mm thick
	0.185 Sq. mtr.

	
	
	
	5
	
	Transfers (labels)
	Net to Net

	
	
	
	6
	
	Snap fasteners
	Net to Net.

	
	
	
	7
	
	Aluminium Flakes
	0.026 Kg.

	
	
	
	8
	
	Polycarbonate Sheet
	0.084 Kgs.

	
	
	
	9
	
	Cyanoacrylate Adhesive
	0.001 ltr.

	Note: 1. In case of variations in the weight of the export product, the quantities of import items 1 and 2 may be allowed in proportion to weight of export product. The quantity of other items will remain unchanged.

	H295
	SAN Resin (Styrene Acrylonitrile Resin)
	1 MT
	1
	
	Acrylonitrile
	296.91 Kgs.

	
	
	
	2
	
	Styrene
	784.59 Kgs.

	
	
	
	3
	
	Tart-Dodecyl Mercaptan
	0.79 Kg.

	
	
	
	4
	
	N.N'-Ethylene Bisstearamide
	0.16 Kg.

	H296
	Scalp Vein Set, one end having Wings cannulae like (Net weight 10 gms each)
	100 Nos.
	1
	
	PVC Compound Extrusion Grade
	1.05 kg/kg content in export product.

	
	
	
	2
	
	PVC Compound Injection Moulding Grade
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Cannulae SS 20G, 21G, 22G, 23G and 24G
	101 Nos./100 Nos. in the export product.

	H297
	Set Squares (made out of Cellulose Acetate)
	1.0 Kg
	1
	
	Cellulose Acetate in Granule form
	1.05 Kg.

	H298
	Single Blood Bag with Tubing
	100 Nos.
	1
	
	PVC Compound Granules (Medical Grade)
	1.10 kg/kg content in the export product.

	
	
	
	2
	
	Polycarbonate Granules
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Stainless Steel Capillary
	1.25 kg/kg content in the export product.

	
	
	
	4
	
	Adenine USP Grade
	0.0021 kg

	
	
	
	5
	
	Hot Melting Adhesive Label Medical Grade, Paper Tamper Evident Label Printed/ Unprinted
OR
Evident Paper in Sheets/Rolls
	1.05 kg/kg content in the export product. 

1.10 kg/kg content in the export product.

	H299
	Single component P.U. Coating
	1.0 Kg
	1
	
	Diphenylmethane-diisocyanate (MDI)
	0.350 Kg

	
	
	
	2
	
	Polyol (Polyurethane)
	0.205 Kg

	
	
	
	3
	
	Ethyl Glycol Acetate
	0.070 Kg

	
	
	
	4
	
	Butyl Benzol Phthalate
	0.050 Kg

	
	
	
	5
	
	Dimethyl Methyl Phosphonate
	0.055 Kg

	
	
	
	6
	
	Pyrogollol
	0.010 Kg

	H300
	Single Layer Printed PVC Sheeting (Thickness 0.06 mm to 0.6 mm)
	1 kg
	1
	
	PVC Resin
	0.603 kg

	
	
	
	2
	
	PVC Plasticizer
	0.371 kg

	
	
	
	3
	
	PVC Stabilizer
	0.025 kg

	
	
	
	4
	
	Processing Aid/Impact Modifier
	0.025 kg

	
	
	
	5
	
	Pigments
	0.025 kg

	
	
	
	6
	
	Solvent (Cyclo- hexanone/ MEK/MIBK)
	0.020 kg

	
	
	
	7
	
	Antistatic Agent/ Fungicide
	0.011 kg

	H301
	Single Side Decorative Laminates with barrier paper
	1 sq meter x 1 mm Thickness of wt. 1.45 Kg +/-2.5%
	1
	
	Kraft paper
	0.937 kg

	
	
	
	2
	
	Base Paper
	0.107 kg

	
	
	
	3
	
	Barrier Paper
	0.086 kg

	
	
	
	4
	
	Tissue Paper
	0.030 kg

	
	
	
	5
	
	Phenol
	0.361 kg

	
	
	
	6
	
	Malamine
	0.181 kg

	
	
	
	7
	
	Paraformaldehyde
(91 +/- 1% Purity)
OR
	0.300 kg

	
	
	
	7
	
	Methanol
	0.398 Kg

	
	
	
	8
	
	B.O.P.P. Film
	0.010 kg

	Note:1. The above norm has been worked out on the 1.00 mm thickness with average wt. of 1.45 Kg +/- 2.5%
2. In Case of variation in thickness/weight, the quantity of item of import viz. Phenol, Para Formaldehyde/Methanol and Kraft Paper to be allowed may be arrived by adopting the following formula:
AxB/ C
Where A=Qty. allowed for 1.00 mm thickness of wt. 1.45 Kg +/-2.5%. 
B= The thickness or wt/sq. meter of decorative laminates proposed to be exported. 
C=Either the Standard thickness of 1.00 mm or the Standard wt. of 1.45 Kg/sq. meter of 1.00 mm thickness.
3.The quantity of items viz. Base Paper, Barrier Paper, Tissue Paper, Melamine and BOPP Film will remain unchanged irrespective of thickness and weight of decorative laminate to be exported.
4. The above norms are applicable only in case of Decorative Laminates having thickness range between 0.5 mm and 20 mm thickness.

	H302
	Single Side Decorative Laminates without Barrier Paper
	1 sq mtr x 1 mm Thickness of wt. 1.45 Kg +/-2.5%
	1
	
	Kraft paper
	1.033 Kg

	
	
	
	2
	
	Base Paper
	0.133 kg

	
	
	
	3
	
	Tissue Paper
	0.033 kg

	
	
	
	4
	
	Phenol
	0.457 kg

	
	
	
	5
	
	Melamine
	0.133 kg

	
	
	
	6
	
	Paraformaldehyde (91+/-1% Purity) 
OR
	0.300 kg

	
	
	
	6
	
	Methanol
	0.398 Kg

	
	
	
	7
	
	B.O.P.P. Film
	0.011 kg

	
	
	
	8
	
	Titanium Dioxide
	0.0055 kg

	Note:1. The above norms has been worked out on the 1.00 mm thickness with average wt. of 1.45 Kg +/-2.5% 
2. In case of variation in thickness/weight,the quantity of item of import viz. Phenol, Paraformaldehyde,Kraft paper and Titanium Dioxide to be allowed may be arrived by adopting Formula:
AxB/C
Where
A= Qty. allowed for 1.00 mm thickness of wt. 1.45 Kg +/2.5%. 
B= The thickness or wt/sq. meter of decorative laminates proposed to be exported.
C=Either the Standard thickness of 1.00 mm or the Standard wt.of 1.45 Kg/sq. meter of 1.00 mm thickness.
3.The quantity of BOPP film given above will be for one sq. meter of Decorative Laminates irrespective of thickness and weight of decorative laminates to be exported.
4. The quantity of all the other items unchanged irrespective of change of thickness and weight of decorative laminates to be exported. 
5. it is clarified that the above formula is applicable only incase of Decorative Laminates having thickness range between 0.5 mm and 1.5 mm.

	H303
	Spectacle Case/ Pouch made of Nylon Cloth
	1 No.
	1
	
	Relevant Nylon Fabric
	1.02 Sq.cm/ Sq.cm. content of Nylon Fabric in export product.

	H304
	Spectacle Frames
	100 pcs
	1
	
	Spectacle Front of relevant Brand / make with or without metal fittings
	Net to Net

	
	
	
	2
	
	Spectacle Sides of relevant Brand/make with or without noted fittings
	Net to Net

	H305
	Spectacle Frames
	1.0 kg
	1
	
	Cellulose Acetate Sheet/Strip in sizes; 140 X 17 cms/ 140 X 18 cms 8mm or 3.5 mm thickness
	2.857 Kg.

	
	
	
	2
	
	Spectacle Hinges with or without screw
	Net to Net

	
	
	
	3
	
	Nickel Silver wire (without Hinges)
	Net to Net

	H306
	Spectacle Sports Head-Band with Buckle width 22 mm to 25 mm
	1 No.
	1
	
	Elastic Webbing with width 22 mm to 25 mm
	1.01 Meter/ Meter content in export.

	
	
	
	2
	
	Polyacetal Granules
	1.05 kg/kg content in the export product.

	H307
	Spherical Shaped Plastic Chart
	1 No.
	1
	
	ABS Resin/ Granules
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Polypropylene Granules
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Polyol
	0.525 kg/kg of rigid Polyurethene foam in the export product

	
	
	
	4
	
	Isocynate(MDI)
	0.525 kg/kg of rigid Polyurethene foam in the export product

	Note:1. Quantity of Item No.3 and 4 are allowed for 1 kg of Rigid Polyurethane Foam contained in the export product.

	H308
	Sports Shoes made out of PVC/PU Coated fabrics with PVC Soles and fitted with Nylon/ Polyester terry towel fabrics on the Socks
	One Pair
	1
	
	PU Leather/PVC Leather Cloth
	0.25 sq. mtr

	
	
	
	2
	
	Laminated foams
	0.145 sq. mtr

	
	
	
	3
	
	Foam
	15 gms

	
	
	
	4
	
	Threads
	25 mtr

	
	
	
	5
	
	Latex
	20 ML

	
	
	
	6
	
	PVC Printing Inks/Colours
	5 Gms

	
	
	
	7
	
	Solvents (MIBK/Ethylacetate/ Cyclohexane)
	5 Gms

	
	
	
	8
	
	Nylon Tapes
	0.5 Mtr

	
	
	
	9
	
	Embelishments :-
	

	
	
	
	
	a)
	Velcro /Elastics
	0.1 Mtr

	
	
	
	
	b)
	PVC Flocked/ printed Sheets
	0.01 sq. mtr

	
	
	
	
	c)
	Printed/ Embroidered label
	2 Pcs

	
	
	
	
	d)
	Plastic Fittings
	4 Pcs

	
	
	
	10
	
	Thermoplastic Sheets
	0.02 sq. mtr

	
	
	
	11
	
	Adhesives/ Bonding Agent/Coupling Agent
	30 Gms

	
	
	
	12
	
	PVC Resins
	460 Gms

	
	
	
	13
	
	Plasticizers
	253 Gms

	
	
	
	14
	
	Stabilizer (other than tin Stabilizers)
	14 Gms

	
	
	
	15
	
	Antimony Trioxides
	13 Gms

	
	
	
	16
	
	Pigments/ Titanium dioxide
	9.2 Gms

	
	
	
	17
	
	Lubricants
	5 Gms

	
	
	
	18
	
	Insole sheets
	0.04 sq. mtr

	
	
	
	19
	
	LLDPE/LDPE
	20 Gms

	
	
	
	20
	
	Mould Release Agents
	5 Gms

	
	
	
	21
	
	Nylon/Polyester skin fit/ Terry Towels
	0.075 sq. mtr

	
	
	
	22
	
	Latex
	10 ML

	
	
	
	23
	
	Solvent (MEK/Acetone MIBK/ Ethyl Trichloro Ethane
	5 gms

	
	
	
	24
	
	PP/HDPE
	20 gms

	
	
	
	25
	
	Card Boards (other than Ivory Board )
	100 gms

	
	
	
	26
	
	Stifner Boards (other than Ivory Board)
	20 gms

	
	
	
	27
	
	Kraft Paper
	50 gms

	
	
	
	28
	
	Adhesive Tapes
	10 cm

	
	
	
	29
	
	Miscellaneous items:
	

	
	
	
	
	
	a)Moulds + Lasts

b)Clinking Dies/ Printing Screens
	6 Pairs for one lakh Pairs
10 Pairs for one lakh Pairs

	H309
	Sterilized Disposable Syringes with or without Needles (1 ml, 2ml/3 ml, 5 ml, 10 ml, 20 ml)
	1 kg
	1
	
	HDPE granules (Medical Grade/ Moulding Grade)
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Polypropylene Granules (Medical Grade/ Moulding Grade)
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Hypodermic Needles (Relevant)
	102 Nos./100 Nos.

	H310
	Sterilized Disposable/ Auto-Disable Syringes with or without Needles (1 ml, 2ml/3ml, 5ml, 10ml, 20 ml)
	1kg
	1
	
	Relevant Plastic Barrel
	103 Nos./100 Nos.

	
	
	
	2
	
	Relevant Plastic Plungers
	103 Nos./100 Nos.

	
	
	
	3
	
	Gaskets
	103 Nos./100 Nos.

	
	
	
	4
	
	Hypodermic Needles (relevant)
	102 Nos./100 Nos.

	H311
	LLDPE Stretch Wrap Film
	1 kg
	1
	
	LLDPE Granules
	0.9975 kg.

	
	
	
	2
	
	Poly Isobutylene
	0.0525 kg

	H312
	Strong Acid Cation Exchange Resin
	1 kg
	1
	
	Styrene
	0.331 kg

	
	
	
	2
	
	Divinyl Benzene
	0.0526 kg

	
	
	
	3
	
	Ethylene Dichloride
	0.105 kg

	
	
	
	4
	
	Polyvinyl Alcohol
	0.0016 kg

	H313
	Strong Acid Cation Exchange Resin
	1 cu.ft. (28.3 litre)
	1
	
	Styrene
	7.669 kg

	
	
	
	2
	
	Divinyl Benzene
	1.217 kg

	
	
	
	3
	
	Ethylene Dichloride
	2.439 kg

	
	
	
	4
	
	Polyvinyl Alcohol
	0.0368 kg

	H314
	Suction Catheter with Moulded Tip having two back eye at one end and other end HDPE Connector (net weight 20 gms each)
	1 kg
	1
	
	Poly Vinyl Chloride, Non-Toxic Medical Grade, Soft PVC Compound
	1.05 kg/kg content in export product.

	
	
	
	2
	
	HDPE Moulded Grade having 18 M.F.I.
	1.05 kg/kg content in export product.

	H315
	Sun Control Polyester Film Non-Reflective Single Ply with Liner
	10,000 sq.ft. (69.44 kgs)
	1
	
	Polyester Film 
OR
	102 kgs.

	
	
	
	1
	
	a) D.M.T. 
b) M.E.G.
	106.99 kgs 
40.75 kgs

	
	
	
	2
	
	Relevant Solvent
	12.36 kg

	
	
	
	3
	
	M.E.G.
	16.48 kg

	
	
	
	4
	
	Disperse Dyes Blue
	0.907 kg

	
	
	
	5
	
	Disperse Dyes Red
	0.2447 kg

	
	
	
	6
	
	Disperse Dyes Yellow
	0.086 kg

	
	
	
	7
	
	U.V.Stabilizer
	1.648 kg

	
	
	
	8
	
	Acrylic Resin Solution
	18.753 kg

	
	
	
	9
	
	Silicon Polymer Solution
	0.907 kg

	
	
	
	10
	
	Cross Linking Agent
	0.0363 kg

	
	
	
	11
	
	Relevant Catalyst
	0.0182 kg

	
	
	
	
	
	
	

	H316
	Sun Control Polyester Film Non-Reflective Two Ply with Liner
	10,000 sq.ft. (100 kgs)
	1
	
	D.M.T.
	164.74 kg

	
	
	
	2
	
	M.E.G.
	62.746 kg

	
	
	
	3
	
	Relevant Solvent
	25.536 kg

	
	
	
	4
	
	M.E.G.
	34.04 kg

	
	
	
	5
	
	Disperse Dyes Blue
	1.864 kg

	
	
	
	6
	
	Disperse Dyes Red
	0.512 kg

	
	
	
	7
	
	Disperse Dyes Yellow
	0.170 kg

	
	
	
	8
	
	U.V.Stabilizer
	1.699 kg

	
	
	
	9
	
	Acrylic Resin Solution
	19.722 kg

	
	
	
	10
	
	Silicone Polymer Solution
	0.952 kg

	
	
	
	11
	
	Cross Linking Agent
	0.039 kg

	
	
	
	12
	
	Relevant Catalyst
	0.329 kg

	
	
	
	13
	
	Adhesive
	8.083 kg

	H317
	Sun Control Polyester Film Reflective Two Ply with Liner
	10,000 sq.ft. (102 kg)
	1
	
	Polyester Film 
OR
	148.99 kgs

	
	
	
	1
	
	a) D.M.T.
b) M.E.G.
	156.15 Kgs
59.49 kgs

	
	
	
	2
	
	Relevant Solvent
	12.577 kg

	
	
	
	3
	
	M.E.G.
	16.789 kg

	
	
	
	4
	
	Disperse Dye Blue
	0.926 kg

	
	
	
	5
	
	Disperse Dye Red
	0.254 kg

	
	
	
	6
	
	Disperse Dye Yellow
	0.081 kg

	
	
	
	7
	
	U.V.Stabilizer
	1.671 kg

	
	
	
	8
	
	Acrylic Resin Solution
	19.544 kg

	
	
	
	9
	
	Silicone Polymer Solution
	0.944 kg

	
	
	
	10
	
	Cross Linking Agent
	0.036 kg

	
	
	
	11
	
	Relevant Catalyst
	0.326 kg

	
	
	
	12
	
	Adhesive
	8.00 kg

	
	
	
	13
	
	Evaporation boat
	1 pc

	
	
	
	14
	
	Aluminium wire
	0.678 kg

	
	
	
	15
	
	Silicon Oil
	0.235 kg

	H318
	Sun Control Polyester Film reflective two ply with liner and Scratch Resistance coating
	10,000 Sq.Ft (104.77 kgs)
	1
	
	D.M.T.
	156.145 kgs

	
	
	
	2
	
	M.E.G.
	59.489 kgs

	
	
	
	3
	
	Relevant Solvent
	12.577 kgs

	
	
	
	4
	
	M.E.G.
	16.789 kgs

	
	
	
	5
	
	Disperse Dye Blue
	0.926 kg

	
	
	
	6
	
	Disperse Dye Red
	0.254 kg

	
	
	
	7
	
	Disperse Dye Yellow
	0.081 kg

	
	
	
	8
	
	U.V. Stabilizer
	1.671 kgs

	
	
	
	9
	
	Acrylic Resin Solution
	19.544 kgs

	
	
	
	10
	
	Silicone Polymer Solution
	0.944 kg

	
	
	
	11
	
	Cross Linking Agent
	0.036 kg

	
	
	
	12
	
	Relevant Catalyst
	0.326 kg

	
	
	
	13
	
	Adhesive
	8.00 kgs

	
	
	
	14
	
	Evaporation Boat
	1 Pc.

	
	
	
	15
	
	Aluminium Wire
	0.678 kg

	
	
	
	16
	
	Silicone Oil
	0.235 kg

	
	
	
	17
	
	Scratch Resistant Chemical - ZM1819(Blend of functional Acrylates) (Solid content 80-85%)
	3.70 kgs

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	H319
	Synthatic Ketonic Resin Cyclohexanone Based (Acid Number 0.5 mg KOH/gm Water 0.5% Hydroxyl No. 167)
	1 kg
	1
	
	Cyclohexanone
	0.85 kg

	
	
	
	2
	
	Formaldehyde (37%)
OR
Paraformaldehyde(98%-100%)
	1.40 kg

0.52 kg

	H320
	Synthetic Acrylic Resin Emulsion (having solid content 55 +/- 1%)
	1 kg
	1
	
	Butyl Acrylate
	0.537 kg

	
	
	
	2
	
	Methacrylic Acid
	0.0108 kg

	
	
	
	3
	
	Potassium Persulphate
	0.0025 kg

	H321
	Synthetic Acrylic Resin Emulsion (Solid content minimum 28%)
	1 Kg
	1
	
	Acrylamide
	0.0209 Kg.

	
	
	
	2
	
	Butyl Acrylate
	0.1730 Kg.

	
	
	
	3
	
	Styrene
	0.1046 Kg.

	H322
	Synthetic Footwear made of NBR-PVC or SBR
	1 Pair
	1
	
	Adhesive
	0.03 kg

	
	
	
	2
	
	Stamping Foil
	6 sq inch

	
	
	
	3
	
	Thermo Plastic Sheet
	0.023 sq mtr

	
	
	
	4
	
	PVC Leather Cloth/ Velvets/ Printed PVC/ Jayguards
	2 sq. ft

	
	
	
	5
	
	Relevant Nitrile Rubber/PVC or SBR
	0.1 kg

	
	
	
	6
	
	Canvas
	2 sq ft

	
	
	
	7
	
	Artificial Leather/P.U. Leather cloth
	1.75 sq ft

	
	
	
	8
	
	Thermoplastic Cement
	0.011 kg

	
	
	
	9
	
	Sheet for insole
	0.05 sq mtr

	
	
	
	10
	
	PVC Resin/ Granules
	0.32 kg

	
	
	
	11
	
	Sewing Thread
	25 mtr

	
	
	
	12
	
	Reinforcement Tape
	0.5 mtr

	
	
	
	13
	
	Nails/ Tacks
	0.015 kg

	
	
	
	14
	
	HDPE/PP/LDPE
	0.06 kg

	H323
	Synthetic Ketonic Resin
	1 Kg.
	1
	
	Cyclohexanone
	0.909 Kg

	H324
	Synthetic Uppers for Footwears
	1 Pair
	1
	
	PVC Leather cloth/Printed PVC jaquard
OR
	2 sq ft

	
	
	
	1
	
	Artificial leather PU Leather cloth
	1.75 sq ft

	
	
	
	2
	
	Adhesives
	10 gms

	
	
	
	3
	
	Stamping Foil
	6 sq inch

	
	
	
	4
	
	Sewing thread
	25 mtr

	
	
	
	5
	
	Thermoplastic Sheet
	0.014 sq. Mtr

	
	
	
	6
	
	Canvas
	2 sq. ft.

	
	
	
	7
	
	Reinforcement Tape
	0.50 mtr

	
	
	
	8
	
	HDPE/ LDPE/ PP Granules
	1.05 kg/kg content in export

	
	
	
	9
	
	Self Adhesive Tape
	10 gms

	
	
	
	10
	
	Kraft paper/ Card Board (other than Ivory Board)/ Tissue paper
	1.05 kg/kg content in export

	H325
	Deleted
	
	
	
	
	

	H326
	Deleted
	
	
	
	
	

	H327
	Deleted
	
	
	
	
	

	H328
	Three Layered Printed PVC Floor Covering (Thickness 0.5 mm to 2.0 mm)
	1 kg
	1
	
	PVC Resin
	627 gms

	
	
	
	2
	
	Phthalate Plasticizer(DOP)
	334 gms

	
	
	
	3
	
	Adipate Plasticizer(DOA)
	34 gms

	
	
	
	4
	
	Epoxy Plasticizer
	30 gms

	
	
	
	5
	
	Titanium Dioxide/ Pigments
	30 gms

	
	
	
	6
	
	Solvent(Cyclo- hexanone/ MEK/MIBK)
	20 gms

	
	
	
	7
	
	Antistatic Agent (Titanate Coupling Agent/Fungicide)
	7 gms

	
	
	
	8
	
	Processing Aid/ Modifier
	14 gms

	
	
	
	9
	
	PVC Stabilizer
	20 gms

	H329
	Timers (Time Switches)
	1 kg.
	1
	
	Nylon 66
	1.05 kg/kg content in export product.

	
	
	
	2
	
	Polycarbonate resin
	1.05 kg/kg content in export product.

	
	
	
	3
	
	Polyester resin
	1.05 kg/kg content in export product.

	
	
	
	4
	
	Delrin(Chemical name to be specified)
	1.05 kg/kg content in export product.

	H330
	Shifted under Engineering Product Group
	
	
	
	
	

	H331
	Tooth Brushes
	1 kg
	1
	a)
	Relevant Polymer for Tooth Brush Handle 
OR
	1.05 kg/kg content in the export product

	
	
	
	1
	b)
	Relevant Tooth Brush Handles
	Net + 2% wastage

	
	
	
	2
	
	Relevant nylon 6/66/612/610 Monofilament
	1.05 kg/kg content in the export product

	
	
	
	3
	
	Relevant Aluminium/ Nickel/ Nickel-Silver Wire/Brasswire
	1.1 kg/kg content in the export product

	H332
	Tracing Film (Polyester Based) thickness - 50/75/100 Microns
	1000 sq.mtrs.
	1
	
	Relevant Polyester Film Thickness - 50/75/100 Microns
	1150 sq.mtrs.

	
	
	
	2
	
	Silica Pigment
	2.30 kgs

	
	
	
	3
	
	Cellulostic Resin - Film Former
	1.15 kgs

	
	
	
	4
	
	Acrylic Resin Binder
	3.45 kgs

	
	
	
	5
	
	Solvents(MIBK/MEK)
	57.50 kgs.

	H333
	Twine/Rope made of HDPE/PP 
OR
Twine/Rope made of a blend of HDPE & PP in varying proportions
	1 kg
	1
	
	Relevant HDPE/ PP Granules/ Chips
	1.07 kg/kg content in the export product.

	Note : 1. The relevant HDPE & PP Granules may be allowed as 1.07 kg/kg content in the export product both for exclusive HDPE/PP Twine/Ropes and for Twine/Rope made of blend of HDPE & PP on the actual net content of the relevant polymer I.e. HDPE of PP inthe blended Twine/Ropes to be exported.2. In case of export of coloured Twine/Ropes, the relevant colour Master Batch shall also be allowed as an additional input @ 0.02 kg/kg weight of relevant polymer and accordingly the quantity of relevant polymer i.e. HDPE/PP shall bereduced to 1.05 kg/kg content in the export product.

	H334
	UHMPDE Sheets/ Liner (Size 2.0mtrX1.0mtr thickness 10mm to 15mm)
	1 kg
	1
	
	UHMWPE Powder
	1.09 kg

	
	
	
	2
	
	Colour Pigments (for coloured product)
	0.003 kg

	H335
	Unreinforced Polycarbonate Compound in Granules (General purpose clear grade)
	1 kg
	1
	
	Polycarbonate Powder
	1.02 kg

	
	
	
	2
	
	Organic Phosphites 
OR
Benzotriazoles
	0.0040 kg

0.0040 kg

	
	
	
	3
	
	Anthraquinone Dyes 
OR
Quinacridone Dyes (for coloured product)
	0.00026 kg

0.00026 kg.

	H336
	Uro Bag with Non-Return Valve and Bottom Drainage (Net weight 83 gms each)
	1 kg
	1
	
	PVC Compound Blow Moulding Grade
	1.05 kg/kg content in export product.

	
	
	
	2
	
	PVC Compound Extrusion Grade
	1.05 kg/kg content in export product.

	
	
	
	3
	
	HDPE Granules
	1.05 kg/kg content in export product.

	
	
	
	4
	
	Nylon Moulding Grade
	1.05 kg/kg content in export product.

	H337
	Vaccine Carrier with Ice Packs
	1 No.
	1
	
	HDPE Granules
	1.03 kg/kg content in export.

	
	
	
	2
	
	HIPS Granules
	1.03 kg/kg content in export.

	
	
	
	3
	
	Polyol
	0.515 kg/kg weight of Polyurethene foam in export

	
	
	
	4
	
	Isocyanate (MDI)
	0.515 kg/kg weight of Polyurethene foam in export

	H338
	Vaccine Cold Box with Ice Packs, Long Range
	1 No.
	1
	
	LLDPE Granules
	1.03 kg/kg content in export.

	
	
	
	2
	
	HDPE Granules
	1.03 kg/kg content in export.

	
	
	
	3
	
	LDPE Granules
	1.03 kg/kg content in export.

	
	
	
	4
	
	P.P. Granules
	1.03 kg/kg content in export.

	
	
	
	5
	
	Polyol
	0.515 kg/kg weight of Polyurethene foam in export

	
	
	
	6
	
	Isocyanate (MDI)
	0.515 kg/kg weight of Polyurethene foam in export

	H339
	Vinyl (PVC) floor Covering with jute Backing
	1 sq meter of PVC Sheeting layer having weight of 1320 gms
	1
	
	PVC Suspension grade
	827 gms

	
	
	
	2
	
	PVC (Paste grade )
	53 gms

	
	
	
	3
	
	Plasticizer DOP/Mesamoll
	440 gms

	
	
	
	4
	
	Plasticizer DOA
	44 gms

	
	
	
	5
	
	Epoxy Plasticizer
	26 gms

	
	
	
	6
	
	PVC Stabilizers including UV Stabilizer
	26 gms

	
	
	
	7
	
	Processing aid/ Modifier
	18 gms

	
	
	
	8
	
	Pigments/TiO2
	26 gms

	
	
	
	9
	
	Solvent (Cyclohexanone/ MEK/ MIBK/ Toluene)
	20 gms

	
	
	
	10
	
	Titannate coupling agent Fungicide/ Antistatic agent
	9 gms

	
	
	
	11
	
	PU adhesives
	

	
	
	
	
	a)
	PU resin
	2 gms

	
	
	
	
	b)
	DMF
	6 gms

	H340
	Vinyl Asbestos Tile
	1 kg
	1
	
	PVC Resin
	0.2903 kg

	
	
	
	2
	
	Plasticizer
	0.0950 kg

	
	
	
	3
	
	Stabilizer
	0.0493 kg

	
	
	
	4
	
	Asbestos
	0.1567 kg

	
	
	
	5
	
	Calcium Carbonate
	0.5616 kg

	
	
	
	6
	
	Easter Gum
OR
	

	
	
	
	6
	
	PE Derivative
	0.0373 kg

	
	
	
	7
	
	Pigment
	0.029 kg

	H341
	Vinyl Flooring
	1 kg
	1
	
	PVC Resin
	0.5294 kg

	
	
	
	2
	
	Plasticizer
	0.1889 kg

	
	
	
	3
	
	Calcium Carbonate
	0.3348 kg

	
	
	
	4
	
	Pigment
	0.0126 kg

	
	
	
	5
	
	Stabilizer
	0.0127 kg

	H342
	Water Based Sketch Pens
	100 pcs
	1
	a)
	Writing Inks
	336 gm

	
	
	
	
	b)
	water soluble dyestuff
	33.6 gm

	
	
	
	2
	
	Synthetic filters
	Net + 2% wastage

	
	
	
	3
	
	Printing Ink
	1.05 gm

	H343
	Weak Acid Cation Exchange Resin
	1 Litre (385 gms Dryweight basis)
	1
	
	Methyl Acrylate
	0.377 Kg.

	
	
	
	2
	
	Divinyl Benzene
	0.058 Kg.

	
	
	
	3
	
	Methacrylic Acid
	0.177 Kg.

	H344
	Weak Acid Cation Exchange Resins(average bulk density 730-790 gms. per litre)
	1 kg
	1
	
	Ethyl Acrylate
	0.448 kg

	
	
	
	2
	
	Metha Acrylic Acid Monomer
	0.21 kg

	
	
	
	3
	
	Divinyl Benzene Monomer
	0.07 kg

	H345
	Weatherable Dyed Polyester Film
	100 Kg
	1
	
	D.M.T.
	154.35 kg

	
	
	
	2
	
	M.E.G.
	58.80 kg

	
	
	
	3
	
	Solvent
	33.60 kg

	
	
	
	4
	
	M.E.G.
	44.80 kg

	
	
	
	5
	
	Disperse Dye Blue
	2.464 kg

	
	
	
	6
	
	Disperse Dye Red
	0.672 kg

	
	
	
	7
	
	Disperse Dye Yellow
	0.224 kg

	
	
	
	8
	
	U.V.Stabilizer
	4.116 kg

	H346
	Deleted
	
	
	
	
	

	H347
	White Master Batches containing 40% Polymer and 60% Titanium dioxide
	1 kg.
	1
	
	Relevant Polymer in export product
	0.408 Kg

	
	
	
	2
	
	Titanium Dioxide
	0.612 Kg

	
	
	
	
	
	
	

	H348
	White Opaque LLDPE Lamination Grade Film
	1 kg
	1
	
	LLDPE Granules (Film Grade) 
OR
	1.05 kg

	
	
	
	2
	
	LLDPE Granules (Film Grade)
	0.966 kgs

	
	
	
	3
	
	White Master Batch
	0.084 kgs

	H349
	Tape/Yarn (Plain/ Twisted) made of HDPE/PP or Tape/Yarn (Plain/Twisted) made of blend of HDPE & PP in varying proportions
	1 kg
	1
	
	Relevant HDPE/ PP Granules/ Chips
	1.05 kg/kg content in the export product.

	Note: 1. The relevant HDPE & PP Granules/Chips may be allowed as 1.05 kg/kg content in the export product both for the exclusive HDPE/PP and Tape/Yarn made of blended HDPE & PP on the actual net content of that relevant polymer i.e. HDPE or PP in theblended Tape / Yarn to be exported.Note : 2. In case of export of coloured Tape / Yarn, the relevant Colour master Batch shall also be allowed as an additional input @ 0.02 kg/kg weight of relevant polymer and accordingly the relevant polymer i.e. HDPE/PP shall be reduced to1.03 kg/kg content in the export product.

	H350
	Nylon 612 Monofilament Yarn (Dia 0.15 mm to 0.30 mm) in cut hanks upto maximum length of 48" for toothbrush bristles
	1 kg
	1
	
	Nylon 612 Resin (Extrusion Grade)
	1.13 kg/kg of Nylon Monofilament Yarn in export product.

	
	
	
	2
	
	Nylon Colour concentrate/ master batch
	0.02 kg

	
	
	
	3
	
	Paper Wrapper
	0.05 kg

	
	
	
	4
	
	Glue - Dextrine
	0.005 kg

	
	
	
	5
	
	Spin Finish Silicon Emulsion
	0.0008 kg

	
	
	
	6
	
	Spin Finish Organic Surface Active Agent
	0.0006 kg

	
	
	
	7
	
	Spin Finish Antifoam A compound
	0.0005 kg

	Note: 1. The Nylon colour concentrate/ master batch will be allowed for coloured Nylon Monofilament Yarn only. In case of uncoloured Monofilament Yarn, the Nylon 612 Resin will be allowed as 1.15 kg instead of 1.13 kg against item No.1 ofthe inputs.

	H351
	Industrial Endless Synthetic Forming Fabric of Single Layer made out of Polyester and Nylon
	1 kg
	1
	
	Polyster Monofilament Yarn of relevant denier
	0.84 Kg

	
	
	
	2
	
	Nylon filament yarn of relevant denier
	0.36 kg

	H352
	Industrial Endless Synthetic Forming Fabric of Multiple Layer made out of Polyester and Nylon
	1 kg
	1
	
	Polyester Monofilament Yarn of relevant denier
	1.0 kg

	
	
	
	2
	
	Nylon Monofilament Yarn of relevant denier
	0.20 kg

	H353
	Dipped Nylon Braided Cord
	1 kg
	1
	
	Nylon Filament Yarn (Tyre Yarn)
	1.02 kg/kg content in the export product.

	
	
	
	2
	
	Resorcinol
	0.001 kg

	
	
	
	3
	
	V P Latex
	0.04 kg

	H354
	Nylon Cord/Twine
	1 kg
	1
	
	Nylon Yarn of relevant grade/denier
	1.02 kg

	H355
	Polypropylene Staple Fibre
	1 kg
	1
	
	Polypropylene Resins/Granules
	1.05 kg

	
	
	
	2
	
	Master Batches
	0.04 kg

	
	
	
	3
	
	Spin Finish Oil
	0.009 kg

	
	
	
	4
	
	U.V. Stabilizers
	0.006 kg

	
	
	
	5
	
	Anti Static Oil
	0.006 kg

	H356
	Articles made of LLDPE
	1 kg
	1
	
	LLDPE Granules
	1.05 kg/kg content in export.

	H357
	Nail Polish Brush
	1 kg
	1
	
	Nylon Monofilament Yarn of relevant grade/denier
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	LDPE Granules
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Stainless Steel Wire of relevant gauge
	1.01 kg/kg content in the export product.

	H358
	Thermo Plastic Rubber Sole
	1 kg
	1
	
	TPR Granules or Styrene Butadiene Styrene Oil bound Copolymer or SBS Oil Bound Copolymer
	1.015 kg/kg content in export.

	H359
	Expanded Polyethylene Wads (Poly Gasket)
	1 kg
	1
	
	LDPE Granules
	1.05 kg

	
	
	
	2
	
	Zinc Stearate
	0.03 kg

	
	
	
	3
	
	Blowing Agent (Hydrocerol B1H)
	0.01 kg

	H360
	Unreinforced Polycarbonate Compound in Granules (Flame Retardant Grade)
	1 kg
	1
	
	Polycarbonate Powder
	0.984 kg

	
	
	
	2
	
	Titanium Dioxide (Rutile Grade)
	0.020 kg

	
	
	
	3
	
	Organic Phosphite
	0.005 kg

	
	
	
	4
	
	Poly Tetrafluoro Ethylene(PTFE)
	0.0150 kg

	H361
	Shifted under Engineering Product Group
	
	
	
	
	

	
	
	
	
	
	
	

	H362
	Modified LLDPE Compound containing 90+/-1% LLDPE Resin (Plastic Processing Aid)
	1 kg
	1
	
	LLDPE Granules
	0.936 kg

	
	
	
	2
	
	Siliquent PA-1 Organo-Silicone (Silicone Fluid)
	0.0518 kg

	H363
	Laminated Polyethylene Tarpaulins containing 65+/-3% Fabric & 35+/-3% Laminating Resin (Minimum Width X Length = 9 feet X 9 feet)
	1 kg
	1
	
	Polyethylene Unlaminated Fabric 90-100 GSM (width not exceeding 2.1 meter)
	0.715 kg

	
	
	
	2
	
	LDPE Granules (Lamination Grade)
	0.350 kg

	
	
	
	3
	
	LDPE Colour Master Batch
	0.0175 kg

	
	
	
	4
	
	U.V. Stabilizer
	0.0175 kg

	
	
	
	5
	
	Aluminium Eyelets (Gromets)
	Net + 1% wastage.

	H364
	Articles made of Acrylic Resin Moulding Powder/Granules
	1 kg
	1
	
	Acrylic Resin Moulding Powder/Granules
	1.05 kg/kg content in export.

	H365
	Printed Polyethylene Film (5 Layer Co-extruded Multilayer Film) consisting of 80% LLDPE and 20% Nylon-6 (by weight)
	1 kg
	1
	
	LLDPE Granules (Film Grade)
	0.525 kg

	
	
	
	2
	
	Modified LLDPE Resin (Film Grade)
	0.315 kg

	
	
	
	3
	
	Nylon-6 Granules (Film Grade)
	0.210 kg

	H366
	Vinyl Copolymer Formulation (White Powder)
	1 kg
	1
	
	Poly Vinyl Alcohol Powder
	1.01 kg/kg content in export product.

	H367
	Nylon 6/ Nylon-66 Monofilament Yarn wound on Disposable Bobbins
	1 kg
	1
	
	Relevant Nylon-6/Nylon-66 Chips
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Antioxidant
	0.002 kg

	
	
	
	3
	
	Finish Oil
	0.001 kg

	
	
	
	4
	
	Surface Active Agent
	0.001 kg

	
	
	
	5
	
	Polypropylene Granules for Bobbins
	1.05 kg/kg content in the export product

	Note: 1. Only the relevant grade of Nylon Chips as contained in the export product shall be allowed.Note: 2. When export is not on Bobbin, Polypropylene Granules shall not be allowed for import

	H368
	HDPE Knitted Coloured Fabrics
	1 kg
	1
	
	HDPE Granules
	1.07 kg

	
	
	
	2
	
	Relevant Colour HDPE Master Batch
	0.01 kg

	H369
	Plastic Insulated Thermo Wares, Casseroles, Ice Packs, Food Server, Lunch Packs, Water Jugs, Water Bottles, Hot and Cold Insulated Flasks, Cups, Mugs, Gifts of all Sizes
	1 kg
	1
	
	Relevant Polymers (polypropylene, HDPE, LDPE, LLDPE Polycarbonate, ABS, Polystyrene)
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Relevant Colour Master Batch
	0.02 kg/kg content within the over all polymer content in the export product

	
	
	
	3
	
	( i ) Polyol
	0.525 kg/kg content in the export product.

	
	
	
	
	
	( ii ) Isocyanate
	0.525 kg/kg content in the export product.

	
	
	
	4
	
	Relevant Stainless Steel Sheet/Coils
	1.05 kg/kg content in the export product.

	
	
	
	5
	
	Relevant Nylon/ Polypropylene Belt
	1.03 kg/kg content in the export product.

	
	
	
	6
	
	Relevant Metalic Parts
	Net + 1% wastage.

	
	
	
	7
	
	Relevant Glass container
	Net to Net

	Note: Import items at S. No. 3 ( i ) & ( ii ) pertains to Polyurethane Foam for insulation. Quantities are for 1 kg content of Polyurethane foam in the export product.

	H370
	ADCM (CR-39) Spectacle Lenses (Both Sides Finished)
	100 Nos.
	1
	
	ADCM (CR-39) Spectacle Lenses (Front Side Finished)
	105 Nos.

	
	
	
	2
	
	Consumables i.e. Smoothing Pad, Polishing Pad, CR-39 Polish, Blocking Tape, Diamond Tool
	Upto 4% of FOB value of export.

	H371
	Thermoplastic Polyurethane DESMOPAN 385
	1000 kgs
	1
	
	Polyester Polyols
	686 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	285 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	72 kgs

	
	
	
	4
	
	ANOX 20 AM (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	4 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
OR
	4 kgs

	
	
	
	1
	
	Adipic Acid
	494 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	285 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	408 kgs

	
	
	
	4
	
	ANOX M-20 (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	4 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
	4 kgs

	H372
	Thermoplastic Polyurethane DESMOPAN KU2 8068
	1000 kgs
	1
	
	Polyester Polyols
	784 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	261 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	41 kgs

	
	
	
	4
	
	ANOX 20 AM (Phenolic Antioxidants)
	5 kgs

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	3 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
	12 kgs

	
	
	
	7
	
	VANOX-12/P.P. Diphenyl Amine
	5 kgs

	H373
	Thermoplastic Polyurethane DESMOPAN 192
	1000 kgs
	1
	
	Polyester Polyols
	606 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	338 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	97 kgs

	
	
	
	4
	
	ANOX 20 AM (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	4 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
OR
	6 kgs

	
	
	
	1
	
	Adipic Acid
	436 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	338 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	394 kgs

	
	
	
	4
	
	ANOX M-20 (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	4 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
	6 kgs

	H374
	Thermoplastic Polyurethane DESMOPAN 359
	1000 kgs
	1
	
	Polyester Polyols
	444 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	472 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	151 kgs

	
	
	
	4
	
	ANOX 20 AM (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	2 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
OR
	3 kgs

	
	
	
	1
	
	Adipic Acid
	320 kgs

	
	
	
	2
	
	MDI/Desmodor Trial product fused (PU 0118 Fused)
	472 kgs

	
	
	
	3
	
	Butane Diol 1,4 1,4 BDO
	369 kgs

	
	
	
	4
	
	ANOX M-20 (Phenolic Antioxidants)
	1 kg

	
	
	
	5
	
	STABAXOL - 1 (Carbodimide)
	2 kgs

	
	
	
	6
	
	LOXAMID EBS (N,N-Ethylene-Bis-Steramide)
	3 kgs

	H375
	Modified PPO(PPE) Compounds
	1 kg
	1
	
	PPO Resin
	0.530 kg

	
	
	
	2
	
	High Impact Polystyrene
	0.347 kg

	
	
	
	3
	
	Resorcinol
	0.127 kg

	Note: 1. The export product is unreinforced flame retardant grade. 2. The above export product contains 50%+/-1% PPO and 33%+/-1% High Impact Polystyrene. Any variation in the ratio, the quantity may be worked out on pro-rata basis.

	H376
	PC/ABS Alloy
	1 kg
	1
	
	Polycarbonate Powder
	0.771 kg

	
	
	
	2
	
	SAN Powder
	0.157 kg

	
	
	
	3
	
	ABS Powder
	0.115 kg

	Note: 1) The export product is unreinforced grade. 2) The above export product contains 73%+/-1% PC and 14.5%+/-1% SAN and 12.5%+/-1% ABS. Any variation in the ratio, the quantity may be worked out on pro-rata basis.

	H377
	Nylon 6/66 Compounded Chips
	1 kg
	1
	
	Relevant Nylon 6/66 Chips
	1.03 kg/kg content in the export product.

	H378
	Silicone Compound "C"
	1 kg
	1
	
	Low Molecular Weight Silanol Octamethylcyclo-tetrasiloxane Siloxane C-45 Octamethylcyclic Hydrolisate
	0.364 kg

	H379
	Polyester Buttons
	1 kg
	1
	
	Polyester Resin
	1.05 kgs

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	H380
	Laminated Polyethylene Tarpaulins containing 65%+/-3% Fabric and 35%+/-3% Laminating Resins (Minimum width X Length 9 Feet X 9 Feet)
	1 kg
	1
	
	Polyethylene Unlaminated Fabric 50-130 GSM width not exceeding 2.1 Meter
	0.715 kg

	
	
	
	2
	
	LDPE Granules (Lamination Grade)
	0.350 kg

	
	
	
	3
	
	LDPE Colour Master Batch
	0.0175 kg

	
	
	
	4
	
	UV Stabilisers
	0.0175 kg

	
	
	
	5
	
	Aluminium Eyelets (Gromets)
	Net+1% wastage.

	Note: 1) The above norms are for laminated polyethylene tarpaulin having 65% of unlaminated fabric and 35% weight of laminating resin (Quantity allowed together at Sl.Nos. 2,3&4). 2) For variations in weight of unlaminated fabrics, the quantity of Sl.No.1 and for Laminating Resin, the quantity of input at Sl.Nos. 2 to 4 may be worked out on pro-rata basis.

	H381
	Tensioner Combination (made out of Polycarbonate)
	1 kg
	1
	
	Polycarbonate Granules
	1.05 kg/kg content in the export product.

	H382
	Fibreglass Tissue with UF/PF Resin content Min. 17%
	1 MT
	1
	
	Chopped Strand of Fibreglass (Moisture content Minimum 13.5%)
	1.225 MT/MT content in the export product.

	
	
	
	2
	
	Fibreglass Yarn
	1.09 MT/MT content in the export product.

	
	
	
	3
	
	Natrosol (Hydroxy Ethyl Cellulose)
	11.60 kgs

	
	
	
	4
	
	Myacide (2-Bromo-2-Nitropropane 1-3 Diol)
	1.61 kgs

	
	
	
	5
	
	Aerosol
	0.30 kgs

	
	
	
	6
	
	Formaline (37%)
	385.00 kgs

	
	
	
	7
	
	Hemopur (Solution of Stabilised Chlorine Dioxide)
	4.97 kgs

	H383
	Multi Layer Co-Extruded plastic packaging material (Printed/ Unprinted)
	1 Kg
	1
	
	LDPE Granules (Film Grade)
	1.05 kg/kg content in the export product

	
	
	
	2
	
	LLDPE Granules (Film Grade)
	1.05 kg/kg content in the export product

	
	
	
	3
	
	Ethylene Acrylic Acid Co-polymer Granules
	1.05 kg/kg content in the export product

	
	
	
	4
	
	Liquid Printing Ink
	0.01 kg

	Note: 1. In case of export of coloured items, Relevant "Colour Master Batch" shall also be allowed as an additional input at 0.02 kg/kg and the weight of Polymers at Sr. No. 1,2 and 3 above may be reduced to 1.03 kg/kg contained in the export product.
Note: 2. The Liquid Printing Ink may be allowed in case of printed export product.

	H384
	Gents Insole
	1 No.
	1
	
	Cellulose Insole Sheet
	0.05 Sq.Mtr.

	
	
	
	2
	
	Shank Board
	0.029 Sq.Mtr.

	H385
	Ladies Insole
	1 No.
	1
	
	Cellulose Insole Sheet
	0.04 Sq.Mtr.

	
	
	
	2
	
	Shank Board
	0.023 Sq.Mtr.

	H386
	Children Insole
	1 No.
	1
	
	Cellulose Insole Sheet
	0.03 Sq.Mtr.

	
	
	
	2
	
	Shank Board
	0.017 Sq.Mtr.

	H387
	Polyvinyl Acetate (Solid)
	1 Kg
	1
	
	Vinyl Acetate Monomer (99.9%)
	1.03 kg

	H388
	Sulphonated Polyethylene Terephthalate Powder/Flakes
	1 kg
	1
	
	Diethylene Glycol
	0.259 kg

	
	
	
	2
	
	Dimethyl Terephthalate
	0.731 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.265 kg

	
	
	
	4
	
	5-Sulfo Dimethyl Isophthalate Sodium Salt
	0.131 kg

	H389
	Injection Moulding High Impact Polystyrene Razor Handles
	1 kg
	1
	
	High Impact Polystyrene Granules
	1.03 kg

	
	
	
	2
	
	Relevant Colour Master Batch
	0.02 kg

	H390
	Plastic Sieve
	1 kg
	1
	
	Polypropelene Moulding Powder/Granules
	1.05 kg/kg content in the export product.

	
	
	
	2
	
	Relevant Nylon Net
	1.05 kg/kg content in the export product.

	
	
	
	3
	
	Tin Plate Waste
	1.05 kg/kg content in the export product.

	H391
	Plastic Hangers
	1 kg
	1
	
	Relevant Plastic Moulding Powder/Granules i.e. PP/HIPS/ABS
	1.05 kg/kg content in export product.

	
	
	
	2
	
	(A) Non-Alloy CRCA Sheet/Slip for metal Clips 
OR


Relevant Metal Clips
	1.05 kg/kg content of metal clips contained in the export product 

Net + 2% wastage

	
	
	
	3
	
	Non-Alloy Steel Wire
	1.01 kg/kg content in the export product

	H392
	Phenol Formaldehyde Knobs with/without Brass/Steel Inserts
	1 kg
	1
	
	Phenolic Moulding Powder
	1.10 kg/kg content in export

	
	
	
	2
	
	Relevant Inserts
OR
Non Alloy Steel Rod
OR
Brass
	Net + 1 % wastage.

1.15kg/kg content in the export.
1.05 kg/kg content in the export.

	H393
	Nylon 6- monofilament Yarn with 20%(by weight) Nylon 6-66 Copolymer(length 2.00 meter and dia 0.5 mm and above) for long lining (commercial fishing)
	1 kg
	1
	
	Nylon 6-chips
	0.880 kg

	
	
	
	2
	
	Nylon 6-66 Copolymer chips
	0.220 kg

	
	
	
	3
	
	Antioxidant
	0.002 kg

	
	
	
	4
	
	Surface Active Agent
	0.001 kg

	
	
	
	5
	
	Finish Oil
	0.001 kg

	H394
	Nylon-6 Monofilament Yarn with 20% Nylon 6-66 Copolymer
	1 kg
	1
	
	Nylon 6-chips
	0.84 kg

	
	
	
	2
	
	Nylon 6-6 copolymer chips
	0.21 kg

	
	
	
	3
	
	Antioxidant
	0.002 kg

	
	
	
	4
	
	Surface Active Agent
	0.001 kg

	
	
	
	5
	
	Finish Oil
	0.001 kg

	H395
	Thermoplastic Rubber Sole
	1 kg
	1
	
	Relevant Thermoplastic Granules (TPR Granules)
	1.035 kg

	H396
	Phenol Formaldehyde Resin
	1 kg
	1
	
	Phenol
	0.843 kg

	
	
	
	2
	
	Paraformaldehyde Powder/Flakes
	0.242 kg

	H397
	Plastic Moulded Luggage Fittings with or without Metallic components in various types and sizes
	1 kg
	1
	
	Any of the following Polymer or in combination with other Polymers with or without Metallic components:
	

	
	
	
	2
	
	Metallic Components
	Net+1% wastage

	H398
	Deleted
	
	
	
	
	

	H399
	Cross Laminated Multi Layer Film
	1 kg
	1
	
	LLDPE Granules
	0.720 kg

	
	
	
	2
	
	HM HDPE Granules
	0.405 kg

	
	
	
	3
	
	U.V. Stabilizer
	0.025 kg

	Note: In case of export product made out of cross laminated multi layer plastic film i.e. tarpaulins, covers, bags, sacks, an additional quantity of 5% in the above raw material may be allowed.

	H400
	Cross Linked Polystryene (Stryene-Divinyl Benzene Co-polymer)
	1 kg
	1
	
	Stryene Monomer
	1.106 kg

	
	
	
	2
	
	Di-Vinyl Benzene
	0.070 kg

	
	
	
	3
	
	Poly Vinyl Alcohol
	0.018 kg

	H401
	Deleted
	
	
	
	
	

	H402
	Mariners mat made of Polythylene/ Polypropylene (Natural, Beige & Coloured)
	1 kg
	1
	
	Relevant Polyethylene/ Polypropylene Monofilament rope (Natural, Beige & coloured) 3 strand, Z Twist, 9.5 mm diametre
	1.02 kg/kg content in the export product.

	H403
	Polyester Staple Fibre/Polyester Tow/Polyester Tops
	1 kg
	1
	
	PET chips/Flakes
	1.05 kg

	
	
	
	2
	
	Carbon Black
	0.0184 kg

	
	
	
	3
	
	Spin Finish Oil
	0.01 kg

	H404
	Printed flexible packaging material of one layer or printed or unprinted adhesive laminated/extrusion laminated/extrusion laminated flexible packaging material of multilayers of relevant substrate with or without hotmel in the form of rolls/strips/sheets/labels/wrappers or in pouch form.
	1 kg
	1
	a)
	Polyethylene Film
	

	
	
	
	
	b)
	Polyester Film
	

	
	
	
	
	c)
	Metallised Polyester Film
	

	
	
	
	
	d)
	BOPP Film
	

	
	
	
	
	e)
	Metallised BOPP Film/ Cast Polypropylene Film
	

	
	
	
	
	f)
	Cellophane Film
	

	
	
	
	
	g)
	Pearlised BOPP Film
	

	
	
	
	
	h)
	PVC Film
	

	
	
	
	
	I)
	Aluminium Foil
	

	
	
	
	
	j)
	CPP (Cast Polypropylene) Film
	

	
	
	
	
	k)
	LDPE Granules (for extrusion coating)
	

	
	
	
	
	l)
	Metallised PVC Film
	

	
	
	
	
	m)
	Paper of various types & grammage
	

	
	
	
	
	n)
	Metalised CPP (Cast Polypropylene) Film
	

	
	
	
	
	o)
	PVC Heat Shrinkable Film
	

	
	
	
	
	p)
	BOPP Heat Sealable Film
	

	
	
	
	
	
	Relevant substrate(various types, thickness & grades) of either one or in combination of more than one layer of any of the following items:-
	Quantity as per the formula below + wastage.

	
	
	
	2
	
	Liquid Printing Ink (total solid 25% +/- 3%)
	10 gms/ Sq. Mtr + wastage.

	
	
	
	3
	
	Liquid Polyurethane Adhesive (total Solid 60% +/- 5%)
	4.0 gms/ Sq. Mtr. + wastage.

	
	
	
	4
	
	Liquid Polyurethane Additive (total Solid 50% +/- 5%)
	0.4 gms/ Sq. Mtr.

	
	
	
	5
	
	Relevant Hotmelt
	Actual Grammage + wastage.

	H405
	White Pulverised Powder(containing minimum 92% of LDPE)
	1 kg
	1
	
	LDPE Granules
	0.935 kg

	
	
	
	2
	
	Titanium Dioxide
	0.085 kg

	H406
	Nylon Twine
	1 kg
	1
	
	Nylon Filament Yarn
	1.02 kg

	H407
	PVC Lace Table covers with film backing (square/rectangular type)
	1 Sq. Mtr. (Net wt. Of PVC film & coating wt. To be indicated)
	1
	
	PVC Film of relevant thickness
	1.10 kg/kg content in the export product

	
	
	
	2
	
	Raw material per kg plastisol:- 
i)PVC Resin 
ii)PVC Plasticizer 
iii)PVC Stabilizer 
iv)Pigments
	
0.603 kg
0.510 kg
0.012 kg
0.035 kg

	H408
	PVC Lace Table covers with film backing(Circular/Oval type)
	1 Sq. Mtr. (Net weight of PVC coating wt. To be indicated)
	1
	
	PVC Film of Relevant thickness
	1.30 kg/kg content in the export product.

	
	
	
	2
	
	Raw material per 1 kg Plastisol:-
i)PVC Resin
ii)PVC Plasticizer
iii)PVC Stabilizer
iv)Pigments
	
0.696 kg
0.572 kg
0.013 kg
0.034 kg

	H409
	PVC Crochet Table Cover with film backing (square/rectangular/Circular/Oval type)
	1 Sq. Mtr. (Net wt. Also to be indicated)
	1
	
	PVC Resin
	0.624 kg

	
	
	
	2
	
	PVC Plastcizer
	0.528 kg

	
	
	
	3
	
	PVC Stabilizer
	0.012 kg

	
	
	
	4
	
	Pigments
	0.036 kg

	H410
	PVC Lace Table Mats/Coasters/Doilesy
	1 Sq. Mtr. (Net wt. to be indicated)
	1
	
	PVC Film of Relevant thickness
	1.32 kg/kg content in the export product.

	
	
	
	2
	
	Raw material for 1 kg Plastisol (coating weight)
i)PVC Resin
ii)PVC Plasticizer
iii)PVC Stabilizer
iv)Pigments
	

0.676 kg
0.572 kg
0.013 kg
0.039 kg

	Note:(1) The applicant shall declare the coating weight in the export product and in the application for the licence.(2) In case of Rectangular product the quantity of PVC Film would be reduced to 1.10 kg/kg content in the export product.

	H411
	PVC Metallic Mat
	1 Sq. Mtr.
	1
	
	Relevant PVC Metallic Film
	1.08 kg/kg content in the export product

	H412
	PVC with Non-Woven Backing Film Apron
	1 No.
	1
	
	PVC Film with Non-Woven Poly Propelene Film Backing
	1.08 kg/kg content in the export product

	H413
	PVC Laundry Bag
	1 No.
	1
	
	Relevant PVC Film
	1.08 kg/kg content in the export product

	H414
	Flame Retardant HDPE Tarpaulin (with 3% UV Stabilizer Master Batch)
	1 kg
	1
	
	HDPE Granules
	0.57 kg

	
	
	
	2
	
	LDPE Granules
	0.38 kg

	
	
	
	3
	
	UV Stabilizer Master Batch
	0.11 kg

	
	
	
	4
	
	Flame Retardant Additive
	0.08 kg

	H415
	Article made of SAN Resin (Styrene Acrylonitrile Resin)
	1 kg
	1
	
	SAN Resin (Styrene Acrylonitrile Resin)
	1.05 kg/kg content in the export product

	H416
	Plastic Sharpeners
	1 No.
	1
	
	Relevant Polymer viz. Polystyrene (GPPS/HIPS)/Acrylic/ABS powder granules
	1.05 kg/kg content in the export product

	
	
	
	2
	
	CRCA Blade
OR
CRCA Strip
	Net to net

1.10 kg/kg weight of Blade in Export

	
	
	
	3
	
	Screws
OR
Steel Wire for Screws
	Net to net

1.10 kg/kg weight of Screws in Export

	H417
	Prepared Adhesives Base on Plastics (Two Component Laminating Adhesives)
A. Adhesive (80% resin content and 20% solvent)
B. Additive (50% resin content and 50% solvent)
	1 kg
	1
	
	Adipic Acid
	0.130 kg

	
	
	
	2
	
	Isophthalic Acid
	0.373 kg

	
	
	
	3
	
	Monoethylene Glycol
	0.069 kg

	
	
	
	4
	
	Diethylene Glycol
	0.281 kg

	
	
	
	5
	
	1,6 Hexanediol
	0.022 kg

	
	
	
	6
	
	Ethyl Acetate/ Methyl Ethyl Ketone (relevant)
	0.200 kg

	
	
	
	7
	
	Adipic Acid
	0.011 kg

	
	
	
	8
	
	Isophthalic Acid
	0.035 kg

	
	
	
	9
	
	Monoethylene Glycol
	0.030 kg

	
	
	
	10
	
	Diethylene Glycol
	0.057 kg

	
	
	
	11
	
	1,6 Hexanediol
	0.002 kg

	
	
	
	12
	
	Ethyl Acetate
	0.500 kg

	
	
	
	13
	
	Toluene Di isocyanate 4,4 Diphenylmethane Di Isocyanate (MDI) (relevant)
	0.372 kg

	Note: Items 1 to 6 is for 1 Kg weight of product (A) & items 7 to 13 is for 1 Kg weight of Product (B).

	H418
	Deleted
	
	
	
	
	

	H419
	Drip Bateral of 13 mm ID, Wall thickness 1.25 mm having inline hold of 3.2 mm at 75 mm equal distance made out of LLDPE & LDPE in 500 mts Roll.
	1 kg
	1
	
	LLDPE Granules
	0.6615 kg

	
	
	
	2
	
	LDPE Granules
	0.3297 kg

	
	
	
	3
	
	Relevant Master Batch
	0.0588 kg

	H420
	Cast Polypropylene Film (Transparent)
	1 kg
	1
	
	Polypropylene Granules
	1.10 kg

	H421
	Cast Polypropylene Film (White Opaque)
	1 kg
	1
	
	Polypropylene Granules
	0.88 kg

	
	
	
	2
	
	Polypropylene master batch containing 55+/- Titanium Dioxide
	0.22 kg

	H422
	Nylon-6 Dipped Tyre Cord Fabric
	1 MT
	1
	
	Nylon-6 Yarn
	1.02 MT

	
	
	
	2
	
	VP Latex
	40 kg

	H423
	PVDC coated PVC film (containing 0.900 kg PVC film and 0.100 kg PVDC coating)
	1 kg
	1
	
	PVC Film
OR
	0.990 kg

	
	
	
	1
	a)
	PVC Resin
	0.8217 kg

	
	
	
	
	b)
	Epoxidised Soyabean Oil
	0.0545 kg

	
	
	
	
	c)
	PVC Stabilizer
	0.0297 kg

	
	
	
	
	d)
	Pigment
	0.0049 kg

	
	
	
	
	e)
	PVC processing aid
	0.0158 kg

	
	
	
	
	f)
	PVC Impact modifier
	0.1010 kg

	
	
	
	
	g)
	Lubricant
	0.0119 kg

	
	
	
	2
	
	Coating materials:
	

	
	
	
	
	a)
	PVDC aqueous dispersion (Total solids 55+/-2%
	0.0204 kg

	
	
	
	
	b)
	Aqueous dispersion of vinylidene chloride)(Total Solid content 60+/-1%)
c) Aqueous dispersion Vinylidenns chloride- Methacrylate Copolymer (Total Solid Content 55+/-1%)
OR
	0.1447 kg


0.0217 kg.

	
	
	
	2
	a)
	Primer - PVDC Dispersions (Total Solid content 50%+/-2%)
	0.0077 kg

	
	
	
	
	b)
	Hardner for PVDC Dispersion (Total solid content 75%+/-2%)
	0.0001 kg

	
	
	
	
	c)
	Aqueous Dispersion of PVDC (Total Solid Content 55%+/-1%)
	0.1929 kg

	
	
	
	
	d)
	Ethyl Acetate Solvent
	0.040 kg

	

	

	Note: 1. In case of variation in the weight of PVC film the qty. of items of import at S.No. 1 or 1(a to g) shall be worked out adopting the following formula:- 
AXB/C
Where A= Quantity allowed for 0.900 kg of PVC film.
B = Weight of PVCfilm in one kg of export product
C =0.900=Note: 2. Increase of variation in the weight of PVDC coating in the export product, the quantity of inputs at S.No. 2 (a to c) and 2 (a to d) shall be worked out by adopting the following:
DXE/F
where D = quantity allowed for 0.100 kgPVC coating
E = Weight of PVDC coating in the export product
F = 0.100
Note: 3. In case of variation in the solid content of solid content at S.No. 2 quantity shall be worked out on pro-rata basis.

	H424
	Special Sealant IM 3000 (Themocuring Acrylic Resin containing min. 92% (by wt.) Hydroxy propyl metha acrylate)
	1 kg
	1
	
	Hydroxy Propyl Metha Acrylate
	0.933 kg

	H425
	EPDM Rubber Grade H-545
	1 MT
	1
	
	Ethylene
	489 kgs

	
	
	
	2
	
	Propylene
	425 kg

	
	
	
	3
	
	Ethylidene norbornene
	108.36 kg

	
	
	
	4
	
	Hexane
	74.52 kg

	
	
	
	5
	
	Ethyle Aluminium Sesquichloride
	16.625 kgs

	
	
	
	6
	
	Vanadium Oxytrichloride
	2.25 kg

	
	
	
	7
	
	Polypropylene Glycol
	6.00 kg

	
	
	
	8
	
	Anti Oxidant
	1.71 kg

	H426
	Linear Low Density Polyethylene/ LLDPE - (Octene Based)
	1 MT
	1
	
	Ethylene
	0.951 MT

	
	
	
	2
	
	Octene-I
	0.135 MT

	
	
	
	3
	
	Cyclohexane
	0.01452 MT

	
	
	
	4
	
	CAB-2/Diethyl aluminum Chloride/ Tri-isobutyl Aluminium or equivalent
	0.000518 MT

	
	
	
	5
	
	PG Parlgonic Acid/ PD Acetyl acetone/ or equivalent
	0.002229 MT

	
	
	
	6
	
	Activated Alumina
	0.009505 MT

	
	
	
	7
	
	Antioxidants/ Silica MB (40%)/ Slip/ Viton MB(5%) or equivalent
	0.008675 MT

	H427
	PVDC coated PVC film (containing 0.900 kg PVC film and 0.100 kg PVDC coating)
	1 kg
	1
	
	PVC film
OR
	0.990 kg

	
	
	
	1
	a)
	PVC Resin
	0.8217 kg

	
	
	
	
	b)
	Epoxidised Soya bean oil
	0.0545 k g

	
	
	
	
	c)
	PVC Stabilizer
	0.0297 kg

	
	
	
	
	d)
	Pigment
	0.0049 kg

	
	
	
	
	e)
	PVC processing aid
	0.0158 kg

	
	
	
	
	f)
	PVC Impact modifier
	0.1010 kg

	
	
	
	
	g)
	Lubricant
	0.0119 kg

	
	
	
	2
	
	Coating Materials
	

	
	
	
	
	a)
	PVDC aqueous dispersion (total Solids 55+/-2%)
	0.0204 kg

	
	
	
	
	b)
	Aqueous dispersion of Vinylidene chloride (total Solid content 60+/-1%)
	0.1447 kg

	
	
	
	
	c)
	Aqueous dispersion Vinylidenns/ chloride - Meth Acrylate Copolymer (total Solid Content 55+/-1%)
OR
	0.0217 kg

	
	
	
	2
	a)
	Primer -PVDC dispersions in Ethyl acetate (total solid content 50+/-2%)
	0.0224 kg

	
	
	
	
	b)
	Hardner -PVDC dispersions in Ethyl acetate (total Solid content 75+/-2%)
	0.1158 kg

	
	
	
	
	c)
	Aqueous dispersion of Vinylidene Chloride - Meth acrylate Copolymer (Total Solid content 55+/-1%)
	0.0217 kg

	
	
	
	
	d)
	Ethyl Acetate Solvent
	0.0400 kg

	Note 1. In case of variation in the weight of PVC film, the quantity of items of import of at Sl. No. 1 or 1 (a) to (g) shall be worked out adopting the following :
AXB/C
Where A= Quantity allowed for 0.900 kg. Of PBVC film,
B=Weight of PVC film in one kg of export product, and C = 0.900Note: 2. In case of variation in the weight of PVDC coating in the export product, the quantity of inputs at S.No. 2(a) to (c ) and 2(a) to (d) shall be worked out by adopting the following:
DXE/F
Where D= quantity allowed for 0.100 kg PVC coating
E= Weight of PVDC coating in the export product F=0.100
Note: 3. In case of variation in the solid content of solid content at S.No. 2 quantity shall be worked out on pro-rata basis.

	H428
	Thermoplastic Rubber Compound, Footwear Grade (containing 66+/-1% SBS Oil bound copolymer & 14+/-1% Polystrene)
	1 kg
	1
	
	Styrene Butadiene Styrene Oil bound copolymer
	0.6656 kg

	
	
	
	2
	
	Napthenic Oil
	0.1050 kg

	
	
	
	3
	
	Polystyrene High Impact (HIPS)
	0.0450 kg

	
	
	
	4
	
	Polystyrene General Purpose (GPPS)
	0.0950 kg

	
	
	
	5
	
	Antioxidants
	0.0050 kg

	H429
	Textile/ Polyester (Yarn Braided Thermoplastic Hose)
	1 kg
	1
	
	Relevant Tyride/ Polyester Elastomer (Hytrel/ OR Arnitel)/ Polyamide/ Polyurethane Resin
	1.05 kg/kg content in the export product

	
	
	
	2
	
	Relevant Polyester Yarn
	1.05 kg/kg content in the export product

	H430
	Wire Braided Thermoplastic Hose/ Jack Gose/ Sewer Jetting Hose
	1 kg
	1
	
	Relevant Tyride/ Polyester Elastomer (Hytrel/ OR Arnitel)/ Polyamide/ Polyurethane Resin
	1.05 kg/kg content in the export product

	
	
	
	2
	
	Relevant High tensile Brass coated Steel Wire
	1.05 kg/kg content in the export product

	H431
	Polyisocyanate (Pale Yellow translucent solid Melting point 85-103 deg C Isocyanate content 11%-13%)
	1 kg
	1
	
	Tri Methylol Propane
	0.144 kg

	
	
	
	2
	
	Phenol
	0.354 kg

	
	
	
	3
	
	Toluene Di Isocyanate
	0.562 kg

	H432
	Slitted PVDC Coated Rigid PVC film/ Slitted Rigid PVC Film
	1 kg
	1
	
	Relevant PVDC Coated rigid PVC Film Jumbo rolls /Rigid PVC film Jumbo Rolls
	1.03 kg

	H433
	Plastic Knitting Pins/Needles including reinforced Plastic Knitting Pins/ Needles made of Cellulose Acetate
	1 kg
	1
	
	Cellulose Acetate Moulding Powder or Cellulose Acetate Granules
	1.10 kg/kg content in the export product

	H434
	Epoxite Novalac Resin Powder (Softening Point - 110 +/- 5 Degree Centigrade)
	1 MT
	1
	
	Bisphenol - A
	0.91 MT

	H435
	Epoxite Novalac Resin Powder (Softening Point - 110 +/- 5 Degree Centigrade)
	1 MT
	1
	
	Bisphenol - A
	0.91 MT

	H436
	Non- Pyrogenic Non- Toxic Sterilized Single/ Double/ Triple Blood Bag 450 ML with anti coagulant Citrate Phosphate Dextrose Adenine Solution
	1 No.
	1
	
	Relevant PVC Film (Frosted/ TOTM)
	1.05 sq.mtr./sq. mtr. content in the export product

	
	
	
	2
	
	Relevant PVC Tubings
	1.05 mm content in the export product

	
	
	
	3
	
	Multi Layer Film
	1.05 sq. mtr./sq. mtr. content in the export product

	
	
	
	4
	
	Hot Stamping Foil
	1.03 sq. mtr./sq. mtr. content in the export product

	
	
	
	5
	
	Twist of Ports/ Snap of Ports/ Y-Site
	1.03 Nos./1 No. in the export product

	
	
	
	6
	
	Needle (16 gauge)
	1.03 Nos./1 No. content in the export product

	
	
	
	7
	
	Dextrose (Monohydrate)
	Net + 2% wastage.

	
	
	
	8
	
	Craft paper
	As per Packing Policy

	H437
	Double sided PVC Coated Polyester Fabrics (with Coating weight of 1000 Gms/ Sq. mtr. And with Base Fabric/ weight of 217 gms) Tolerance +/-7.5% on the total coated fabric weight
	1 sq. mtr.
	1
	
	Raw Material:
	

	
	
	
	
	a)
	Polyester Industrial Yarn
OR
	260 gms

	
	
	
	1
	b)
	Unprocessed Wover Polyester fabrics
OR
	1.17 sq. mtr.

	
	
	
	1
	c)
	Polyester Wrap Knitted fabrics
	1.17 sq. mtr.

	
	
	
	2
	
	PVC Resin
	570.60 gms

	
	
	
	3
	
	DOP/DIDP/DNIP
	405.30 gms

	
	
	
	4
	
	Stabilizer (Tinbase, BaZn. Ba/Ca)
	11.58 gms

	
	
	
	5
	
	Ranuvin P/T inuvin P
	1.52 gms

	
	
	
	6
	
	Pigments
	19.90 gms

	
	
	
	7
	
	Calcium carbonate
	142.74 gms

	
	
	
	8
	
	Expoxidised Soyabean Oil
	11.58 gms

	
	
	
	9
	
	Bonding Agent (Vulcabond-E)
	6.78 gms

	Note: 1. In the case of variation in the weight of Base Fabric, the quantity of yarn imports covered under 1(a) will be arrived by adopting the following formula:
i.e.AXB/217
Where A= Quantity of Polyester Yarn allowed (B) weight of base fabric in PVC coated Polyester fabric to be exported/sq. meter
Note: 2. In the case of variation in coating weight, the quantity of import under items Nos. 2 to 8 will be arrived at by adopting the following formula:
i.e.CXD/1000
Where C= Quantity allowed for 1000 gms. Coating weight per Sq. meter
(D) Coating weight of PVC Coated Polyester Fabric to be exported/sq. meter
Note: 3 There will be no change in the quantity of item No. 9 i.e. Bonding Agent with change in the Coating weight.
Note: 4. In case of export of "Double side PVC Coated Polyester fabricated covers/Tarpaulins/Cricket pitch covers (Tolerance of +/-7.7% on the total coated fabric weight), the quantity for all items at S.Nos. 1 to 9 allowed for Double side PVC Coated Polyester fabrics will be arrived by multiplying with 1.05

	H438
	Multilayer Foiless Plastic Laminated tubes with or without Caps (5 Ply printed)
	1 kg
	1
	
	LDPE Granules
	1.17 kg/kg content in the export product

	
	
	
	2
	
	LLDPE Granules
	1.17 kg/kg content in the export product

	
	
	
	3
	
	Polyester Film
	1.12 kg/kg content in the export product

	
	
	
	4
	
	Master Batch (70% Titanium Di-oxide)
	1.12% of weight of LDPE Granules in the export product.

	
	
	
	5
	
	U.V.Ink
	0.5% of weightof LDPE/LLDPE in the export product

	
	
	
	6
	
	U.V. Varnish
	0.3% of weight of LDPE/LLDPE in the export product

	
	
	
	7
	
	HDPE Granules (for Shoulder of tubes)
	1.05 kg/kg content in the export product

	
	
	
	8
	
	Polypropylene Granules (for caps)
	1.05 kg/kg content in the export product

	H439
	Aluminium Metallized PVC Film
	1 kg
	1
	
	PVC Film
	1.10 kg

	
	
	
	2
	
	Aluminium Wire
	0.0246 kg

	
	
	
	3
	
	Induction/ Evaportion Boats
	0.007 Nos.

	H440
	Aluminium Metallized BOPP Film
	1 kg
	1
	
	BOPP Film
OR
Polypropylene Resin/ Granules
	1.10 kg

1.32 kg

	
	
	
	2
	
	Aluminium Wire
	0.0246 kg

	
	
	
	3
	
	Induction/ Evaporation Boats
	0.007 No.

	H441
	Artificial X MAS Trees
	1 No.
	1
	
	Relevant PVC Film
	1.05 kg/kg content in the export product

	
	
	
	2
	
	PVC Coated GI Wire/ GI pipe
	1.02 kg/kg content in the export product

	
	
	
	3
	
	ABS Granules
	1.05 kg/kg content in the export product

	
	
	
	4
	
	Kraft Paper / Chromoart Paper
	As per packing Policy

	H442
	Alkyl Phenol Resin Super Beackacite 100
	1 kg
	1
	
	Para Tertiary Butyl Phenol
	0.833 kg

	
	
	
	2
	
	Para Formaldehyde (Purity 91% +/- 1%)
	0.240 kg

	H443
	Polypropelene (Homo Polymer)
	1 MT
	1
	
	Propylene
	1.03 MT

	
	
	
	2
	
	Active Shac-103
	0.069 kg

	
	
	
	3
	
	Triethyl Aluminium
	0.208 kg

	
	
	
	4
	
	PEER (SCA)
	0.139 kg

	
	
	
	5
	
	Antioxidants:
Irgonox-11-/ Irgonox-3114/ Ethanox-330/ Ultranox-626/ Irgofos-168 or Irgonox-1330
	
1.717 kgs

	
	
	
	6
	
	Additives:
Hydrotalcite DHT-4A/ Erucamide/ Olemide/ Gasil AB-720/ Glyceryl Mono Sterate (Myverol 18-6) Zinc Oxide/ Acrawax
	
2.500 kgs

	H444
	Asceptic Packaging of Aluminium Foil of thickness less than 0.2 mm backed by paper & LDPE with/without Polypropylene/ MPM Strips
	1 MT 1 MT
	1
	
	Relevant Duplex Paper Board/ Bleached Paper / Bleached Paper Board/ Kraft Paper
	1.10 MT/ MT content in the export product.

	
	
	
	2
	
	Aluminium Foil
	1.10 MT/ MT content in the export product.

	
	
	
	3
	
	LDPE Granules
	1.10 MT/ MT content in the export product.

	
	
	
	4
	
	LLDPE/ HDPE/MLLDPE Granules
	1.12 MT/ MT content in the export product.

	
	
	
	5
	
	Ethylene Acrylic Acid Copolymer/Adhesive Copolymer Granules
	1.12 MT/ MT content in the export product.

	
	
	
	6
	
	Relevant Polypropylene Strips Modified Poly Metallosene Strips
	Net to net

	
	
	
	7
	
	Printing Ink
	12 kgs./MT of export product

	
	
	
	8
	
	Photo Polymer plates
	0.5 No./MT of export product

	H445
	Poly Vinyl Formal Resin
	1 kg
	1
	
	Vinyl Acetate Monomer
	1.690 kg

	
	
	
	2
	
	Paraformaldehyde
	0.462 kg

	
	
	
	3
	
	Poly Vinyl Alcohol
	0.100 kg

	H446
	P.P. Woven Sacks with/ without Liner or with/ without U.V. Stabilization (2% by weight) or with/ without Lamination with Kraft Paper or with/ without stiched with P.P. Yarn
	1 kg
	1
	
	P.P. Granules (For export without U.V. Stabilization)
OR
	1.10 kg/kg content in the export item.

	
	
	
	1
	a)
	P.P. Granules
	1.10 kg/kg content in the export item.

	
	
	
	
	b)
	U.V. Stabilizer (For export with U.V. Stabilizer)
	0.022 kg

	
	
	
	2
	
	Relevant PP/ LDPE Granules for liner/ coating
	1.05 kg/kg content in the export item.

	
	
	
	3
	
	Relevant Kraft Paper
	1.05 kg/kg content in the export item.

	
	
	
	4
	
	Relevant P.P. Yarn for stiching
	1.05 kg/kg content in the export item.

	H447
	P.P. Woven Fabrics with/ without U.V. Stabilization (2% by weight)
	1 kg
	1
	
	P.P. Granules
	1.058 kg

	
	
	
	2
	
	U.V. Stabilizer
	0.022 kg

	H448
	ION Exchange Resin (Mix Bed) Strong Acid Cation Exchange Resin 60 parts & Strong Base Anion Exchange Resin 40 parts
	1 Cubic Ft.
	1
	
	Styrene
	7.93 kgs

	
	
	
	2
	
	Divinyl Benzene
	0.48 kg

	
	
	
	3
	
	Ethylene Dichloride
	3.98 kgs

	
	
	
	4
	
	Paraformaldehyde
	2.74 kgs

	
	
	
	5
	
	Ethylene Glycol Dimethacrylate
	0.29 kg

	H449
	Deleted
	
	
	
	
	

	H450
	Plastic Files/ Folders/ Laver Arch Files
	1 No.
	1
	
	Relevant PVC/ Polypropylene Sheet
	1.05 kg/ kg content in the export product.

	
	
	
	2
	
	Relevant Book Binding Board
	1.05 kg/ kg content in the export product.

	
	
	
	3
	
	Relevant components as contained in the export product:
	

	
	
	
	
	a)
	Paper Filling Machanism
	Net to net.

	
	
	
	
	b)
	Metal Rado Slots
	Net to net.

	
	
	
	
	c)
	Metal Fingerings
	Net to net.

	
	
	
	
	d)
	Metal Riverts
	Net to net.

	H451
	PVC Folder/ Polypropylene Files/ Zip Lock Bag
	1 No.
	1
	
	Relevant PVC/ Polypropylene Sheet
	1.05 kg/ kg content in the export product.

	
	
	
	2
	
	Relevant Book Binding Board
	1.05 kg/ kg content in the export product.

	
	
	
	3
	
	Relevant components as contained in the export product:
	

	
	
	
	
	a)
	Paper Filling Machanism
	Net to net.

	
	
	
	
	b)
	Metal Rado Slots
	Net to net.

	
	
	
	
	c)
	Metal Fingerings
	Net to net.

	
	
	
	
	d)
	Metal Riverts
	Net to net.

	H452
	Opaque White Polyester Chip
	1 kg
	1
	
	DMT
	0.819 kg

	
	
	
	2
	
	MEG
	0.297 kg

	
	
	
	3
	
	Barium Sulphate
	0.185 kg

	
	
	
	4
	
	DMIP
	0.014 kg

	
	
	
	5
	
	Antifoam
	0.00001 kg

	
	
	
	6
	
	Calcium Acetate
	0.0007 kg

	
	
	
	7
	
	Maganese Acetate
	0.000125 kg

	
	
	
	8
	
	TPP
	0.0014 kg

	H453
	Silicone Polymer RS-103 (Trimethyl Sliyl Vinyl Methyl Polysiloxame)
	1 kg
	1
	
	Residual Polymer Mixture (Average content - 95%)
	1.2 kg

	H454
	PVC Braided Hoses with Synthetic Yarn (Nylon/ Polyester)
	1 kg
	1
	
	PVC Resin
	0.7 kg

	
	
	
	2
	
	Dioctyl Ophthalate
	0.250 kg

	
	
	
	3
	
	PVC Stabilizer
	0.030 kg

	
	
	
	4
	
	Relevant Synthetic Yarn (Nylon/ Polyester)
	0.070 kg

	Note: 1. The quantity of inputs at Sl.No.1, 2 & 3 are for PVC Compound weight of 933 gms in the export product. For any variation in the PVC compound weight the item at Sl.No.1, 2 & 3 shall be allowed adopting the following formula:
A x B/933
Where A = Quantity allowed for 933 gms PVC Compound
B = Weight of PVC compound in the export product.
2. The quanitity of relevant Synthetic Yarn at Sl.No. 4 is 67 gms of Yarn in theproduct. For any variation in the relevant Yarn weight, the relevant Yarn shall be allowed adopting the following formula:
C x D/67
Where C = Quantity allowed for 67 gms Yarn content in the export product.
D = Weight of relevant Synthetic Yarn in the export product.

	H455
	Polyvinyl Butyral Resin
	1 kg
	1
	
	Poly Vinyl Alcohol
	0.710 kg

	
	
	
	2
	
	N-Butyraldehyde
	0.429 kg

	H456
	BOPP Bags with/ without Adhesives Tape
	1 kg
	1
	
	BOPP Film (relevant thickness and grade)
	1.02 kg/ kg content in export product.

	
	
	
	2
	
	Double Side Self-adhesive Tape(only if exported with Adhesive Tape)
	1.02 kg/ kg content in export product.

	H457
	Polytetrafluoro Ethylene Dispension (Emulsion Grade, TFE content 59.5% +/- 0.5%)
	1 MT
	1
	
	Chloroform
	4.75 MT

	
	
	
	2
	
	Perfluoro-Octanic Acid (FC-Z6)
	0.0075 MT

	
	
	
	3
	
	Anhydrous Hydro Fluoric Acid
	1.42 MT

	H458
	Articles made of Polyester (PET/ PBT)
	1 kg
	1
	
	Relevant Polyester (PET/ PBT Resin)
	1.05 kg/ kg content in the export product.

	H459
	Polypropylene (Co-polymer) Resin
	1 MT
	1
	
	Propylene
	0.980 MT

	
	
	
	2
	
	Ethylene
	0.070 MT

	
	
	
	3
	
	Active Shac-103
	0.064 MT

	
	
	
	4
	
	Triethyl Aluminium
	0.215 kg

	
	
	
	5
	
	PEEB (SCA)
	0.173 kg

	
	
	
	6
	
	Antioxidant: Irgonox-1010/ Irgonox-3114/ Ethanox-330/ Ultranox-626/ Igofos-168
	1.486 kg

	
	
	
	7
	
	Additives: Zinc Oxide/ Hydrotal Cite DHT-4A/ Myverol 18-6 (GSM)/ Millad-3988
	1.821 kg

	H460
	Integral Drip Leteral with in line Dripper (OD 16 mm, Wall thickness 0.99 mm)
	100 Mtrs. (approx. weight 4.734 kgs)
	1
	
	LLDPE
	3.367 kgs

	
	
	
	2
	
	LDPE
	1.421 kg

	
	
	
	3
	
	Colour Master Batch
	0.305 kg

	H461
	Prepared adhesives based on Plastic (Two component Laminating Adhesives) Adhesive (Polyurethane solution containing 60% Resin content and 40% Solvent)
	1 kg
	1
	
	Adipic Acid
	0.090 kg

	
	
	
	2
	
	Isophthalic Acid
	0.258 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.050 kg

	
	
	
	4
	
	Diethylene Glycol
	0.195 kg

	
	
	
	5
	
	1,6-Hexane Diol
	0.015 kg

	
	
	
	6
	
	Toluene Di-iso-cyanate
	0.035 kg

	
	
	
	7
	
	Ethyl Acetate/ Methyl Ethyl Ketone (Relevant)
	0.400 kg

	H462
	Prepared Adhesives based on Plastics (Two component Laminating Adhesives)consisting of:-
A. Adhesive (Polyurethane Solution containing 66% Resin content and 34% Solvent)and
B. Additive (Poly Isocyanate Solution containing 50%Solid and 50% Solvent)
	1 kg
	1
	
	Adipic Acid
	0.103 kg

	
	
	
	2
	
	Isophthalic Acid
	0.297 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.055 kg

	
	
	
	4
	
	Diethylene Glycol
	0.224 kg

	
	
	
	5
	
	1,6-Hexane Diol
	0.018 kg

	
	
	
	6
	
	Toluene Di-Isocyanate
	0.038 kg

	
	
	
	7
	
	Ethyl Acetate/ Methyl Ethyl Ketone (relevant)
	0.340 kg

	
	
	
	8
	
	Adipic Acid
	0.012 kg

	
	
	
	9
	
	Isophthalic Acid
	0.037 kg

	
	
	
	10
	
	Mono Ethylene Glycol
	0.032 kg

	
	
	
	11
	
	Diethylene Glycol
	0.060 kg

	
	
	
	12
	
	1,6-Hexane Diol
	0.002 kg

	
	
	
	13
	
	Toluene Di-Isocyanate
	0.372 kg

	
	
	
	14
	
	Ethyl Acetate/ Methyl Ethyl Ketone (relevant)
	0.500 kg

	Note: Items at Sl.Nos.1 to 7 are per kg weight of Adhesive and items at Sl.Nos. 8 to 14 are per kg weight of additive.

	H463
	Prepared Adhesives based on Plastics (Two component Laminating Adhesives)consisting of
A. Adhesive (Polyurethane Solution containing 25% Resin content and 75% Solvent)and
B. Additive (Poly Isocyanate Solution containing 50%Solid and 50% Solvent)
	1 kg
	1
	
	Adipic Acid
	0.039 kg

	
	
	
	2
	
	Isophthalic Acid
	0.113 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.021 kg

	
	
	
	4
	
	Diethylene Glycol
	0.085 kg

	
	
	
	5
	
	1,6-Hexane Diol
	0.007 kg

	
	
	
	6
	
	Toluene Di-Isocyanate
	0.015 kg

	
	
	
	7
	
	Ethyl Acetate/ Methyl Ethyl Ketone (relevant)
	0.750 kg

	
	
	
	8
	
	Adipic Acid
	0.012 kg

	
	
	
	9
	
	Isophthalic Acid
	0.037 kg

	
	
	
	10
	
	Mono Ethylene Glycol
	0.032 kg

	
	
	
	11
	
	Diethylene Glycol
	0.060 kg

	
	
	
	12
	
	1,6-Hexane Diol
	0.002 kg

	
	
	
	13
	
	Toluene Di-Isocyanate
	0.372 kg

	
	
	
	14
	
	Ethyl Acetate/ Methyl Ethyl Ketone (relevant)
	0.500 kg

	Note: Items at Sl.Nos.1 to 7 are per kg weight of Adhesive and items at Sl.Nos. 8 to 14 are per kg weight of additive.

	H464
	PVC Shower Curtains
	1 kg
	1
	
	Relevant PVC Film
	1.06 kg/ kg content in the export product.

	H465
	Synthetic Acrylic Resin Emulsion (having Solid content 59% +/- 1%)
	1 kg
	1
	
	Butyl Acrylate
	0.5768 kg

	
	
	
	2
	
	Metha Acrylic Acid
	0.0116 kg

	
	
	
	3
	
	Potassium Persulphate
	0.0027 kg

	H466
	Polyvinyl Acetal Resins
	1 kg
	1
	
	Polyvinyl Alcohol
	0.660 kg

	
	
	
	2
	
	N Buraldehyde
	0.155 kg

	
	
	
	3
	
	3-Hydroxy Benzaldehyde
	0.396 kg

	
	
	
	4
	
	Propylene Glycol Monomethyl Ether
	9.00 kgs

	H467
	PVC Granulated Compound (Gasket/ Crown Cork Liner Grade)
	1 kg
	1
	
	PVC Resin
	0.530 kg

	
	
	
	2
	
	DOP Plasticiser
	0.405 kg

	
	
	
	3
	
	Epoxidised Soyabean Oil
	0.017 kg

	
	
	
	4
	
	PVC Stabilizer
	0.028 kg

	
	
	
	5
	
	Processing Aid
	0.020 kg

	
	
	
	6
	
	Calcium Carbonate
	0.020 kg

	
	
	
	7
	
	Pigments
	0.010 kg

	
	
	
	8
	
	Antioxidant
	0.020 kg

	H468
	PVC Erasers
	1 kg
	1
	
	PVC Resin
	0.258 kg

	
	
	
	2
	
	D.O.P.
	0.366 lg

	
	
	
	3
	
	Calcite Powder
	0.416 kg

	
	
	
	4
	
	Titanium Dioxide
	0.010 kg

	H469
	Poly Ether Sulfone
	1 kg
	1
	
	Phenol
	0.745 kg

	
	
	
	2
	
	Methanol
	0.116 kg

	
	
	
	3
	
	Dichloro Diphenyl Sulfone
	0.685 kg

	
	
	
	4
	
	Sulfolane Aqueous (2,3,4,5 Tetrahydro Thiophene 1,1 Dioxide)
	0.140 kg

	H470
	Polysulphide Sealant containing 26% (by weight) Polysulphide Polymer
	1 MT
	1
	
	Liquid Hydrocarbon Resin
	12.24 kgs

	
	
	
	2
	
	Polysulphide Polymer
	265.20 kgs

	
	
	
	3
	
	Maganese Oxide
	25.50 kgs

	
	
	
	
	
	
	

	H471
	Polyacetal Resin Compound
	1 MT
	1
	
	Polyacetal Resin (Fluff)
	1021.54 kgs

	
	
	
	2
	
	Polacrylamide
	6.54 kgs

	
	
	
	3
	
	Eva Co-polymer
	1.56 kg

	
	
	
	4
	
	Polyethylene Glycol
	9.05 kgs

	
	
	
	5
	
	Antioxidant (Irganox)
	1.04 kg

	
	
	
	6
	
	Artificial Wax
	0.25 kg

	H472
	Polyurethane Arm Resets/ Seats/ Backs
	1 kg
	1
	
	Polyol (Premixed with 12% Blowing Agent)
	0.79 kg/ kg of Polyurethane content in the export product.

	
	
	
	2
	
	Isocyanate (MDI)
	0.35 kg/ kg of Polyurethane content in the export product.

	
	
	
	3
	
	Inmould Spray Paint/ Lacquer
	0.028 kg/ kg of Polyurethane content in the export product.

	H473
	Polyurethane Resin (containing 30% Resin/ Total Solid content in MEK/ IPA/ Toluene Solvent)
	1 MT
	1
	
	Polyol
	238.40 kgs

	
	
	
	2
	
	Di-Isocyanate
	52.40 kgs

	
	
	
	3
	
	Tri-Ethylene Diamine
	0.12 kg

	
	
	
	4
	
	Diamine
	16.67 kgs

	
	
	
	5
	
	Methyl Ethyl Ketone
	287.87 kgs

	
	
	
	6
	
	Toluene
	287.87 kgs

	
	
	
	7
	
	Isopropyl alcohol
	142.40 kgs

	
	
	
	8
	
	Monoethnol Amine
	0.65 kg

	H474
	Polybutylene Terephthalate Compound
	1 kg
	1
	
	Polycarbonate
	0.46 kg

	
	
	
	2
	
	Polybutylene Terephthalate
	0.39 kg

	
	
	
	3
	
	Additives (Heat Stabilizers - Phosphite based, Sulfide based; Light Stabilizers - Benzotriazole based; Stabilizers - Phosphate based, Epoxy based; Anti Oxidants - Phenolic based; Proscessing Aids - Sterates;Flame Retardant Sulphonate based, Bromine, Anti Dripping Agent - PTFE based - SB203, MBS Rubber, SVS Rubber)
	0.17 kg

	
	
	
	4
	
	Pigments (Chromium Oxide, Green, Iron Oxide, Carbon Black, Titanium Dioxide, Thiphene Brightner, Anthraquinone - Blue/ Green, Quinophtaine Yellow, Styrol Yellow,Quinacridone - Red, Oerylene - Red, Perylene - Red)
	0.024 kg

	Note: 1. The Poly Butylene Terephthalate is based on 37% +/- 1% and Polycarbonate is based on 44% +/- 1% content. In case of any variation, the quantity shall be calculated on pro-rata basis.
2. Combination of various Additives and Pigments is to be permitted within the quantities indicated against each.

	H475
	Polycarbonate Compound
	1 kg
	1
	
	TNPP (Tris(nonyl Phenol) Phosphite)
	0.00105 kg

	
	
	
	2
	
	Tinuvin 234 {2-(2H-Benz-Otriazol-2-yl)-4-6, Bis (1-Methyl-1Phenylethyl) Phenol)
	0.10500 kg

	
	
	
	3
	
	Polycarbonate Powder
	0.94374 kg

	
	
	
	4
	
	Colorant (Relevant)
OR
	0.00021 kg

	
	
	
	1
	
	Tris (Di-butylpheneil) Phos
	0.00053 kg

	
	
	
	2
	
	UVA 1577 {2-(4,6 Diphenyl-1,3,50 Triaz in-2yl) 5-(Hexy) Oxy-Phenol}
	0.04725 kg

	
	
	
	3
	
	Polycarbonate Powder
	1.00219 kg

	
	
	
	4
	
	Colorants (Relevant)
OR
	0.00003 kg

	
	
	
	1
	
	Polycarbonate Resin
	1.0430 kg

	
	
	
	2
	
	Additives (Heat Stabilizers - Phosphite based; Light Stabilizers - Benzotriazole based; Stabilizers - Epoxy based, Phosphite based; Anti Oxidants - Phenolic based; Proscessing Aids - Silicone Oil , Sterates;Flame Retardant - Phosphate based, Sulphonate based, Bromine based; Anti Dripping Agent - PTFE based)
	0.0047 kg

	
	
	
	3
	
	Pigments (Chromium Oxide, Green, Iron Oxide, Carbon Black, Titanium Dioxide, Thiophene Brightner, Anthraquinone - Violet/ Green, Quinophtaine Yellow, Styrol Yellow,Quinacridone - Red, Anthrapyridone Red Dye, Thio Indigo Dye compound, Phtalprinone Red Dye, Imide Derivatives)
	0.0018 kg

	Note: 1. The Polycarbonate Compound is based on 99.5% +/- 0.5% Polycarbonate Resin content. In case of any variation, the quantity shall be calculated on pro-rata basis.
2. Combination of various Additives and Pigments is to be permitted within the quantities indicated against each.

	H476
	Glass Reinforced Polybutylene Terephthalate Compound
	1 kg
	1
	
	Polybutylene Terephthalate
	0.597 kg

	
	
	
	2
	
	Additives (Heat Stabilizers -Sulfide based, Phosphite based, Epoxy based, Phosphate based; Light Stabilizers - Benzotriazole based; Anti Oxidants - Phenolic based;Proscessing Aids - Sterates; Flame Retardant - Sulphonate based/ Bromine based; Anti Dripping Agent - PTFE based - SB203)
	0.21 kg

	
	
	
	3
	
	Pigments (Chromium Oxide, Green, Iron Oxide, Carbon Black, Titanium Dioxide, Thiophene Brightner, Anthraquinone - Violet/ Green/ Yellow/ Red, Solvent Red; Phtalocyanine - Quinophtaine Yellow, Styrol Yellow,Blue/ Green, Quinophtaine Yellow, Styrol Perylene - Red,Methine Orange Dye, Anthrapyridone Red Dye, Thio Indigo Dye compound, Phtalprinone Red Dye, Imide Derivatives)
	0.019 kg

	
	
	
	4
	
	Glass Fibre
	0.224 kg

	Note: 1. The Poly Butylene Terephthalate is based on 57% +/- 1% and Additives are based on 20% +/- 1% content. In case of any variation, the quantity shall be calculated on pro-rata basis.
2. Combination of various Additives and Pigments is to be permitted within the quantities indicated against each.

	H477
	Glass Reinforced Modified Poly Phenylene Oxide (PPO) Compound
	1 kg
	1
	
	Poly Phenylene Oxide (PPO)
	0.310 kg

	
	
	
	2
	
	Additives (Heat Stabilizers -Sulfide based; Light Stabilizers - Benzotriazole based; Anti Oxidants - Phenolic based;Proscessing Aids - Sterates; Flame Retardant - Sulphonate based/ Bromine based; Anti Dripping Agent - PTFE based - SB203)
	0.042 kg

	
	
	
	3
	
	Pigments (Chromium Oxide, Green, Iron Oxide, Carbon Black, Titanium Dioxide, Thiophene Brightner, Anthraquinone - Violet/ Green/ Yellow/ Red, Solvent Red; Phtalocyanine - Quinophtaine Yellow, Styrol Yellow,Blue/ Green, Quinophtaine Yellow, Styrol Perylene - Red,Methine Orange Dye, Anthrapyridone Red Dye, Thio Indigo Dye compound, Phtalprinone Red Dye, Imide Derivatives)
	0.010 kg

	
	
	
	4
	
	Glass Fibre
	0.210 kg

	
	
	
	5
	
	High Impact Polystyrene
	0.480 kg

	Note: 1. The export product input quantities have been worked out with Poly Phenylene Oxide 30% +/- 1%, High Impact Polystyrene 45% +/- 1% and Glass Fibre 20% +/- 1% content. In case of any variation, the quantity shall be calculated onpro-rata basis.
2. Combination of various Additives and Pigments is to be permitted within the permitted within the quantities indicated against each.

	H478
	Glass Reinforced Polycarbonate Compound
	1 kg
	1
	
	Polycarbonate Resin
	0.898 kg

	
	
	
	2
	
	Additives (Heat Stabilizers -Sulfide based; Light Stabilizers - Benzotriazole based; Anti Oxidants - Phenolic based;Proscessing Aids - Sterates; Flame Retardant - Sulphonate based/ Bromine based; Anti Dripping Agent - PTFE based - SB203)
	0.026 kg

	
	
	
	3
	
	Pigments (Carbon Black, Titanium Dioxide)Blue/ Green, Quinophtaine Yellow, Styrol Perylene - Red,Methine Orange Dye, Anthrapyridone Red Dye, Thio Indigo Dye compound, Phtalprinone Red Dye, Imide Derivatives)
	0.009 kg

	
	
	
	4
	
	Glass Fibre
	0.117 kg

	Note: 1. The Polycarbonate Compound is based on 85% +/- 1% Polycarbonate Resin content and 11% +/- 1% Glass Fibre content. In case of any variation, the quantity shall be calculated on pro-rata basis.
2. Combination of various Additives and Pigments is to be permitted within the permitted within the quantities indicated against each.

	H479
	Polypropylene (Homo-polymer)
	1 MT
	1
	
	Naphtha
	1.273 MT

	
	
	
	2
	
	Active SHAC-103
	0.069 kg

	
	
	
	3
	
	Triethyl Aluminium
	0.208 kg

	
	
	
	4
	
	PEEB (SCA)
	0.139 kg

	
	
	
	5
	
	Antioxidants (Irgonox-1010/ Irgonox-3114/ Ethanox-330/ Ultranox-6261 Irgophos-168)
	1.717 kg

	
	
	
	6
	
	Additives (Dydrotalcite/ DHT-4A/ Emcamide/ Oleamide/ Gasil/ AB-720/ Glyceryl Mono Stearate (Myverol 18-6)/ Zinc Oxide/ Acrowax)
	2.500 kgs

	H480
	Ethyl Acrylate Homo-polymer Emulsion having solid 35% +/- 1% Stabilized with Emulsifier
	1 kg
	1
	
	Ethyl Acrylate
	0.327 kg

	
	
	
	2
	
	Itaconic Acid
	0.015 kg

	H481
	Methyl Methacrylate Homo-polymer in Solid form
	1 kg
	1
	
	Methyl Methacrylate
	1.009 kg

	H482
	Ethyl Acrylate and Methyl Methacrylate Copolymer Emulsion having Solid 35% +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Ethyl Acrylate
	0.291 kg

	
	
	
	2
	
	Methyl Methacrylate
	0.031 kg

	
	
	
	3
	
	Methacrylic Acid
	0.005 kg

	
	
	
	4
	
	Methacrylamide
	0.005 kg

	
	
	
	5
	
	Acrylamide
	0.004 kg

	H483
	Ethyl Acrylate and Methacrylic Acid Copolymer Aqueous Solution with Solid content 22% +/- 1%
	1 kg
	1
	
	Methacrylic Acid
	0.085 kg

	
	
	
	2
	
	Ethyl Acrylate Monomer
	0.132 kg

	H484
	Aqueous Polyurethane Dispersion having Solid 20% +/- 2%
	1 kg
	1
	
	Isophorane Di-Isocyanate
	0.060 kg

	
	
	
	2
	
	Dicarboxylic Acid
	0.044 kg

	
	
	
	3
	
	Phthalic Anhydride
	0.030 kg

	
	
	
	4
	
	Neopentone Glycol
	0.069 kg

	
	
	
	5
	
	Dimethylol Propionic Acid
	0.014 kg

	H485
	Butyl Acrylate and Ethyl Acrylate Copolymer Emulsion having Solid 40% +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Butyl Acrylate
	0.138 kg

	
	
	
	2
	
	Ethyl Acrylate
	0.171 kg

	
	
	
	3
	
	Acrylamide
	0.003 kg

	H486
	EVA Polymer Based Adhesive in Solid form (containing 45% +/- 1% EVA, 27% +/- 1% Ester Gum & 20% +/- 1% Paraffin Wax)
	1 kg
	1
	
	Ethylene Vinyl Acetate (Solid Copolymer)
	0.458 kg

	
	
	
	2
	
	Ester Gum
	0.274 kg

	
	
	
	3
	
	Paraffin Wax
	0.204 kg

	H487
	Vinyl Acetate Copolymer Emulsion Stabilized with Colloid
	1 kg
	
	
	A) For Solid content 54 +/- 1%
	

	
	
	
	1
	
	Vinyl Acetate Monomer
	0.315 kg

	
	
	
	2
	
	Hydroxy Ethyl Cellulose
OR
	0.018 kg

	
	
	
	
	
	B) For Solid content 48 +/- 1%
	

	
	
	
	1
	
	Vinyl Acetate Monomer
	0.294 kg

	
	
	
	2
	
	Hydroxy Ethyl Cellulose
	0.019 kg

	Note: The two variations in the solid contents are due to different materials. The input quantities are specific quantities and not the pro-rata quantities. The applications therefore have to be considered either as per A or B as per applicants declaration.

	H488
	Styrene and Butadiene Copolymer Emulsion with Solids 48 +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Styrene
	0.221 kg

	
	
	
	2
	
	Acrylic Acid
	0.005 kg

	H489
	Butyl Acrylate and Acrylonitrile Copolymer Emulsion having Solids 45% +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Butyl Acrylate
	0.218 kg

	
	
	
	2
	
	Acrylic Acid
	0.005 kg

	
	
	
	3
	
	Acrylonitrile
	0.200 kg

	
	
	
	4
	
	Acrylamide
	0.013 kg

	H490
	Butyl Acrylate and Methyl Methacrylate Copolymer Emulsion having Solids 55% +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Butyl Acrylate
	0.252 kg

	
	
	
	2
	
	Methyl Methacrylate
	0.279 kg

	
	
	
	3
	
	Acrylamide
	0.003 kg

	
	
	
	4
	
	Methacrylamide
	0.010 kg

	H491
	Ethyl Acrylate and Methacrylic Acid Copolymer Emulsion having Solids 29+/-1% Stabilized with Emulsifier
	1 kg
	1
	
	Methacrylic Acid
	0.114 kg

	
	
	
	2
	
	Ethyl Acrylate
	0.171 kg

	H492
	Styrene and Acrylate Co-polymer Emulsion Stabilized with Emulsifier
	1 kg
	
	
	A) For 50 +/- 1% Solid content:
	

	
	
	
	1
	
	Styrene
	0.231 kg

	
	
	
	2
	
	Butyl Acrylate
	0.239 kg

	
	
	
	3
	
	Acrylic Acid
	0.012 kg

	
	
	
	4
	
	Acryl Amide
OR
	0.007 kg

	
	
	
	
	
	B) For 50 +/- 1% Solid content:
	

	
	
	
	1
	
	Styrene
	0.185 kg

	
	
	
	2
	
	Butyl Acrylate
	0.117 kg

	
	
	
	3
	
	Ethyl Acrylate
OR
	0.167 kg

	
	
	
	
	
	C) For 47 +/- 1% Solid content:
	

	
	
	
	1
	
	Styrene
	0.281 kg

	
	
	
	2
	
	Butyl Acrylate
	0.149 kg

	Note: The three variations in the solid contents are due to different materials. The input quantities are specific quantities and not the pro-rata quantities. The applications therefore have to be considered either as per A, B or C as per applicants declaration.

	H493
	Methacrylic Acid Homopolymer Aqueous Solution with Solids 40% +/- 1%
	1 kg
	1
	
	Methacrylic Acid
	0.335 kg

	H494
	Vinyl Acetate and 2-Ethyl Hexyl Acrylate Copolymer Emulsion with Solids 56% +/- 1% Stabilized with Colloid
	1 kg
	1
	
	2-Ethyl Hexyl Acrylate
	0.135 kg

	
	
	
	2
	
	Vinyl Acetate Monomer
	0.400 kg

	
	
	
	3
	
	Hydroxy Ethyl Cellulose
	0.016 kg

	H495
	Butyl Acrylate and Acrylonitrile Copolymer Emulsion having Solids 40% +/- 1% Stabilized with Emulsifier
	1 kg
	1
	
	Butyl Acrylate
	0.287 kg

	
	
	
	2
	
	Acrylonitrile
	0.056 kg

	H496
	Butyl Acrylate, Ethyl Acrylate and Acrylonitrile Copolymer Emulsion having Solids 40% +/- 1% Stabilized with Emulsifier
	1 kg
	1
	
	Acrylic Acid
	0.006 kg

	
	
	
	2
	
	Acrylonitrile
	0.047 kg

	
	
	
	3
	
	Butyl Acrylate
	0.136 kg

	
	
	
	4
	
	Ethyl Acrylate
	0.168 kg

	
	
	
	5
	
	Methyl Methacrylate
	0.012 kg

	
	
	
	6
	
	Methacrylamide
	0.006 kg

	
	
	
	7
	
	Acrylamide
	0.002 kg

	H497
	Acrylic Acid and Acrylonitrile Copolymer Aqueous Solution with Solids 35% +/- 1%
	1 kg
	1
	
	Acrylic Acid
	0.180 kg

	
	
	
	2
	
	Acrylonitrile
	0.103 kg

	H498
	Ethyl Acrylate and Methyl Methacrylate Copolymer Emulsion with solids 55+/-1% Stablilized and Emulsifier
	1 kg
	1
	
	Ethyl Acrylate
	0.482 kg

	
	
	
	2
	
	Itacnoic Acid
	0.010 kg

	
	
	
	3
	
	Methyl Metha Acrylate
	0.055 kg

	H499
	Synthetic Tanning Agent - Metha acrylic Acid Homopolymer Aqueous Solution:
A. Solid content 30+/-1%
OR
B. Solid content 40+/-1%
	1 kg
	
	
	A. Metha Acrylic Acid
OR
B. Metha Acrylic Acid
	0.212 kg

0.335 kg

	Note: The inputs quantities of Metha Acrylic Acid are specific quantities and not the pro-rata quantities. The applications therefore have to be considered either as per A or B as per applicants declarations.

	H500
	Butyl Acrylate and Ethyl Acrylate Copolymer Emulsion having Solids 50% +/- 1% Stabilized by Emulsifier
	1 kg
	1
	
	Butyl Acrylate
	0.118 kg

	
	
	
	2
	
	Ethyl Acrylate
	0.169 kg

	
	
	
	3
	
	Acrylic Acid
	0.013 kg

	H501
	Hot Melt Pressure Sensitive Adhesives in Solid form containing Hydrocarbon resin 61% +/- 1% & Styrene Isoprene Styrene Synthetic Rubber 26.5% +/- 1%
	1 kg
	1
	
	Hydrocarbon Resin
	0.623 kg

	
	
	
	2
	
	Styrene Isoprene Styrene Synthetic Rubber
	0.270 kg

	H502
	Methacrylic Acid & Acrylonitrile Copolymer Aqueous Solution with Solids 20% +/- 1%
	1 kg
	1
	
	Methacrylic Acid
	0.168 kg

	
	
	
	2
	
	Acrylonitrile
	0.023 kg

	H503
	Solid Epoxy resin (having Epoxy value between 2.1 and 2.4)
	1 kg
	1
	
	Epichlorohydrin
	0.470 kg

	
	
	
	2
	
	Bisphenol-A
	0.750 kg

	H504
	Solvent Based Epoxy resin containing 25% Xylene content (having Epoxy value between 1.5 and 2.2)
	1 kg
	1
	
	Epichlorohydrin
	0.350 kg

	
	
	
	2
	
	Bisphenol-A
	0.560 kg

	
	
	
	3
	
	Xylene
	0.255 kg

	
	
	
	
	
	
	

	H505
	Solid Epoxy Resin (having Epoxy value between 1.1 and 1.4)
	1 kg
	1
	
	Epichlorohydrin
	0.430 kg

	
	
	
	2
	
	Bisphenol-A
	0.757 kg

	H506
	Polyester (PET) Preform
	1 kg
	1
	
	Polyester (PET) Chips
	1.02 kg/kg content in the export product

	H507
	Deleted
	
	
	
	
	

	H508
	Self Adhesive Tear Tape/ Tear Off Ribbon width 1.00 mm - 9.00 mm minimum length 1000 meters
	1 kg
	1
	
	MOPP/BOPP Film
	0.830 kg

	
	
	
	2
	
	Acrylic Synthetic Emulsion/ Water Based Adhesive (Solid content 55% +/- 10%)
	0.640 kg

	
	
	
	3
	
	Release Coat
OR
	0.016 kg

	
	
	
	
	1)
	Pancakes of Self Adhesive Tear Tape/ Tear Off Ribbon (width range 25.1 mm - 1050 mm)
	1.07 kg

	
	
	
	
	2)
	Relevant Bobbin
	Net to net

	H509
	Printed / Design Self Adhesive Tear Tape / Tear Off Ribbon width 1.00 mm - 9.00 mm minimum Length 1000 meters
	1 kg
	1
	
	MOPP / BOPP Film
	0.835 kg

	
	
	
	2
	
	Acrylic Synthetic Emulsion / Water Based Adhesive (Solid content 55% +/- 10%)
	0.645 kg

	
	
	
	3
	
	Release Coat
	0.017 kg

	
	
	
	4
	
	Printing Ink (Solid content 40% +/- 10%)
	0.077 kg

	
	
	
	5
	
	Additive
	0.007 kg

	
	
	
	6
	
	Thinner
OR
	0.039 kg

	
	
	
	
	1)
	Pancakes of Printed / Design Self Adhesive Tear Tape/ Tear Off Ribbon (width Range 25.1 mm - 1050 mm)
	1.09 kg

	
	
	
	
	2)
	Relevant Bobbin
	Net to net

	H510
	Plain Self Adhesive Tear Tape/ Tear Off Ribbon width 9.1 mm - 25.00 mm minimum Length 1000 meters
	1 kg
	1
	
	MOPP/ BOPP Film
	0.816 kg

	
	
	
	2
	
	Acrylic Synthetic Emulsion / Water Based Adhesive (Solid content 55% +/- 10%)
	0.627 kg

	
	
	
	3
	
	Release Coat
	0.016 kg

	H511
	Pancakes of Self Adhesive Tear Tape/ Tear Off Ribbon width 25.1 mm - 1050 mm
	1 kg
	1
	
	MOPP/ BOPP Film
	0.775 kg

	
	
	
	2
	
	Acrylic Synthetic Emulsion/ Water Based Adhesive (Solid content 55% +/- 10%)
	0.595 kg

	
	
	
	3
	
	Release Coat
	0.015 kg

	H512
	PVC Sole for Hawai Chappal (without Filler)
	1 kg
	1
	
	PVC Compound without filler (Hawai Chappal Grade)
OR
1. a) PVC Resin (Suspension Grade)
	1.03 kg


0.752 kg

	
	
	
	
	
	b) Dioctyl Phthalate Plasticizer (DOP)
	0.280 kg

	
	
	
	
	
	c) Di-iso-Decyl Phthalate Plasticizer (DIDP)
	0.032 kg

	
	
	
	
	
	d) Lead Stabilizer
	0.011 kg

	H513
	HDPE Telecom Duct
	1 kg
	1
	
	HDPE Resin
	1.003 kg

	
	
	
	2
	
	Silicore
	0.037 kg

	
	
	
	3
	
	Colour Master Batch
	0.009 kg

	
	
	
	4
	
	White Master batch
	0.001 kg

	
	
	
	5
	
	Cord Strap
	As per packing policy

	
	
	
	6
	
	Buckles
	As per packing policy

	
	
	
	7
	
	Polyester Strap
	As per packing policy

	
	
	
	8
	
	Printing Ink
	0.04 gms

	
	
	
	9
	
	Solvent for Ink
	0.05 gms

	H514
	Thermoplastic Polyurethane Grade Desmopan 585 U-101
	1 MT
	1
	
	Polyester Polyol 225 B
	475.2 kg

	
	
	
	2
	
	1,4 Butane-Diol
	160.8 kg

	
	
	
	3
	
	MDI (Desmodur TPPU 0118 FUSED)
	310.20 kg

	
	
	
	4
	
	Stabaxol
	2.7 kg

	
	
	
	5
	
	Vinyzene S.B-1 PS
	2.7 kg

	
	
	
	6
	
	Desmopan KA 8551
	10.00 kg

	
	
	
	7
	
	Nacol 18-94
	2.45 kg

	
	
	
	8
	
	Adipic Acid
	109.4 kg

	H515
	Low Density Polyethylene (LDPE)
	1 MT
	1
	
	Ethylene
	1025 kgs

	
	
	
	2
	
	Oleamide (Crodamide)
	0.50 kg

	
	
	
	3
	
	Force Feed Lub Oil
	1.60 kg

	
	
	
	4
	
	LPG
	3.5 kg

	
	
	
	5
	
	Propylene
	10 kgs

	H516
	Hot Melt Adhesive / thermosetting Glue containing 51+ -1% EVA Copolymer, 26 + - 1% Tackifier and 23+ - 1% paraffin/ Sasol Wax
	1 kg
	1
	
	EVA Copolymer
	0.53 kg

	
	
	
	2
	
	Relevant Tackifier Resin/Petroleum Hydrocarbon Resin
	0.27 kg

	
	
	
	3
	
	Relevant Paraffin Wax/Sasol Wax
	0.24 kg

	H517
	GRP (SMC) Moulded Components
	1 kg
	1
	
	Fibre Glass
	0.3675 kg

	
	
	
	2
	
	Low Profile Additive
	0.0975 kg

	
	
	
	3
	
	p-Benzoquinone
	0.0003 kg

	
	
	
	4
	
	Unsaturated Polyester Resin
	0.2280 kg

	
	
	
	5
	
	Catalyst
	0.0079 kg

	
	
	
	6
	
	Wetting and Dispersion Additives
	0.0100 kg

	
	
	
	7
	
	Coathylene Powder
	0.0110 kg

	
	
	
	8
	
	Magnesium Oxide Paste/ Luvitol
	0.0080 kg

	
	
	
	9
	
	Carrier Web Film
	0.0100 kg

	
	
	
	10
	
	Filler (Calcium Carbonate, Aluminium, Tryhydrate etc.)
	0.2900 kg

	
	
	
	11
	
	Release Agents
	0.0110 kg

	
	
	
	12
	
	Pigments
	0.0220 kg

	Note: 1) The export product description should also include the different types of panels exported along with their unit weight and numbers. 
2) The Glass Fibre content in the export product will be 35% +/- 2%. 
3) Against the raw materials imported, wherever items are imported on brand name in addition to the above mentioned description, the brand names are to be indicated below the description of the export item as in above entries in the licences.

	H518
	Poly Methyl Methacrylate Copolymer (White Free Flowing Powder)
	1 kg
	1
	
	Methyl Metha Acrylate
	1.01 kg

	
	
	
	2
	
	Ethyl Metha Acrylate
	0.11 kg

	H519
	Poly Acrylic Acid Complex (White Free Flowing Powder)
	1 kg
	1
	
	Acrylic Acid
	1.03 kg

	
	
	
	2
	
	Triemethylol Propane Triacrylate/ 1,3 Butylene Glycol Diacrylate Santomer
	0.17 kg

	
	
	
	3
	
	Solvent (Benzene/ Toluene)
	3.3 kg

	H520
	Vinyl Acetate Homo-polymer Emulsions Stabilized by Colloids
	1 kg
	
	
	A) For Solid content 44%:
	

	
	
	
	1
	
	Vinyl Acetate Monomer
	0.408 kg

	
	
	
	2
	
	Poly Vinyl Alcohol
OR
	0.024 kg

	
	
	
	
	
	B) For Solid content 46%:
	

	
	
	
	1
	
	Vinyl Acetate Monomer
	0.364 kg

	
	
	
	2
	
	Poly Vinyl Alcohol
	0.021 kg

	
	
	
	3
	
	Diethylene Glycol Dibenzoate
OR
	0.109 kg

	
	
	
	
	
	C) For Solid content 40%:
	

	
	
	
	1
	
	Vinyl Acetate Monomer
	0.373 kg

	
	
	
	2
	
	Poly Vinyl Alcohol
	0.052 kg

	Note: The three variations in the solid contents are due to diferent materials. The input quantities are specific quantities and not the pro-rata quantities. The applications therefore have to be considered either as per A, B or C as per applicants declaration.

	H521
	Ethyl Acrylate and Acrylonitrile Copolymer Emulsion having Solids 45 +/- 1% Stabilized with Emulsifier
	1 kg
	1
	
	Ethyl Acrylate
	0.249 kg

	
	
	
	2
	
	Acrylonitrile
	0.143 kg

	
	
	
	3
	
	Acrylamide
	0.028 kg

	
	
	
	4
	
	Acrylic Acid
	0.004 kg

	H522
	Synthetic Tanning Agent - Acrylic Acid & Acrylonitrile Co-polymer Aqueous Solution Solid content 35 +/- 1%
	1 kg
	1
	
	Acrylic Acid
	0.180 kg

	
	
	
	2
	
	Acrylonitrile
	0.103 kg

	
	
	
	
	
	
	

	H523
	Synthetic Organic Tanning substance consisting of Methacrylic Acid & Acrylonitrile copolymer Aqueous Solution with solids 20+/-1%
	1 kg
	1
	
	Metha Acrylic Acid
	0.168 kg

	
	
	
	2
	
	Acrylonitrile
	0.023 kg

	H524
	Polyurethane Based Adhesive having Solid content 11.5 +/- 0.5% kg
	1 kg
	1
	
	Polyurethane Resins
	0.095 kg

	Note: For any variation in the Solid content the imported raw material content shall be worked out on pro-rata basis.

	H525
	Polyestyrene Foam Products
	1 kg
	1
	
	Expandable Polystyrene Beads
	1.07 kg/kg content in the export product.

	H526
	PVC Compound without Filler (Hawai Chappal Grade)
	1 kg
	1
	
	PVC Resin (Suspension Grade)
	0.734 kg

	
	
	
	2
	
	Dioctyl Phthalate Plasticizer (DOP)
	0.274 kg

	
	
	
	3
	
	Di-Iso-Decyl Phthalate Plasticizer (DIDP)
	0.031 kg

	
	
	
	4
	
	Lead Stabilizer
	0.011 kg

	H527
	Polycarbonate Printed Self Adhesive Labels (Square/ Rectangular)
	1 kg
	1
	
	Relevant Polycarbonate Film/ Sheet (125 micron to 500 micron)
	1.20 kg/kg content in the export product.

	
	
	
	2
	
	Double Sided Adhesive Tape with Release Paper
	1.20 kg/kg content in the export product.

	
	
	
	3
	
	Screen Printing Ink
	0.03 kg (CIF value restricted to 3% of FOB value of exports)

	H528
	Plastic Domes i.e. Polyurethane capped Printed Self Adhesive Labels (other than Square & Rectangular)
	1 kg
	1
	
	Relevant Metallized/ Non-Metallized Polyester/ PVC Self Ashesive Label Stock
	1.40 kg/kg content in the export product.

	
	
	
	2
	
	i) Polyurethane Pre-polymer
	0.55 kg

	
	
	
	
	
	ii)Polyether Polyol Hardener
	0.55 kg

	
	
	
	3
	
	Screen Printing Ink
	0.030 kg (CIF value restricted to 3% of FOB value of exports)

	Note: The item No. 2 (i) & (ii) is allowed for 1 kg of Polyurethane Resin content in the export product.

	H529
	Polycarbonate Printed Self Adhesive Labels for Appliances/ Instruments (Slotted/ circular)
	1 kg
	1
	
	Relevant Polycarbonate Film/ Sheet
	1.35 kg/kg content in the export product.

	
	
	
	2
	
	Double Sided Adhesive Tape with release paper
	1.35 kg/kg content in the export product.

	
	
	
	3
	
	Screen Printing Ink
	0.03 kg (CIF value restricted to 3% of FOB value of exports)

	H530
	PVC/ Polyester Printed Self Adhesive Labels - Square/ Rectangular Shapes (warning/ cautions/ specifications)
	1 kg
	1
	
	Relevant PVC/ Polyester Self Adhesive Label Stock with Release Paper
	1.20 kg/kg content in the export product.

	
	
	
	2
	
	Screen Printing Inks
	0.03 kg (CIF value restricted to 3% of FOB value of exports)

	H531
	Plastic Domes i.e. Polyurethane capped Printed Self Adhesive Labels (Square & Rectangular)
	1 kg
	1
	
	Relevant Metallized/ Non-Metallized Polyester/ PVC Self Adhesive Label Stock
	1.25 kg/kg content in the export product.

	
	
	
	2
	
	i) Polyurethane Pre-polymer
	0.55 kg

	
	
	
	
	
	ii)Polyether Polyol Hardener
	0.55 kg

	
	
	
	3
	
	Screen Printing Ink
	0.030 kg (CIF value restricted to 3% of FOB value of exports)

	Note: The item No. 2 (i) & (ii) is allowed for 1 kg of Polyurethane Resin content in the export product.

	H532
	Flame Retardant High Impact Polystyrene (With MFI<6)
	1 MT
	1
	
	Styrene Monomer
	0.770 MT

	
	
	
	2
	
	Polybutadiene Rubber
	0.071 MT

	
	
	
	3
	
	Mineral Oil
	0.018 MT

	
	
	
	4
	
	Flame Retardant Additive
	0.140 MT

	
	
	
	5
	
	Antimony Trioxide
	0.046 MT

	
	
	
	6
	
	Titanium Dioxide/ Pigment/ Relevant Colour Master Batch
	0.020 MT

	H533
	Flame Retardant High Impact Polystyrene (With MFI>6)
	1 MT
	1
	
	Styrene Monomer
	0.714 MT

	
	
	
	2
	
	Polybutadiene Rubber
	0.066 MT

	
	
	
	3
	
	Mineral Oil
	0.017 MT

	
	
	
	4
	
	Styrene Butadiene Copolymer
	0.082 MT

	
	
	
	5
	
	Flame Retardant Additive
	0.123 MT

	
	
	
	6
	
	Antimony Trioxide
	0.041 MT

	
	
	
	7
	
	Titanium Dioxide/ Pigment/ Relevant Colour Master Batch
	0.020 MT

	H534
	Toughened Polystyrene (S.B. Copolymer)
	1 MT
	1
	
	Styrene Monomer
	0.371 MT

	
	
	
	2
	
	Mineral Oil
	0.006 MT

	
	
	
	3
	
	Styrene Butadiene Copolymer
	0.663 MT

	H535
	Coloured High Impact Polystyrene
	1 MT
	1
	
	Styrene Monomer
	0.942 MT

	
	
	
	2
	
	Polybutadiene Rubber
	0.087 MT

	
	
	
	3
	
	Mineral Oil
	0.022 MT

	
	
	
	4
	
	Titanium Dioxide/Pigment/Relevant Colour Master Batch
	0.025MT

	H536
	Multi-layer Plastic laminated Tubes with / without caps (5 layer printed)
	1 kg
	1
	
	Relevant Plastic Laminated Film (core of Aluminium Foil covered on both sides with Plastic film
	1.12 kg/kg content in the export product

	
	
	
	2
	
	U.V. Ink
	0.5% of weight of multilayer film in the export

	
	
	
	3
	
	U.V Varnish
	0.3% of weight of Multilayer film in the export product

	
	
	
	4
	
	HDPE Granules (for shoulder of the tube)
	1.05 kg/kg content in the export product

	
	
	
	5
	
	Polypropylene Granules (for caps)
	1.05 kg/kg content in the export product

	Note: In case of use of additive / Colour master batches in the shoulder & caps, the relevant additive / Colour master Batch may be allowed as an input 0.02 kg and relevant Polymer at Sl. No. 4 & 5 will be reduced to 1.03 kg/kg content in the export product.

	H537
	Low Density Polyethylene (LDPE)
	1 MT
	1
	
	Propane
	1421 kg

	
	
	
	2
	
	Oleamide
	0.5 kg

	
	
	
	3
	
	Force Feed Lubricating Oil
	1.6 kg

	
	
	
	4
	
	LPG
	3.5 kg

	
	
	
	5
	
	Propylene
	10.0 kg

	H538
	White Opaque BOPP Film
	1 kg
	1
	
	Polypropylene Resin (Homopolymer)
	0.854 kg

	
	
	
	2
	
	Polypropylene Resin (Copolymer)
	0.133 kg

	
	
	
	3
	
	Polypropylene Based Antiblock Compound
	0.002 kg

	
	
	
	4
	
	Polypropylene Based Antistatic Compound
	0.004 kg

	
	
	
	5
	
	Polypropylene based Slip Agent compound
	0.011 kg

	
	
	
	6
	
	Polypropylene based Titanium compound
	0.196 kg

	H539
	BOPP Film "Matte for Third Generation (MTG)"/ "Matte"/ "For Thermo Lamination"
	1 kg
	1
	
	Polypropylene Resin Homopolymer
	1.051 kg

	
	
	
	2
	
	Polypropylene Based Anti Block
	0.012 kg

	
	
	
	3
	
	Polypropylene Based Resin Slip Agent Compound
	0.0118 kg

	
	
	
	4
	
	Polypropylene Based Antistatic Compound
	0.0235 kg

	
	
	
	5
	
	PP Based Matte Compound (Blend of Polypropylene Copolymer and High Density Polyethylene)
	0.1017 kg

	
	
	
	6
	
	LLDPE Resin
	0.1017 kg

	Note : For export of "BOPP" Film Matte for Third Generation (MTG)" : item no 1,2,3,4 & 5 shall be allowed. For export of "BOPP Film Matte" : Item No. 1,2,3 & item No. 5 will be allowed as 0.1252 kg. For export of BOPP Film for Thermo-Lamination" :Item No. 1,2,3,4 & 6 shall be allowed.

	H540
	Plastic (CR 39) Ophthalmic Hard Coated/Multicoated (Antireflection)/Coloured/Edged Lenses
	1 No.
	1
	
	Relevant Plastic (CR-39) Ophthalmic Lenses
	1.05 No.

	H541
	Plain Linoleum Floor Covering 3.2 mm thickness in Sheet or Tiles Form with coating weight of 366 + 3% kg/100 Sq. mtr.
	100 Sq. Mtr.
	1
	
	Wood Powder
	60.94 kgs

	
	
	
	2
	
	Linseed Oil
	124.32 kgs

	
	
	
	3
	
	Gum Rosin
	23.86 kgs

	
	
	
	4
	
	Copal Gum
	2.38 kgs

	
	
	
	5
	
	Titanium Dioxide
	2.4 kgs

	
	
	
	6
	
	Cork Powder
	47.8 kgs

	
	
	
	7
	
	Necires
	1.18 kgs

	
	
	
	
	
	
	

	H542
	Additive (Poly Isocyanate Solution containing 50% Solid and 50% Solvent)
	1 kg
	1
	
	Adipic Acid
	0.012 kg

	
	
	
	2
	
	Isophthalic Acid
	0.037 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.032 kg

	
	
	
	4
	
	Diethylene Glycol
	0.060 kg

	
	
	
	5
	
	1,6-Hexane Diol
	0.002 kg

	
	
	
	6
	
	Toluene Di-iso-cyanate
	0.372 kg

	
	
	
	7
	
	Ethyl acetate/methyl Ethyl Ketone (Relevant)
	0.500 kg

	H543
	Additive (Polyester Solution containing 50% Resin content and 50% Ethyl Acetate)
	1 kg
	1
	
	Adipic Acid
	0.385 kg

	
	
	
	2
	
	Diethylene Glycol
	0.165 kg

	
	
	
	3
	
	Ethyl Acetate
	0.500 kg

	H544
	Synthetic (Plastic) Sport Nets
	1 kg
	1
	
	For 1 kg content of HDPE net content in the export product
	

	
	
	
	
	a)
	HDPE Granules
	1.078 kg

	
	
	
	
	b)
	Relevant Colour Master batch
	0.011 kg

	
	
	
	
	c)
	Anti UV Master batch
	0.011 kg

	
	
	
	2
	
	Relevant PVC Coated Polyester Fabric
	1.05 kg/kg content in the export product

	
	
	
	3
	
	Relevant Grommets
	102 No/100 No content in the export product

	
	
	
	4
	
	Relevant PVC Coated Galvanized Steel Cable
	1.02 kg/kg content in the export product

	
	
	
	5
	
	Relevant Polyester Twine
	1.02 kg/kg content in the export product

	H545
	Polyolefin compound (containing minimum 67+/-1% Polyethylene content
	1 kg
	1
	
	Polyethylene resin Granules (Sp. Gravity 0.85-0.93)
	0.600 kg

	
	
	
	2
	
	EVA Co-polymer granules
	0.030 kg

	
	
	
	3
	
	LDPE Granules
	0.100 kg

	H546
	Synthetic (Plastic) Fishing Nets
	1 kg
	1
	
	Relevant Knotless HDPE Raschel Netting (For bottom of fishing net)
	1.05 kg/kg content in the export

	
	
	
	2
	
	For 1 kg of HDPE Knotted netting content in the export product
	

	
	
	
	
	
	(i) HDPE Granules
	1.06 kg/kg content in the export product

	
	
	
	
	
	(ii) Relevant Colour Master Batch
	0.02 kg

	
	
	
	3
	
	For 1 Kg of PP Twine/ Rope content in the export product
	

	
	
	
	
	
	(i) PP Granules
	1.05 kg/kg content in the export product

	
	
	
	
	
	(ii) Relevant Colour Master Batch
	0.02 kg

	
	
	
	4
	
	Relevant Lead Sinkers
	102 No./100 No. content in the export product

	
	
	
	5
	
	Relevant EVA Floats
	102 No./100 No. content in the export product

	Note: In case of export of coloured items, Relevant "Colour Master Batch" shall be allowed and not in other cases.

	H547
	Prepared Adhesive based on Plastics (Two component Laminating Adhesives) Adhesive (Polyurethane Resin containing 100% Resin)
	1 kg
	1
	
	Adipic Acid
	0.221 kg

	
	
	
	2
	
	Diethylene Glycol
	0.107 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.010 kg

	
	
	
	4
	
	Methyl Propane Diol
	0.100 kg

	
	
	
	5
	
	Diphenyl Methane 4,4 Diisocynate
	0.623 kg

	H548
	Prepared Adhesive based on Plastics (Two component Laminating Adhesives) Additive (Polyester Resin containing 100% Resin)
	1 kg
	1
	
	Adipic Acid
	0.587 kg

	
	
	
	2
	
	Diethylene Glycol
	0.284 kg

	
	
	
	3
	
	Mono Ethylene Glycol
	0.025 kg

	
	
	
	4
	
	Methyl Propane Diol
	0.264 kg


PAGE  
H1

